**Appendix B: Table B**

|  |  |  |  |
| --- | --- | --- | --- |
| Stage | Sample | Location | M:S Ratio (S / (Zn + Metals)) |
| 1 | PS1-2 | Dark | 1.009 |
|  |  | Light | 0.999 |
| 2 | PS2-1 | Dark | 1.047 |
|  |  | Light | 1.005 |
| X | PSX-1 | Darkest red | 1.021 |
|  |  | Yellow | 1.01 |
|  |  | Clear | 1.029 |