data_b2a

_audit_creation_method            SHELXL-97

_chemical_name_systematic

;

?

;

_chemical_name_common             ?

_chemical_melting_point           ?

_chemical_formula_moiety          ?

_chemical_formula_sum

'Ca2 Fe6 Mg0.10 Mn3 O232 P8'

_chemical_formula_weight          1342.25

loop_

_atom_type_symbol

_atom_type_description

_atom_type_scat_dispersion_real

_atom_type_scat_dispersion_imag

_atom_type_scat_source

'O'  'O2-'   0.0080   0.0060

'International Tables Vol C Tables 4.2.6.8 and 6.1.1.4'

'P'  'P'   0.1023   0.0942

'International Tables Vol C Tables 4.2.6.8 and 6.1.1.4'

'Ca'  'Ca'   0.2262   0.3064

'International Tables Vol C Tables 4.2.6.8 and 6.1.1.4'

'Mn'  'Mn'   0.3368   0.7283

'International Tables Vol C Tables 4.2.6.8 and 6.1.1.4'

'Fe'  'Fe'   0.3463   0.8444

'International Tables Vol C Tables 4.2.6.8 and 6.1.1.4'

'Mg'  'Mg'   0.0486   0.0363

'International Tables Vol C Tables 4.2.6.8 and 6.1.1.4'

_symmetry_cell_setting            ?

_symmetry_space_group_name_H-M    ?

loop_

_symmetry_equiv_pos_as_xyz

'x, y, z'

'-x, y+1/2, -z+1/2'

'-x, -y, -z'

'x, -y-1/2, z-1/2'

_cell_length_a                    8.790

_cell_length_b                    11.5380(10)

_cell_length_c                    6.165

_cell_angle_alpha                 90.00

_cell_angle_beta                  99.20

_cell_angle_gamma                 90.00

_cell_volume                      617.21(5)

_cell_formula_units_Z             1

_cell_measurement_temperature     293(2)

_cell_measurement_reflns_used     ?

_cell_measurement_theta_min       ?

_cell_measurement_theta_max       ?

_exptl_crystal_description        ?

_exptl_crystal_colour             ?

_exptl_crystal_size_max           ?

_exptl_crystal_size_mid           ?

_exptl_crystal_size_min           ?

_exptl_crystal_density_meas       ?

_exptl_crystal_density_diffrn     3.611

_exptl_crystal_density_method     'not measured'

_exptl_crystal_F_000              698

_exptl_absorpt_coefficient_mu     5.971

_exptl_absorpt_correction_type    ?

_exptl_absorpt_correction_T_min   ?

_exptl_absorpt_correction_T_max   ?

_exptl_absorpt_process_details    ?

_exptl_special_details

;

?

;

_diffrn_ambient_temperature       293(2)

_diffrn_radiation_wavelength      0.71073

_diffrn_radiation_type            MoK\a

_diffrn_radiation_source          'fine-focus sealed tube'

_diffrn_radiation_monochromator   graphite

_diffrn_measurement_device_type   ?

_diffrn_measurement_method        ?

_diffrn_detector_area_resol_mean  ?

_diffrn_reflns_number             1975

_diffrn_reflns_av_R_equivalents   0.0108

_diffrn_reflns_av_sigmaI/netI     0.0192

_diffrn_reflns_limit_h_min        -12

_diffrn_reflns_limit_h_max        12

_diffrn_reflns_limit_k_min        0

_diffrn_reflns_limit_k_max        16

_diffrn_reflns_limit_l_min        0

_diffrn_reflns_limit_l_max        8

_diffrn_reflns_theta_min          2.35

_diffrn_reflns_theta_max          30.06

_reflns_number_total              1818

_reflns_number_gt                 1618

_reflns_threshold_expression      >2sigma(I)

_computing_data_collection        ?

_computing_cell_refinement        ?

_computing_data_reduction         ?

_computing_structure_solution     'SHELXS-97 (Sheldrick, 2008)'

_computing_structure_refinement   'SHELXL-97 (Sheldrick, 2008)'

_computing_molecular_graphics     ?

_computing_publication_material   ?

_refine_special_details

;

Refinement of F^2^ against ALL reflections.  The weighted R-factor wR and

goodness of fit S are based on F^2^, conventional R-factors R are based

on F, with F set to zero for negative F^2^. The threshold expression of

F^2^ > 2sigma(F^2^) is used only for calculating R-factors(gt) etc. and is

not relevant to the choice of reflections for refinement.  R-factors based

on F^2^ are statistically about twice as large as those based on F, and R-

factors based on ALL data will be even larger.

;

_refine_ls_structure_factor_coef  Fsqd

_refine_ls_matrix_type            full

_refine_ls_weighting_scheme       calc

_refine_ls_weighting_details

'calc w=1/[\s^2^(Fo^2^)+(0.1000P)^2^+0.0000P] where P=(Fo^2^+2Fc^2^)/3'

_atom_sites_solution_primary      direct

_atom_sites_solution_secondary    difmap

_atom_sites_solution_hydrogens    geom

_refine_ls_hydrogen_treatment     mixed

_refine_ls_extinction_method      none

_refine_ls_extinction_coef        ?

_refine_ls_number_reflns          1818

_refine_ls_number_parameters      123

_refine_ls_number_restraints      0

_refine_ls_R_factor_all           0.0260

_refine_ls_R_factor_gt            0.0217

_refine_ls_wR_factor_ref          0.0852

_refine_ls_wR_factor_gt           0.0801

_refine_ls_goodness_of_fit_ref    0.705

_refine_ls_restrained_S_all       0.705

_refine_ls_shift/su_max           4.389

_refine_ls_shift/su_mean          0.038

loop_

_atom_site_label

_atom_site_type_symbol

_atom_site_fract_x

_atom_site_fract_y

_atom_site_fract_z

_atom_site_U_iso_or_equiv

_atom_site_adp_type

_atom_site_occupancy

_atom_site_symmetry_multiplicity

_atom_site_calc_flag

_atom_site_refinement_flags

_atom_site_disorder_assembly

_atom_site_disorder_group

M1CA Ca 0.94359(5) 0.11983(3) 0.83895(7) 0.01645(13) Uani 0.287(10) 1 d P . .

M1MN Mn 0.94359(5) 0.11983(3) 0.83895(7) 0.01645(13) Uani 0.713(10) 1 d P . .

M2 Fe 0.71698(5) 0.07658(4) 0.32918(6) 0.01859(15) Uani 0.905(2) 1 d P . .

M3 Mn 0.36046(4) 0.19106(3) 0.12856(6) 0.01261(13) Uani 1.000(3) 1 d . . .

P1 P 0.09041(6) 0.13579(5) 0.39343(9) 0.00892(15) Uani 1 1 d . . .

P2 P 0.60284(6) 0.08868(5) 0.80688(9) 0.00857(15) Uani 1 1 d . . .

O1 O2- 0.0769(2) 0.06887(15) 0.1767(3) 0.0151(3) Uani 1 1 d . . .

O2 O2- 0.4758(2) 0.17685(15) 0.8306(3) 0.0133(3) Uani 1 1 d . . .

O3 O2- 0.9370(2) 0.19535(18) 0.4158(3) 0.0209(4) Uani 1 1 d . . .

O4 O2- 0.6926(2) 0.12751(15) 0.6259(3) 0.0132(3) Uani 1 1 d . . .

O5 O2- 0.2122(2) 0.23011(16) 0.3788(3) 0.0172(4) Uani 1 1 d . . .

O6 O2- 0.72566(19) 0.08733(15) 0.0145(3) 0.0122(3) Uani 1 1 d . . .

O7 O2- 0.1373(2) 0.06170(16) 0.5966(3) 0.0194(4) Uani 1 1 d . . .

O8 O2- 0.53289(19) -0.03337(15) 0.7606(3) 0.0122(3) Uani 1 1 d . . .

loop_

_atom_site_aniso_label

_atom_site_aniso_U_11

_atom_site_aniso_U_22

_atom_site_aniso_U_33

_atom_site_aniso_U_23

_atom_site_aniso_U_13

_atom_site_aniso_U_12

M1CA 0.0172(2) 0.0117(2) 0.0188(2) -0.00324(13) -0.00230(16) 0.00104(13)

M1MN 0.0172(2) 0.0117(2) 0.0188(2) -0.00324(13) -0.00230(16) 0.00104(13)

M2 0.0180(2) 0.0295(3) 0.0081(2) 0.00009(14) 0.00200(14) 0.00531(15)

M3 0.0144(2) 0.0130(2) 0.01027(19) 0.00025(11) 0.00138(13) 0.00235(12)

P1 0.0085(3) 0.0097(2) 0.0087(3) -0.00054(17) 0.00184(19) -0.00127(17)

P2 0.0085(3) 0.0102(3) 0.0072(3) 0.00007(17) 0.00197(19) 0.00058(17)

O1 0.0192(8) 0.0133(7) 0.0125(8) -0.0047(6) 0.0017(6) 0.0004(6)

O2 0.0128(7) 0.0147(8) 0.0131(8) 0.0013(6) 0.0037(6) 0.0063(6)

O3 0.0120(8) 0.0287(10) 0.0231(9) -0.0064(8) 0.0064(7) 0.0059(7)

O4 0.0136(7) 0.0163(8) 0.0108(7) 0.0004(6) 0.0052(6) -0.0023(6)

O5 0.0212(9) 0.0197(8) 0.0114(7) -0.0004(6) 0.0044(6) -0.0134(7)

O6 0.0087(7) 0.0198(8) 0.0078(7) 0.0006(6) 0.0002(5) 0.0017(6)

O7 0.0270(10) 0.0157(8) 0.0132(8) 0.0052(7) -0.0034(7) -0.0043(7)

O8 0.0125(7) 0.0108(7) 0.0130(7) -0.0004(6) 0.0013(6) -0.0017(6)

_geom_special_details

;

All esds (except the esd in the dihedral angle between two l.s. planes)

are estimated using the full covariance matrix.  The cell esds are taken

into account individually in the estimation of esds in distances, angles

and torsion angles; correlations between esds in cell parameters are only

used when they are defined by crystal symmetry.  An approximate (isotropic)

treatment of cell esds is used for estimating esds involving l.s. planes.

;

loop_

_geom_bond_atom_site_label_1

_geom_bond_atom_site_label_2

_geom_bond_distance

_geom_bond_site_symmetry_2

_geom_bond_publ_flag

M1CA O1 2.1856(18) 3_656 ?

M1CA O3 2.187(2) 4_566 ?

M1CA O1 2.2967(19) 1_656 ?

M1CA O6 2.3758(17) 1_556 ?

M1CA O4 2.3819(18) . ?

M1CA O7 2.529(2) 1_655 ?

M1CA O3 2.742(2) . ?

M1CA O5 2.906(2) 4_666 ?

M1CA P2 2.9917(7) . ?

M1CA P1 3.0968(7) 4_666 ?

M1CA P1 3.2213(7) 1_655 ?

M1CA P1 3.2716(7) 3_656 ?

M1MN O1 2.1856(18) 3_656 ?

M1MN O3 2.187(2) 4_566 ?

M1MN O1 2.2967(19) 1_656 ?

M1MN O6 2.3758(17) 1_556 ?

M1MN O4 2.3819(18) . ?

M1MN O7 2.529(2) 1_655 ?

M1MN M1CA 3.4560(8) 3_757 ?

M1MN M2 3.4773(6) . ?

M1MN M2 3.9084(6) 1_556 ?

M1MN M2 4.0252(7) 4_566 ?

M1MN M2 4.0125(6) 3_756 ?

M2 O6 1.9577(17) . ?

M2 O4 1.9657(17) . ?

M2 O7 2.051(2) 3_656 ?

M2 O8 2.2339(17) 3_656 ?

M2 O3 2.361(2) . ?

M2 P2 3.2188(7) 1_554 ?

M2 P2 3.2626(7) . ?

M2 P1 3.3139(7) 1_655 ?

M2 P1 3.2968(7) 3_656 ?

M2 P2 3.3895(7) 3_656 ?

M2 M3 3.4432(5) . ?

M2 O2 3.4436(19) 3_656 ?

M2 O1 3.4425(19) 1_655 ?

M2 O2 3.5488(19) 4_565 ?

M2 O8 3.5609(17) . ?

M2 O2 3.6327(17) 1_554 ?

M2 O4 3.6314(18) 4_565 ?

M2 O1 3.6896(19) 3_656 ?

M2 O7 3.802(2) 1_655 ?

M2 O8 3.8340(17) 1_554 ?

M2 M1CA 3.9084(6) 1_554 ?

M2 M1MN 3.9084(6) 1_554 ?

M2 P2 3.9872(8) 4_565 ?

M2 O5 3.974(2) 3_656 ?

M2 M1MN 4.0252(7) 4_565 ?

M2 M1CA 4.0252(7) 4_565 ?

M2 O6 4.0398(18) 4_566 ?

M2 M1MN 4.0125(6) 3_756 ?

M2 M1CA 4.0125(6) 3_756 ?

M2 O2 4.1815(17) . ?

M2 M3 4.1651(6) 3_655 ?

M2 O1 4.1992(17) 3_655 ?

M2 O6 4.2152(17) 1_556 ?

M2 O5 4.2741(18) 2_645 ?

M2 O3 4.3284(19) 4_565 ?

M2 O4 4.3463(17) 1_554 ?

M2 O4 4.3476(17) 3_656 ?

M2 O3 4.476(2) 3_756 ?

M3 O5 2.0631(18) 4_565 ?

M3 O8 2.1097(17) 3_656 ?

M3 O2 2.1210(17) 4_565 ?

M3 O5 2.2193(19) . ?

M3 O2 2.2415(17) 1_554 ?

M3 M2 4.1651(6) 3_655 ?

M3 M2 4.5138(7) 2_655 ?

M3 M2 4.7186(6) 4_565 ?

M3 M2 4.6801(6) 3_656 ?

M3 M2 5.5979(5) 4_566 ?

P1 O7 1.5180(18) . ?

P1 O1 1.5312(18) . ?

P1 O3 1.5391(19) 1_455 ?

P1 O5 1.5390(18) . ?

P1 M1CA 3.0968(7) 4_465 ?

P1 M1CA 3.2213(7) 1_455 ?

P1 M1CA 3.2717(7) 3_656 ?

P1 M2 3.3139(7) 1_455 ?

P1 M2 3.2969(7) 3_656 ?

P1 M1CA 3.4604(7) 1_454 ?

P1 M2 5.4988(7) 4_465 ?

P1 M2 5.5792(7) 3_655 ?

P2 O2 1.5347(17) . ?

P2 O4 1.5326(17) . ?

P2 O6 1.5368(18) 1_556 ?

P2 O8 1.5448(18) . ?

P2 M2 3.2188(7) 1_556 ?

P2 M2 3.3895(7) 3_656 ?

P2 M2 3.9872(8) 4_566 ?

O1 M1MN 2.1855(18) 3_656 ?

O1 M1CA 2.1855(18) 3_656 ?

O1 M1CA 2.2967(19) 1_454 ?

O1 M1MN 2.2967(19) 1_454 ?

O1 M2 3.4424(19) 1_455 ?

O1 M2 3.6896(19) 3_656 ?

O1 M2 4.1992(17) 3_655 ?

O2 M3 2.1210(17) 4_566 ?

O2 M3 2.2415(17) 1_556 ?

O2 M2 3.4436(19) 3_656 ?

O2 M2 3.5488(19) 4_566 ?

O2 M2 3.6327(17) 1_556 ?

O3 P1 1.5392(19) 1_655 ?

O3 M1MN 2.187(2) 4_565 ?

O3 M1CA 2.187(2) 4_565 ?

O3 M2 4.3283(19) 4_566 ?

O3 M2 4.476(2) 3_756 ?

O3 M2 4.638(2) 4_565 ?

O4 M2 3.6313(18) 4_566 ?

O4 M2 4.3463(17) 1_556 ?

O4 M2 4.3476(17) 3_656 ?

O5 M3 2.0631(18) 4_566 ?

O5 M1CA 2.906(2) 4_465 ?

O5 M2 3.974(2) 3_656 ?

O5 M2 4.2741(18) 2_655 ?

O5 M2 4.6637(18) 1_455 ?

O6 P2 1.5368(18) 1_554 ?

O6 M1CA 2.3757(17) 1_554 ?

O6 M1MN 2.3757(17) 1_554 ?

O6 M2 4.0398(18) 4_565 ?

O6 M2 4.2152(17) 1_554 ?

O6 M2 4.5352(17) 3_655 ?

O7 M2 2.051(2) 3_656 ?

O7 M1CA 2.529(2) 1_455 ?

O7 M1MN 2.529(2) 1_455 ?

O7 M2 3.801(2) 1_455 ?

O8 M3 2.1097(17) 3_656 ?

O8 M2 2.2340(17) 3_656 ?

O8 M2 3.8340(17) 1_556 ?

loop_

_geom_angle_atom_site_label_1

_geom_angle_atom_site_label_2

_geom_angle_atom_site_label_3

_geom_angle

_geom_angle_site_symmetry_1

_geom_angle_site_symmetry_3

_geom_angle_publ_flag

O1 M1CA O3 167.41(7) 3_656 4_566 ?

O1 M1CA O1 79.14(7) 3_656 1_656 ?

O3 M1CA O1 94.62(7) 4_566 1_656 ?

O1 M1CA O6 78.24(6) 3_656 1_556 ?

O3 M1CA O6 90.23(7) 4_566 1_556 ?

O1 M1CA O6 83.01(6) 1_656 1_556 ?

O1 M1CA O4 87.14(6) 3_656 . ?

O3 M1CA O4 91.66(7) 4_566 . ?

O1 M1CA O4 143.39(6) 1_656 . ?

O6 M1CA O4 60.90(6) 1_556 . ?

O1 M1CA O7 76.60(6) 3_656 1_655 ?

O3 M1CA O7 115.48(7) 4_566 1_655 ?

O1 M1CA O7 100.00(6) 1_656 1_655 ?

O6 M1CA O7 153.56(6) 1_556 1_655 ?

O4 M1CA O7 109.63(6) . 1_655 ?

O1 M1CA O3 106.59(6) 3_656 . ?

O3 M1CA O3 84.21(5) 4_566 . ?

O1 M1CA O3 150.93(6) 1_656 . ?

O6 M1CA O3 125.98(6) 1_556 . ?

O4 M1CA O3 65.60(6) . . ?

O7 M1CA O3 55.67(6) 1_655 . ?

O1 M1CA O5 131.10(6) 3_656 4_666 ?

O3 M1CA O5 56.64(6) 4_566 4_666 ?

O1 M1CA O5 77.65(6) 1_656 4_666 ?

O6 M1CA O5 139.36(6) 1_556 4_666 ?

O4 M1CA O5 133.85(6) . 4_666 ?

O7 M1CA O5 66.00(6) 1_655 4_666 ?

O3 M1CA O5 77.55(6) . 4_666 ?

O1 M1CA P2 78.63(5) 3_656 . ?

O3 M1CA P2 94.05(5) 4_566 . ?

O1 M1CA P2 112.92(5) 1_656 . ?

O6 M1CA P2 30.62(4) 1_556 . ?

O4 M1CA P2 30.54(4) . . ?

O7 M1CA P2 133.69(5) 1_655 . ?

O3 M1CA P2 96.12(4) . . ?

O5 M1CA P2 150.26(4) 4_666 . ?

O1 M1CA P1 160.36(5) 3_656 4_666 ?

O3 M1CA P1 27.60(5) 4_566 4_666 ?

O1 M1CA P1 89.51(5) 1_656 4_666 ?

O6 M1CA P1 116.53(4) 1_556 4_666 ?

O4 M1CA P1 111.05(4) . 4_666 ?

O7 M1CA P1 89.84(5) 1_655 4_666 ?

O3 M1CA P1 76.05(5) . 4_666 ?

O5 M1CA P1 29.49(4) 4_666 4_666 ?

P2 M1CA P1 120.798(19) . 4_666 ?

O1 M1CA P1 93.48(5) 3_656 1_655 ?

O3 M1CA P1 99.04(5) 4_566 1_655 ?

O1 M1CA P1 124.88(5) 1_656 1_655 ?

O6 M1CA P1 149.26(5) 1_556 1_655 ?

O4 M1CA P1 89.42(4) . 1_655 ?

O7 M1CA P1 27.38(4) 1_655 1_655 ?

O3 M1CA P1 28.49(4) . 1_655 ?

O5 M1CA P1 66.87(4) 4_666 1_655 ?

P2 M1CA P1 118.939(19) . 1_655 ?

P1 M1CA P1 79.841(17) 4_666 1_655 ?

O1 M1CA P1 23.29(5) 3_656 3_656 ?

O3 M1CA P1 165.95(6) 4_566 3_656 ?

O1 M1CA P1 99.43(5) 1_656 3_656 ?

O6 M1CA P1 91.91(4) 1_556 3_656 ?

O4 M1CA P1 77.31(4) . 3_656 ?

O7 M1CA P1 61.66(4) 1_655 3_656 ?

O3 M1CA P1 83.30(4) . 3_656 ?

O5 M1CA P1 126.17(4) 4_666 3_656 ?

P2 M1CA P1 80.930(17) . 3_656 ?

P1 M1CA P1 151.119(15) 4_666 3_656 ?

P1 M1CA P1 72.493(18) 1_655 3_656 ?

O1 M1MN O3 167.41(7) 3_656 4_566 ?

O1 M1MN O1 79.14(7) 3_656 1_656 ?

O3 M1MN O1 94.62(7) 4_566 1_656 ?

O1 M1MN O6 78.24(6) 3_656 1_556 ?

O3 M1MN O6 90.23(7) 4_566 1_556 ?

O1 M1MN O6 83.01(6) 1_656 1_556 ?

O1 M1MN O4 87.14(6) 3_656 . ?

O3 M1MN O4 91.66(7) 4_566 . ?

O1 M1MN O4 143.39(6) 1_656 . ?

O6 M1MN O4 60.90(6) 1_556 . ?

O1 M1MN O7 76.60(6) 3_656 1_655 ?

O3 M1MN O7 115.48(7) 4_566 1_655 ?

O1 M1MN O7 100.00(6) 1_656 1_655 ?

O6 M1MN O7 153.56(6) 1_556 1_655 ?

O4 M1MN O7 109.63(6) . 1_655 ?

O1 M1MN M1CA 40.74(5) 3_656 3_757 ?

O3 M1MN M1CA 132.12(6) 4_566 3_757 ?

O1 M1MN M1CA 38.39(4) 1_656 3_757 ?

O6 M1MN M1CA 77.89(4) 1_556 3_757 ?

O4 M1MN M1CA 120.13(5) . 3_757 ?

O7 M1MN M1CA 88.21(4) 1_655 3_757 ?

O1 M1MN M2 77.63(5) 3_656 . ?

O3 M1MN M2 107.73(6) 4_566 . ?

O1 M1MN M2 156.66(5) 1_656 . ?

O6 M1MN M2 90.11(4) 1_556 . ?

O4 M1MN M2 32.95(4) . . ?

O7 M1MN M2 76.73(4) 1_655 . ?

M1CA M1MN M2 118.343(19) 3_757 . ?

O1 M1MN M2 81.86(5) 3_656 1_556 ?

O3 M1MN M2 85.56(5) 4_566 1_556 ?

O1 M1MN M2 61.01(5) 1_656 1_556 ?

O6 M1MN M2 23.06(4) 1_556 1_556 ?

O4 M1MN M2 83.65(4) . 1_556 ?

O7 M1MN M2 153.84(4) 1_655 1_556 ?

M1CA M1MN M2 65.696(15) 3_757 1_556 ?

M2 M1MN M2 113.044(16) . 1_556 ?

O1 M1MN M2 146.01(5) 3_656 4_566 ?

O3 M1MN M2 28.92(5) 4_566 4_566 ?

O1 M1MN M2 114.57(5) 1_656 4_566 ?

O6 M1MN M2 73.21(4) 1_556 4_566 ?

O4 M1MN M2 63.06(4) . 4_566 ?

O7 M1MN M2 126.89(4) 1_655 4_566 ?

M1CA M1MN M2 143.20(2) 3_757 4_566 ?

M2 M1MN M2 84.305(13) . 4_566 ?

M2 M1MN M2 79.078(13) 1_556 4_566 ?

O1 M1MN M2 59.03(5) 3_656 3_756 ?

O3 M1MN M2 130.78(5) 4_566 3_756 ?

O1 M1MN M2 78.29(5) 1_656 3_756 ?

O6 M1MN M2 135.68(4) 1_556 3_756 ?

O4 M1MN M2 122.68(4) . 3_756 ?

O7 M1MN M2 25.70(4) 1_655 3_756 ?

M1CA M1MN M2 62.587(14) 3_757 3_756 ?

M2 M1MN M2 91.583(13) . 3_756 ?

M2 M1MN M2 128.283(12) 1_556 3_756 ?

M2 M1MN M2 150.954(14) 4_566 3_756 ?

O6 M2 O4 158.56(8) . . ?

O6 M2 O7 98.54(7) . 3_656 ?

O4 M2 O7 100.48(7) . 3_656 ?

O6 M2 O8 87.77(7) . 3_656 ?

O4 M2 O8 92.76(7) . 3_656 ?

O7 M2 O8 115.83(7) 3_656 3_656 ?

O6 M2 O3 91.56(7) . . ?

O4 M2 O3 79.82(7) . . ?

O7 M2 O3 86.64(7) 3_656 . ?

O8 M2 O3 157.38(7) 3_656 . ?

O6 M2 P2 20.15(5) . 1_554 ?

O4 M2 P2 148.78(6) . 1_554 ?

O7 M2 P2 109.91(5) 3_656 1_554 ?

O8 M2 P2 67.97(4) 3_656 1_554 ?

O3 M2 P2 108.31(5) . 1_554 ?

O6 M2 P2 163.37(5) . . ?

O4 M2 P2 18.56(5) . . ?

O7 M2 P2 95.91(6) 3_656 . ?

O8 M2 P2 78.54(4) 3_656 . ?

O3 M2 P2 97.47(5) . . ?

P2 M2 P2 144.04(2) 1_554 . ?

O6 M2 P1 84.87(5) . 1_655 ?

O4 M2 P1 94.61(5) . 1_655 ?

O7 M2 P1 64.06(6) 3_656 1_655 ?

O8 M2 P1 172.50(5) 3_656 1_655 ?

O3 M2 P1 24.95(5) . 1_655 ?

P2 M2 P1 104.773(17) 1_554 1_655 ?

P2 M2 P1 108.962(18) . 1_655 ?

O6 M2 P1 117.58(5) . 3_656 ?

O4 M2 P1 82.11(5) . 3_656 ?

O7 M2 P1 19.21(5) 3_656 3_656 ?

O8 M2 P1 111.45(5) 3_656 3_656 ?

O3 M2 P1 88.85(5) . 3_656 ?

P2 M2 P1 127.101(19) 1_554 3_656 ?

P2 M2 P1 76.709(16) . 3_656 ?

P1 M2 P1 71.006(18) 1_655 3_656 ?

O6 M2 P2 87.28(5) . 3_656 ?

O4 M2 P2 100.89(5) . 3_656 ?

O7 M2 P2 94.65(6) 3_656 3_656 ?

O8 M2 P2 21.47(4) 3_656 3_656 ?

O3 M2 P2 178.37(6) . 3_656 ?

P2 M2 P2 70.325(17) 1_554 3_656 ?

P2 M2 P2 83.389(17) . 3_656 ?

P1 M2 P2 155.79(2) 1_655 3_656 ?

P1 M2 P2 92.698(18) 3_656 3_656 ?

O6 M2 M3 78.30(5) . . ?

O4 M2 M3 89.50(5) . . ?

O7 M2 M3 151.45(6) 3_656 . ?

O8 M2 M3 36.32(4) 3_656 . ?

O3 M2 M3 121.62(5) . . ?

P2 M2 M3 60.253(13) 1_554 . ?

P2 M2 M3 85.080(15) . . ?

P1 M2 M3 142.286(19) 1_655 . ?

P1 M2 M3 146.495(19) 3_656 . ?

P2 M2 M3 57.021(13) 3_656 . ?

O6 M2 O2 82.28(6) . 3_656 ?

O4 M2 O2 113.46(6) . 3_656 ?

O7 M2 O2 70.39(6) 3_656 3_656 ?

O8 M2 O2 47.17(5) 3_656 3_656 ?

O3 M2 O2 154.89(6) . 3_656 ?

P2 M2 O2 71.96(3) 1_554 3_656 ?

P2 M2 O2 94.95(3) . 3_656 ?

P1 M2 O2 129.94(3) 1_655 3_656 ?

P1 M2 O2 72.88(3) 3_656 3_656 ?

P2 M2 O2 25.94(3) 3_656 3_656 ?

M3 M2 O2 81.08(3) . 3_656 ?

O6 M2 O1 63.13(6) . 1_655 ?

O4 M2 O1 120.24(6) . 1_655 ?

O7 M2 O1 58.17(6) 3_656 1_655 ?

O8 M2 O1 146.78(5) 3_656 1_655 ?

O3 M2 O1 47.27(5) . 1_655 ?

P2 M2 O1 83.17(3) 1_554 1_655 ?

P2 M2 O1 132.55(3) . 1_655 ?

P1 M2 O1 26.11(3) 1_655 1_655 ?

P1 M2 O1 72.80(3) 3_656 1_655 ?

P2 M2 O1 132.84(3) 3_656 1_655 ?

M3 M2 O1 137.33(3) . 1_655 ?

O2 M2 O1 109.37(4) 3_656 1_655 ?

O6 M2 M1MN 141.18(5) . . ?

O4 M2 M1MN 41.22(5) . . ?

O7 M2 M1MN 70.31(5) 3_656 . ?

O8 M2 M1MN 130.88(5) 3_656 . ?

O3 M2 M1MN 51.83(5) . . ?

P2 M2 M1MN 160.01(2) 1_554 . ?

P2 M2 M1MN 52.585(13) . . ?

P1 M2 M1MN 56.569(14) 1_655 . ?

P1 M2 M1MN 57.684(14) 3_656 . ?

P2 M2 M1MN 129.568(17) 3_656 . ?

M3 M2 M1MN 128.794(15) . . ?

O2 M2 M1MN 124.40(3) 3_656 . ?

O1 M2 M1MN 80.32(3) 1_655 . ?

O6 M2 M1CA 141.18(5) . . ?

O4 M2 M1CA 41.22(5) . . ?

O7 M2 M1CA 70.31(5) 3_656 . ?

O8 M2 M1CA 130.88(5) 3_656 . ?

O3 M2 M1CA 51.83(5) . . ?

P2 M2 M1CA 160.01(2) 1_554 . ?

P2 M2 M1CA 52.585(13) . . ?

P1 M2 M1CA 56.569(14) 1_655 . ?

P1 M2 M1CA 57.684(14) 3_656 . ?

P2 M2 M1CA 129.568(17) 3_656 . ?

M3 M2 M1CA 128.794(15) . . ?

O2 M2 M1CA 124.40(3) 3_656 . ?

O1 M2 M1CA 80.32(3) 1_655 . ?

M1MN M2 M1CA 0.000(13) . . ?

O6 M2 O2 93.99(6) . 4_565 ?

O4 M2 O2 66.67(6) . 4_565 ?

O7 M2 O2 167.13(6) 3_656 4_565 ?

O8 M2 O2 67.39(5) 3_656 4_565 ?

O3 M2 O2 90.13(6) . 4_565 ?

P2 M2 O2 82.93(3) 1_554 4_565 ?

P2 M2 O2 72.15(3) . 4_565 ?

P1 M2 O2 114.53(3) 1_655 4_565 ?

P1 M2 O2 148.43(3) 3_656 4_565 ?

P2 M2 O2 88.82(3) 3_656 4_565 ?

M3 M2 O2 35.28(3) . 4_565 ?

O2 M2 O2 114.493(14) 3_656 4_565 ?

O1 M2 O2 126.64(4) 1_655 4_565 ?

M1MN M2 O2 97.98(3) . 4_565 ?

M1CA M2 O2 97.98(3) . 4_565 ?

O6 M2 O8 149.01(6) . . ?

O4 M2 O8 44.03(6) . . ?

O7 M2 O8 84.16(6) 3_656 . ?

O8 M2 O8 63.86(6) 3_656 . ?

O3 M2 O8 119.44(6) . . ?

P2 M2 O8 131.04(3) 1_554 . ?

P2 M2 O8 25.69(3) . . ?

P1 M2 O8 122.95(3) 1_655 . ?

P1 M2 O8 66.72(3) 3_656 . ?

P2 M2 O8 61.74(3) 3_656 . ?

M3 M2 O8 84.77(3) . . ?

O2 M2 O8 69.49(4) 3_656 . ?

O1 M2 O8 137.90(4) 1_655 . ?

M1MN M2 O8 68.84(3) . . ?

M1CA M2 O8 68.84(3) . . ?

O2 M2 O8 86.60(4) 4_565 . ?

O6 M2 O2 41.52(6) . 1_554 ?

O4 M2 O2 123.82(6) . 1_554 ?

O7 M2 O2 134.07(6) 3_656 1_554 ?

O8 M2 O2 56.20(5) 3_656 1_554 ?

O3 M2 O2 110.66(6) . 1_554 ?

P2 M2 O2 24.96(3) 1_554 1_554 ?

P2 M2 O2 121.87(3) . 1_554 ?

P1 M2 O2 117.93(3) 1_655 1_554 ?

P1 M2 O2 149.03(3) 3_656 1_554 ?

P2 M2 O2 67.73(3) 3_656 1_554 ?

M3 M2 O2 36.81(3) . 1_554 ?

O2 M2 O2 80.47(4) 3_656 1_554 ?

O1 M2 O2 102.40(4) 1_655 1_554 ?

M1MN M2 O2 153.06(3) . 1_554 ?

M1CA M2 O2 153.06(3) . 1_554 ?

O2 M2 O2 58.58(3) 4_565 1_554 ?

O8 M2 O2 118.17(4) . 1_554 ?

O6 M2 O4 66.92(6) . 4_565 ?

O4 M2 O4 91.77(4) . 4_565 ?

O7 M2 O4 143.96(6) 3_656 4_565 ?

O8 M2 O4 97.06(5) 3_656 4_565 ?

O3 M2 O4 62.18(6) . 4_565 ?

P2 M2 O4 67.81(3) 1_554 4_565 ?

P2 M2 O4 105.16(3) . 4_565 ?

P1 M2 O4 81.38(3) 1_655 4_565 ?

P1 M2 O4 151.03(3) 3_656 4_565 ?

P2 M2 O4 116.27(3) 3_656 4_565 ?

M3 M2 O4 61.00(3) . 4_565 ?

O2 M2 O4 134.46(4) 3_656 4_565 ?

O1 M2 O4 86.34(4) 1_655 4_565 ?

M1MN M2 O4 99.82(3) . 4_565 ?

M1CA M2 O4 99.82(3) . 4_565 ?

O2 M2 O4 40.96(4) 4_565 4_565 ?

O8 M2 O4 125.72(4) . 4_565 ?

O2 M2 O4 54.15(4) 1_554 4_565 ?

O6 M2 O1 139.04(6) . 3_656 ?

O4 M2 O1 58.65(6) . 3_656 ?

O7 M2 O1 41.87(6) 3_656 3_656 ?

O8 M2 O1 115.89(5) 3_656 3_656 ?

O3 M2 O1 78.51(6) . 3_656 ?

P2 M2 O1 151.52(3) 1_554 3_656 ?

P2 M2 O1 57.01(3) . 3_656 ?

P1 M2 O1 69.44(3) 1_655 3_656 ?

P1 M2 O1 24.50(3) 3_656 3_656 ?

P2 M2 O1 103.11(3) 3_656 3_656 ?

M3 M2 O1 140.32(3) . 3_656 ?

O2 M2 O1 90.24(4) 3_656 3_656 ?

O1 M2 O1 82.08(4) 1_655 3_656 ?

M1MN M2 O1 35.35(3) . 3_656 ?

M1CA M2 O1 35.35(3) . 3_656 ?

O2 M2 O1 125.26(4) 4_565 3_656 ?

O8 M2 O1 56.15(4) . 3_656 ?

O2 M2 O1 170.58(4) 1_554 3_656 ?

O4 M2 O1 134.96(4) 4_565 3_656 ?

O6 M2 O7 104.09(6) . 1_655 ?

O4 M2 O7 81.54(6) . 1_655 ?

O7 M2 O7 48.65(8) 3_656 1_655 ?

O8 M2 O7 161.15(5) 3_656 1_655 ?

O3 M2 O7 39.09(6) . 1_655 ?

P2 M2 O7 124.17(3) 1_554 1_655 ?

P2 M2 O7 91.62(3) . 1_655 ?

P1 M2 O7 23.37(3) 1_655 1_655 ?

P1 M2 O7 50.10(3) 3_656 1_655 ?

P2 M2 O7 142.38(3) 3_656 1_655 ?

M3 M2 O7 159.85(3) . 1_655 ?

O2 M2 O7 119.04(4) 3_656 1_655 ?

O1 M2 O7 41.00(4) 1_655 1_655 ?

M1MN M2 O7 40.35(3) . 1_655 ?

M1CA M2 O7 40.35(3) . 1_655 ?

O2 M2 O7 125.08(4) 4_565 1_655 ?

O8 M2 O7 100.73(4) . 1_655 ?

O2 M2 O7 140.95(4) 1_554 1_655 ?

O4 M2 O7 101.05(4) 4_565 1_655 ?

O1 M2 O7 46.09(4) 3_656 1_655 ?

O6 M2 O8 36.16(6) . 1_554 ?

O4 M2 O8 148.97(6) . 1_554 ?

O7 M2 O8 95.96(6) 3_656 1_554 ?

O8 M2 O8 56.29(6) 3_656 1_554 ?

O3 M2 O8 127.57(6) . 1_554 ?

P2 M2 O8 23.27(3) 1_554 1_554 ?

P2 M2 O8 133.92(3) . 1_554 ?

P1 M2 O8 116.28(3) 1_655 1_554 ?

P1 M2 O8 109.57(3) 3_656 1_554 ?

P2 M2 O8 51.35(3) 3_656 1_554 ?

M3 M2 O8 64.64(3) . 1_554 ?

O2 M2 O8 48.78(4) 3_656 1_554 ?

O1 M2 O8 90.79(4) 1_655 1_554 ?

M1MN M2 O8 166.11(3) . 1_554 ?

M1CA M2 O8 166.11(3) . 1_554 ?

O2 M2 O8 95.89(4) 4_565 1_554 ?

O8 M2 O8 112.91(4) . 1_554 ?

O2 M2 O8 39.46(4) 1_554 1_554 ?

O4 M2 O8 90.15(4) 4_565 1_554 ?

O1 M2 O8 133.16(4) 3_656 1_554 ?

O7 M2 O8 128.35(4) 1_655 1_554 ?

O6 M2 M1CA 28.38(5) . 1_554 ?

O4 M2 M1CA 145.74(5) . 1_554 ?

O7 M2 M1CA 83.95(6) 3_656 1_554 ?

O8 M2 M1CA 116.06(4) 3_656 1_554 ?

O3 M2 M1CA 66.45(5) . 1_554 ?

P2 M2 M1CA 48.456(12) 1_554 1_554 ?

P2 M2 M1CA 163.915(18) . 1_554 ?

P1 M2 M1CA 56.537(13) 1_655 1_554 ?

P1 M2 M1CA 102.303(15) 3_656 1_554 ?

P2 M2 M1CA 112.677(15) 3_656 1_554 ?

M3 M2 M1CA 102.731(13) . 1_554 ?

O2 M2 M1CA 100.11(3) 3_656 1_554 ?

O1 M2 M1CA 35.70(3) 1_655 1_554 ?

M1MN M2 M1CA 113.044(16) . 1_554 ?

M1CA M2 M1CA 113.044(16) . 1_554 ?

O2 M2 M1CA 106.14(3) 4_565 1_554 ?

O8 M2 M1CA 166.36(3) . 1_554 ?

O2 M2 M1CA 66.78(3) 1_554 1_554 ?

O4 M2 M1CA 67.82(3) 4_565 1_554 ?

O1 M2 M1CA 116.92(3) 3_656 1_554 ?

O7 M2 M1CA 76.17(3) 1_655 1_554 ?

O8 M2 M1CA 61.84(3) 1_554 1_554 ?

O6 M2 M1MN 28.38(5) . 1_554 ?

O4 M2 M1MN 145.74(5) . 1_554 ?

O7 M2 M1MN 83.95(6) 3_656 1_554 ?

O8 M2 M1MN 116.06(4) 3_656 1_554 ?

O3 M2 M1MN 66.45(5) . 1_554 ?

P2 M2 M1MN 48.456(12) 1_554 1_554 ?

P2 M2 M1MN 163.915(18) . 1_554 ?

P1 M2 M1MN 56.537(13) 1_655 1_554 ?

P1 M2 M1MN 102.303(15) 3_656 1_554 ?

P2 M2 M1MN 112.677(15) 3_656 1_554 ?

M3 M2 M1MN 102.731(13) . 1_554 ?

O2 M2 M1MN 100.11(3) 3_656 1_554 ?

O1 M2 M1MN 35.70(3) 1_655 1_554 ?

M1MN M2 M1MN 113.044(16) . 1_554 ?

M1CA M2 M1MN 113.044(16) . 1_554 ?

O2 M2 M1MN 106.14(3) 4_565 1_554 ?

O8 M2 M1MN 166.36(3) . 1_554 ?

O2 M2 M1MN 66.78(3) 1_554 1_554 ?

O4 M2 M1MN 67.82(3) 4_565 1_554 ?

O1 M2 M1MN 116.92(3) 3_656 1_554 ?

O7 M2 M1MN 76.17(3) 1_655 1_554 ?

O8 M2 M1MN 61.84(3) 1_554 1_554 ?

M1CA M2 M1MN 0.000(11) 1_554 1_554 ?

O6 M2 P2 87.36(5) . 4_565 ?

O4 M2 P2 71.23(5) . 4_565 ?

O7 M2 P2 154.93(6) 3_656 4_565 ?

O8 M2 P2 88.60(5) 3_656 4_565 ?

O3 M2 P2 68.78(5) . 4_565 ?

P2 M2 P2 83.514(15) 1_554 4_565 ?

P2 M2 P2 82.972(15) . 4_565 ?

P1 M2 P2 92.488(17) 1_655 4_565 ?

P1 M2 P2 147.493(18) 3_656 4_565 ?

P2 M2 P2 110.012(13) 3_656 4_565 ?

M3 M2 P2 53.594(12) . 4_565 ?

O2 M2 P2 134.67(3) 3_656 4_565 ?

O1 M2 P2 104.64(3) 1_655 4_565 ?

M1MN M2 P2 89.814(14) . 4_565 ?

M1CA M2 P2 89.814(14) . 4_565 ?

O2 M2 P2 22.55(3) 4_565 4_565 ?

O8 M2 P2 103.23(3) . 4_565 ?

O2 M2 P2 63.43(3) 1_554 4_565 ?

O4 M2 P2 22.59(3) 4_565 4_565 ?

O1 M2 P2 123.83(3) 3_656 4_565 ?

O7 M2 P2 106.29(3) 1_655 4_565 ?

O8 M2 P2 102.82(3) 1_554 4_565 ?

M1CA M2 P2 90.356(13) 1_554 4_565 ?

M1MN M2 P2 90.356(13) 1_554 4_565 ?

O6 M2 O5 118.51(6) . 3_656 ?

O4 M2 O5 82.94(6) . 3_656 ?

O7 M2 O5 32.78(6) 3_656 3_656 ?

O8 M2 O5 89.44(5) 3_656 3_656 ?

O3 M2 O5 110.55(6) . 3_656 ?

P2 M2 O5 119.54(3) 1_554 3_656 ?

P2 M2 O5 71.20(3) . 3_656 ?

P1 M2 O5 92.80(3) 1_655 3_656 ?

P1 M2 O5 22.01(3) 3_656 3_656 ?

P2 M2 O5 71.03(3) 3_656 3_656 ?

M3 M2 O5 124.89(3) . 3_656 ?

O2 M2 O5 53.69(4) 3_656 3_656 ?

O1 M2 O5 90.94(4) 1_655 3_656 ?

M1MN M2 O5 72.10(3) . 3_656 ?

M1CA M2 O5 72.10(3) . 3_656 ?

O2 M2 O5 139.74(4) 4_565 3_656 ?

O8 M2 O5 53.23(4) . 3_656 ?

O2 M2 O5 134.02(4) 1_554 3_656 ?

O4 M2 O5 171.83(4) 4_565 3_656 ?

O1 M2 O5 36.89(4) 3_656 3_656 ?

O7 M2 O5 72.08(4) 1_655 3_656 ?

O8 M2 O5 97.60(4) 1_554 3_656 ?

M1CA M2 O5 113.68(3) 1_554 3_656 ?

M1MN M2 O5 113.68(3) 1_554 3_656 ?

P2 M2 O5 153.96(3) 4_565 3_656 ?

O6 M2 M1MN 82.08(5) . 4_565 ?

O4 M2 M1MN 81.56(5) . 4_565 ?

O7 M2 M1MN 112.57(6) 3_656 4_565 ?

O8 M2 M1MN 131.49(5) 3_656 4_565 ?

O3 M2 M1MN 26.61(5) . 4_565 ?

P2 M2 M1MN 92.956(15) 1_554 4_565 ?

P2 M2 M1MN 99.910(15) . 4_565 ?

P1 M2 M1MN 48.738(13) 1_655 4_565 ?

P1 M2 M1MN 115.288(16) 3_656 4_565 ?

P2 M2 M1MN 151.899(17) 3_656 4_565 ?

M3 M2 M1MN 95.241(14) . 4_565 ?

O2 M2 M1MN 164.35(3) 3_656 4_565 ?

O1 M2 M1MN 63.41(3) 1_655 4_565 ?

M1MN M2 M1MN 69.574(12) . 4_565 ?

M1CA M2 M1MN 69.574(12) . 4_565 ?

O2 M2 M1MN 66.22(3) 4_565 4_565 ?

O8 M2 M1MN 125.57(3) . 4_565 ?

O2 M2 M1MN 87.48(3) 1_554 4_565 ?

O4 M2 M1MN 35.78(3) 4_565 4_565 ?

O1 M2 M1MN 101.94(3) 3_656 4_565 ?

O7 M2 M1MN 65.70(3) 1_655 4_565 ?

O8 M2 M1MN 115.92(3) 1_554 4_565 ?

M1CA M2 M1MN 65.689(11) 1_554 4_565 ?

M1MN M2 M1MN 65.689(11) 1_554 4_565 ?

P2 M2 M1MN 43.845(11) 4_565 4_565 ?

O5 M2 M1MN 136.61(3) 3_656 4_565 ?

O6 M2 M1CA 82.08(5) . 4_565 ?

O4 M2 M1CA 81.56(5) . 4_565 ?

O7 M2 M1CA 112.57(6) 3_656 4_565 ?

O8 M2 M1CA 131.49(5) 3_656 4_565 ?

O3 M2 M1CA 26.61(5) . 4_565 ?

P2 M2 M1CA 92.956(15) 1_554 4_565 ?

P2 M2 M1CA 99.910(15) . 4_565 ?

P1 M2 M1CA 48.738(13) 1_655 4_565 ?

P1 M2 M1CA 115.288(16) 3_656 4_565 ?

P2 M2 M1CA 151.899(17) 3_656 4_565 ?

M3 M2 M1CA 95.241(14) . 4_565 ?

O2 M2 M1CA 164.35(3) 3_656 4_565 ?

O1 M2 M1CA 63.41(3) 1_655 4_565 ?

M1MN M2 M1CA 69.574(12) . 4_565 ?

M1CA M2 M1CA 69.574(12) . 4_565 ?

O2 M2 M1CA 66.22(3) 4_565 4_565 ?

O8 M2 M1CA 125.57(3) . 4_565 ?

O2 M2 M1CA 87.48(3) 1_554 4_565 ?

O4 M2 M1CA 35.78(3) 4_565 4_565 ?

O1 M2 M1CA 101.94(3) 3_656 4_565 ?

O7 M2 M1CA 65.70(3) 1_655 4_565 ?

O8 M2 M1CA 115.92(3) 1_554 4_565 ?

M1CA M2 M1CA 65.689(11) 1_554 4_565 ?

M1MN M2 M1CA 65.689(11) 1_554 4_565 ?

P2 M2 M1CA 43.845(11) 4_565 4_565 ?

O5 M2 M1CA 136.61(3) 3_656 4_565 ?

M1MN M2 M1CA 0.000(13) 4_565 4_565 ?

O6 M2 O6 102.56(5) . 4_566 ?

O4 M2 O6 56.62(6) . 4_566 ?

O7 M2 O6 134.48(6) 3_656 4_566 ?

O8 M2 O6 104.93(5) 3_656 4_566 ?

O3 M2 O6 53.21(5) . 4_566 ?

P2 M2 O6 103.30(3) 1_554 4_566 ?

P2 M2 O6 72.44(3) . 4_566 ?

P1 M2 O6 78.16(3) 1_655 4_566 ?

P1 M2 O6 125.58(3) 3_656 4_566 ?

P2 M2 O6 125.97(3) 3_656 4_566 ?

M3 M2 O6 73.04(3) . 4_566 ?

O2 M2 O6 151.90(4) 3_656 4_566 ?

O1 M2 O6 97.20(4) 1_655 4_566 ?

M1MN M2 O6 67.94(3) . 4_566 ?

M1CA M2 O6 67.94(3) . 4_566 ?

O2 M2 O6 38.19(4) 4_565 4_566 ?

O8 M2 O6 96.95(4) . 4_566 ?

O2 M2 O6 85.16(4) 1_554 4_566 ?

O4 M2 O6 36.15(4) 4_565 4_566 ?

O1 M2 O6 102.63(4) 3_656 4_566 ?

O7 M2 O6 87.00(4) 1_655 4_566 ?

O8 M2 O6 124.21(4) 1_554 4_566 ?

M1CA M2 O6 96.15(3) 1_554 4_566 ?

M1MN M2 O6 96.15(3) 1_554 4_566 ?

P2 M2 O6 22.06(3) 4_565 4_566 ?

O5 M2 O6 137.06(4) 3_656 4_566 ?

M1MN M2 O6 34.26(2) 4_565 4_566 ?

M1CA M2 O6 34.26(2) 4_565 4_566 ?

O6 M2 M1MN 68.37(5) . 3_756 ?

O4 M2 M1MN 127.27(5) . 3_756 ?

O7 M2 M1MN 32.31(5) 3_656 3_756 ?

O8 M2 M1MN 123.51(5) 3_656 3_756 ?

O3 M2 M1MN 76.72(5) . 3_756 ?

P2 M2 M1MN 83.790(14) 1_554 3_756 ?

P2 M2 M1MN 127.302(17) . 3_756 ?

P1 M2 M1MN 51.985(13) 1_655 3_756 ?

P1 M2 M1MN 51.160(13) 3_656 3_756 ?

P2 M2 M1MN 103.880(16) 3_656 3_756 ?

M3 M2 M1MN 142.703(14) . 3_756 ?

O2 M2 M1MN 78.39(3) 3_656 3_756 ?

O1 M2 M1MN 32.98(3) 1_655 3_756 ?

M1MN M2 M1MN 88.417(13) . 3_756 ?

M1CA M2 M1MN 88.417(13) . 3_756 ?

O2 M2 M1MN 157.30(3) 4_565 3_756 ?

O8 M2 M1MN 115.93(3) . 3_756 ?

O2 M2 M1MN 108.59(3) 1_554 3_756 ?

O4 M2 M1MN 116.56(3) 4_565 3_756 ?

O1 M2 M1MN 70.68(3) 3_656 3_756 ?

O7 M2 M1MN 51.34(3) 1_655 3_756 ?

O8 M2 M1MN 78.44(3) 1_554 3_756 ?

M1CA M2 M1MN 51.717(12) 1_554 3_756 ?

M1MN M2 M1MN 51.717(12) 1_554 3_756 ?

P2 M2 M1MN 137.018(15) 4_565 3_756 ?

O5 M2 M1MN 62.93(3) 3_656 3_756 ?

M1MN M2 M1MN 96.243(11) 4_565 3_756 ?

M1CA M2 M1MN 96.243(11) 4_565 3_756 ?

O6 M2 M1MN 129.34(3) 4_566 3_756 ?

O6 M2 M1CA 68.37(5) . 3_756 ?

O4 M2 M1CA 127.27(5) . 3_756 ?

O7 M2 M1CA 32.31(5) 3_656 3_756 ?

O8 M2 M1CA 123.51(5) 3_656 3_756 ?

O3 M2 M1CA 76.72(5) . 3_756 ?

P2 M2 M1CA 83.790(14) 1_554 3_756 ?

P2 M2 M1CA 127.302(17) . 3_756 ?

P1 M2 M1CA 51.985(13) 1_655 3_756 ?

P1 M2 M1CA 51.160(13) 3_656 3_756 ?

P2 M2 M1CA 103.880(16) 3_656 3_756 ?

M3 M2 M1CA 142.703(14) . 3_756 ?

O2 M2 M1CA 78.39(3) 3_656 3_756 ?

O1 M2 M1CA 32.98(3) 1_655 3_756 ?

M1MN M2 M1CA 88.417(13) . 3_756 ?

M1CA M2 M1CA 88.417(13) . 3_756 ?

O2 M2 M1CA 157.30(3) 4_565 3_756 ?

O8 M2 M1CA 115.93(3) . 3_756 ?

O2 M2 M1CA 108.59(3) 1_554 3_756 ?

O4 M2 M1CA 116.56(3) 4_565 3_756 ?

O1 M2 M1CA 70.68(3) 3_656 3_756 ?

O7 M2 M1CA 51.34(3) 1_655 3_756 ?

O8 M2 M1CA 78.44(3) 1_554 3_756 ?

M1CA M2 M1CA 51.717(12) 1_554 3_756 ?

M1MN M2 M1CA 51.717(12) 1_554 3_756 ?

P2 M2 M1CA 137.018(15) 4_565 3_756 ?

O5 M2 M1CA 62.93(3) 3_656 3_756 ?

M1MN M2 M1CA 96.243(11) 4_565 3_756 ?

M1CA M2 M1CA 96.243(11) 4_565 3_756 ?

O6 M2 M1CA 129.34(3) 4_566 3_756 ?

M1MN M2 M1CA 0.000(14) 3_756 3_756 ?

O6 M2 O2 145.07(6) . . ?

O4 M2 O2 23.88(6) . . ?

O7 M2 O2 114.99(6) 3_656 . ?

O8 M2 O2 69.54(5) 3_656 . ?

O3 M2 O2 99.55(5) . . ?

P2 M2 O2 127.86(3) 1_554 . ?

P2 M2 O2 19.16(2) . . ?

P1 M2 O2 117.66(3) 1_655 . ?

P1 M2 O2 95.81(3) 3_656 . ?

P2 M2 O2 80.80(3) 3_656 . ?

M3 M2 O2 67.64(2) . . ?

O2 M2 O2 99.32(4) 3_656 . ?

O1 M2 O2 143.68(4) 1_655 . ?

M1MN M2 O2 64.98(3) . . ?

M1CA M2 O2 64.98(3) . . ?

O2 M2 O2 53.32(3) 4_565 . ?

O8 M2 O2 37.03(4) . . ?

O2 M2 O2 103.95(4) 1_554 . ?

O4 M2 O2 89.20(4) 4_565 . ?

O1 M2 O2 75.85(4) 3_656 . ?

O7 M2 O2 105.33(4) 1_655 . ?

O8 M2 O2 125.28(4) 1_554 . ?

M1CA M2 O2 156.59(3) 1_554 . ?

M1MN M2 O2 156.59(3) 1_554 . ?

P2 M2 O2 66.61(3) 4_565 . ?

O5 M2 O2 88.43(4) 3_656 . ?

M1MN M2 O2 93.23(3) 4_565 . ?

M1CA M2 O2 93.23(3) 4_565 . ?

O6 M2 O2 60.94(3) 4_566 . ?

M1MN M2 O2 146.41(3) 3_756 . ?

M1CA M2 O2 146.41(3) 3_756 . ?

O6 M2 M3 53.38(5) . 3_655 ?

O4 M2 M3 145.27(5) . 3_655 ?

O7 M2 M3 66.61(5) 3_656 3_655 ?

O8 M2 M3 67.60(4) 3_656 3_655 ?

O3 M2 M3 128.53(5) . 3_655 ?

P2 M2 M3 50.460(12) 1_554 3_655 ?

P2 M2 M3 127.069(17) . 3_655 ?

P1 M2 M3 106.577(15) 1_655 3_655 ?

P1 M2 M3 79.348(15) 3_656 3_655 ?

P2 M2 M3 51.391(12) 3_656 3_655 ?

M3 M2 M3 90.014(12) . 3_655 ?

O2 M2 M3 32.54(3) 3_656 3_655 ?

O1 M2 M3 81.59(3) 1_655 3_655 ?

M1MN M2 M3 136.610(15) . 3_655 ?

M1CA M2 M3 136.610(15) . 3_655 ?

O2 M2 M3 124.27(3) 4_565 3_655 ?

O8 M2 M3 101.39(3) . 3_655 ?

O2 M2 M3 69.68(3) 1_554 3_655 ?

O4 M2 M3 117.97(3) 4_565 3_655 ?

O1 M2 M3 103.16(3) 3_656 3_655 ?

O7 M2 M3 107.61(3) 1_655 3_655 ?

O8 M2 M3 30.22(3) 1_554 3_655 ?

M1CA M2 M3 67.608(10) 1_554 3_655 ?

M1MN M2 M3 67.608(10) 1_554 3_655 ?

P2 M2 M3 132.986(14) 4_565 3_655 ?

O5 M2 M3 69.12(3) 3_656 3_655 ?

M1MN M2 M3 133.016(13) 4_565 3_655 ?

M1CA M2 M3 133.016(13) 4_565 3_655 ?

O6 M2 M3 153.75(3) 4_566 3_655 ?

M1MN M2 M3 56.907(10) 3_756 3_655 ?

M1CA M2 M3 56.907(10) 3_756 3_655 ?

O2 M2 M3 131.20(3) . 3_655 ?

O6 M2 O1 36.82(6) . 3_655 ?

O4 M2 O1 159.22(6) . 3_655 ?

O7 M2 O1 61.75(6) 3_656 3_655 ?

O8 M2 O1 104.51(5) 3_656 3_655 ?

O3 M2 O1 87.99(5) . 3_655 ?

P2 M2 O1 51.45(3) 1_554 3_655 ?

P2 M2 O1 156.78(3) . 3_655 ?

P1 M2 O1 68.56(3) 1_655 3_655 ?

P1 M2 O1 80.88(3) 3_656 3_655 ?

P2 M2 O1 91.76(3) 3_656 3_655 ?

M3 M2 O1 111.25(3) . 3_655 ?

O2 M2 O1 72.49(4) 3_656 3_655 ?

O1 M2 O1 42.47(5) 1_655 3_655 ?

M1MN M2 O1 118.41(3) . 3_655 ?

M1CA M2 O1 118.41(3) . 3_655 ?

O2 M2 O1 130.62(4) 4_565 3_655 ?

O8 M2 O1 135.56(4) . 3_655 ?

O2 M2 O1 76.21(4) 1_554 3_655 ?

O4 M2 O1 97.36(4) 4_565 3_655 ?

O1 M2 O1 102.60(4) 3_656 3_655 ?

O7 M2 O1 78.42(4) 1_655 3_655 ?

O8 M2 O1 50.05(4) 1_554 3_655 ?

M1CA M2 O1 31.01(3) 1_554 3_655 ?

M1MN M2 O1 31.01(3) 1_554 3_655 ?

P2 M2 O1 119.84(3) 4_565 3_655 ?

O5 M2 O1 85.74(4) 3_656 3_655 ?

M1MN M2 O1 95.03(3) 4_565 3_655 ?

M1CA M2 O1 95.03(3) 4_565 3_655 ?

O6 M2 O1 127.07(4) 4_566 3_655 ?

M1MN M2 O1 32.38(3) 3_756 3_655 ?

M1CA M2 O1 32.38(3) 3_756 3_655 ?

O2 M2 O1 171.74(4) . 3_655 ?

M3 M2 O1 40.86(3) 3_655 3_655 ?

O6 M2 O6 173.78(8) . 1_556 ?

O4 M2 O6 17.35(6) . 1_556 ?

O7 M2 O6 83.61(6) 3_656 1_556 ?

O8 M2 O6 96.58(5) 3_656 1_556 ?

O3 M2 O6 82.72(6) . 1_556 ?

P2 M2 O6 162.58(3) 1_554 1_556 ?

P2 M2 O6 18.72(2) . 1_556 ?

P1 M2 O6 90.88(3) 1_655 1_556 ?

P1 M2 O6 64.94(3) 3_656 1_556 ?

P2 M2 O6 98.39(3) 3_656 1_556 ?

M3 M2 O6 102.61(3) . 1_556 ?

O2 M2 O6 103.94(4) 3_656 1_556 ?

O1 M2 O6 113.85(4) 1_655 1_556 ?

M1MN M2 O6 34.31(2) . 1_556 ?

M1CA M2 O6 34.31(2) . 1_556 ?

O2 M2 O6 83.63(4) 4_565 1_556 ?

O8 M2 O6 36.80(4) . 1_556 ?

O2 M2 O6 138.87(4) 1_554 1_556 ?

O4 M2 O6 107.99(4) 4_565 1_556 ?

O1 M2 O6 42.10(4) 3_656 1_556 ?

O7 M2 O6 72.91(4) 1_655 1_556 ?

O8 M2 O6 149.70(4) 1_554 1_556 ?

M1CA M2 O6 147.30(3) 1_554 1_556 ?

M1MN M2 O6 147.30(3) 1_554 1_556 ?

P2 M2 O6 88.29(3) 4_565 1_556 ?

O5 M2 O6 66.15(4) 3_656 1_556 ?

M1MN M2 O6 91.71(3) 4_565 1_556 ?

M1CA M2 O6 91.71(3) 4_565 1_556 ?

O6 M2 O6 72.05(4) 4_566 1_556 ?

M1MN M2 O6 112.36(3) 3_756 1_556 ?

M1CA M2 O6 112.36(3) 3_756 1_556 ?

O2 M2 O6 35.01(3) . 1_556 ?

M3 M2 O6 132.51(3) 3_655 1_556 ?

O1 M2 O6 144.63(4) 3_655 1_556 ?

O6 M2 O5 74.42(6) . 2_645 ?

O4 M2 O5 126.98(6) . 2_645 ?

O7 M2 O5 39.07(6) 3_656 2_645 ?

O8 M2 O5 84.35(5) 3_656 2_645 ?

O3 M2 O5 117.22(5) . 2_645 ?

P2 M2 O5 77.15(3) 1_554 2_645 ?

P2 M2 O5 113.04(3) . 2_645 ?

P1 M2 O5 92.27(3) 1_655 2_645 ?

P1 M2 O5 51.17(3) 3_656 2_645 ?

P2 M2 O5 63.54(3) 3_656 2_645 ?

M3 M2 O5 114.77(3) . 2_645 ?

O2 M2 O5 37.69(4) 3_656 2_645 ?

O1 M2 O5 73.12(4) 1_655 2_645 ?

M1MN M2 O5 108.39(3) . 2_645 ?

M1CA M2 O5 108.39(3) . 2_645 ?

O2 M2 O5 150.03(4) 4_565 2_645 ?

O8 M2 O5 89.79(4) . 2_645 ?

O2 M2 O5 97.90(4) 1_554 2_645 ?

O4 M2 O5 141.19(4) 4_565 2_645 ?

O1 M2 O5 75.31(4) 3_656 2_645 ?

O7 M2 O5 84.82(4) 1_655 2_645 ?

O8 M2 O5 58.45(4) 1_554 2_645 ?

M1CA M2 O5 76.75(3) 1_554 2_645 ?

M1MN M2 O5 76.75(3) 1_554 2_645 ?

P2 M2 O5 160.66(3) 4_565 2_645 ?

O5 M2 O5 44.214(8) 3_656 2_645 ?

M1MN M2 O5 136.30(3) 4_565 2_645 ?

M1CA M2 O5 136.30(3) 4_565 2_645 ?

O6 M2 O5 170.25(4) 4_566 2_645 ?

M1MN M2 O5 40.91(3) 3_756 2_645 ?

M1CA M2 O5 40.91(3) 3_756 2_645 ?

O2 M2 O5 126.58(4) . 2_645 ?

M3 M2 O5 28.26(3) 3_655 2_645 ?

O1 M2 O5 45.78(4) 3_655 2_645 ?

O6 M2 O5 110.37(3) 1_556 2_645 ?

O6 M2 O3 44.45(6) . 4_565 ?

O4 M2 O3 119.45(6) . 4_565 ?

O7 M2 O3 106.41(6) 3_656 4_565 ?

O8 M2 O3 120.26(5) 3_656 4_565 ?

O3 M2 O3 49.71(3) . 4_565 ?

P2 M2 O3 58.79(3) 1_554 4_565 ?

P2 M2 O3 137.42(3) . 4_565 ?

P1 M2 O3 54.39(3) 1_655 4_565 ?

P1 M2 O3 121.10(3) 3_656 4_565 ?

P2 M2 O3 128.85(3) 3_656 4_565 ?

M3 M2 O3 91.26(3) . 4_565 ?

O2 M2 O3 126.41(4) 3_656 4_565 ?

O1 M2 O3 48.57(4) 1_655 4_565 ?

M1MN M2 O3 101.51(3) . 4_565 ?

M1CA M2 O3 101.51(3) . 4_565 ?

O2 M2 O3 80.64(4) 4_565 4_565 ?

O8 M2 O3 162.86(4) . 4_565 ?

O2 M2 O3 64.12(4) 1_554 4_565 ?

O4 M2 O3 39.88(4) 4_565 4_565 ?

O1 M2 O3 123.78(4) 3_656 4_565 ?

O7 M2 O3 77.76(4) 1_655 4_565 ?

O8 M2 O3 79.98(4) 1_554 4_565 ?

M1CA M2 O3 30.25(3) 1_554 4_565 ?

M1MN M2 O3 30.25(3) 1_554 4_565 ?

P2 M2 O3 61.61(3) 4_565 4_565 ?

O5 M2 O3 139.08(4) 3_656 4_565 ?

M1MN M2 O3 38.11(3) 4_565 4_565 ?

M1CA M2 O3 38.11(3) 4_565 4_565 ?

O6 M2 O3 65.98(4) 4_566 4_565 ?

M1MN M2 O3 76.74(3) 3_756 4_565 ?

M1CA M2 O3 76.74(3) 3_756 4_565 ?

O2 M2 O3 126.45(4) . 4_565 ?

M3 M2 O3 95.27(3) 3_655 4_565 ?

O1 M2 O3 61.26(4) 3_655 4_565 ?

O6 M2 O3 129.35(4) 1_556 4_565 ?

O5 M2 O3 106.96(4) 2_645 4_565 ?

O6 M2 O4 6.49(5) . 1_554 ?

O4 M2 O4 153.21(7) . 1_554 ?

O7 M2 O4 104.90(6) 3_656 1_554 ?

O8 M2 O4 83.87(5) 3_656 1_554 ?

O3 M2 O4 93.16(6) . 1_554 ?

P2 M2 O4 15.95(2) 1_554 1_554 ?

P2 M2 O4 157.13(3) . 1_554 ?

P1 M2 O4 88.93(3) 1_655 1_554 ?

P1 M2 O4 123.87(3) 3_656 1_554 ?

P2 M2 O4 85.56(3) 3_656 1_554 ?

M3 M2 O4 72.12(2) . 1_554 ?

O2 M2 O4 83.45(4) 3_656 1_554 ?

O1 M2 O4 68.41(4) 1_655 1_554 ?

M1MN M2 O4 144.28(3) . 1_554 ?

M1CA M2 O4 144.28(3) . 1_554 ?

O2 M2 O4 87.70(4) 4_565 1_554 ?

O8 M2 O4 146.87(4) . 1_554 ?

O2 M2 O4 35.30(3) 1_554 1_554 ?

O4 M2 O4 62.48(4) 4_565 1_554 ?

O1 M2 O4 145.53(4) 3_656 1_554 ?

O7 M2 O4 109.16(4) 1_655 1_554 ?

O8 M2 O4 35.56(3) 1_554 1_554 ?

M1CA M2 O4 33.00(2) 1_554 1_554 ?

M1MN M2 O4 33.00(2) 1_554 1_554 ?

P2 M2 O4 82.11(3) 4_565 1_554 ?

O5 M2 O4 123.47(4) 3_656 1_554 ?

M1MN M2 O4 80.95(2) 4_565 1_554 ?

M1CA M2 O4 80.95(2) 4_565 1_554 ?

O6 M2 O4 98.51(3) 4_566 1_554 ?

M1MN M2 O4 74.86(2) 3_756 1_554 ?

M1CA M2 O4 74.86(2) 3_756 1_554 ?

O2 M2 O4 138.60(3) . 1_554 ?

M3 M2 O4 56.48(2) 3_655 1_554 ?

O1 M2 O4 43.24(3) 3_655 1_554 ?

O6 M2 O4 170.38(3) 1_556 1_554 ?

O5 M2 O4 79.25(3) 2_645 1_554 ?

O3 M2 O4 44.43(4) 4_565 1_554 ?

O6 M2 O4 105.14(6) . 3_656 ?

O4 M2 O4 83.57(6) . 3_656 ?

O7 M2 O4 93.34(6) 3_656 3_656 ?

O8 M2 O4 26.30(5) 3_656 3_656 ?

O3 M2 O4 163.09(6) . 3_656 ?

P2 M2 O4 87.61(3) 1_554 3_656 ?

P2 M2 O4 65.70(3) . 3_656 ?

P1 M2 O4 156.71(3) 1_655 3_656 ?

P1 M2 O4 85.77(3) 3_656 3_656 ?

P2 M2 O4 17.93(2) 3_656 3_656 ?

M3 M2 O4 61.00(3) . 3_656 ?

O2 M2 O4 35.28(4) 3_656 3_656 ?

O1 M2 O4 144.09(4) 1_655 3_656 ?

M1MN M2 O4 112.38(3) . 3_656 ?

M1CA M2 O4 112.38(3) . 3_656 ?

O2 M2 O4 86.15(4) 4_565 3_656 ?

O8 M2 O4 43.92(4) . 3_656 ?

O2 M2 O4 81.32(4) 1_554 3_656 ?

O4 M2 O4 121.83(2) 4_565 3_656 ?

O1 M2 O4 90.20(4) 3_656 3_656 ?

O7 M2 O4 134.85(4) 1_655 3_656 ?

O8 M2 O4 69.28(3) 1_554 3_656 ?

M1CA M2 O4 130.39(3) 1_554 3_656 ?

M1MN M2 O4 130.39(3) 1_554 3_656 ?

P2 M2 O4 108.69(3) 4_565 3_656 ?

O5 M2 O4 63.91(4) 3_656 3_656 ?

M1MN M2 O4 152.03(3) 4_565 3_656 ?

M1CA M2 O4 152.03(3) 4_565 3_656 ?

O6 M2 O4 118.70(3) 4_566 3_656 ?

M1MN M2 O4 111.59(3) 3_756 3_656 ?

M1CA M2 O4 111.59(3) 3_756 3_656 ?

O2 M2 O4 65.16(3) . 3_656 ?

M3 M2 O4 66.06(2) 3_655 3_656 ?

O1 M2 O4 106.91(3) 3_655 3_656 ?

O6 M2 O4 80.48(3) 1_556 3_656 ?

O5 M2 O4 71.00(4) 2_645 3_656 ?

O3 M2 O4 145.01(4) 4_565 3_656 ?

O4 M2 O4 103.15(3) 1_554 3_656 ?

O6 M2 O3 105.10(6) . 3_756 ?

O4 M2 O3 92.97(6) . 3_756 ?

O7 M2 O3 8.72(6) 3_656 3_756 ?

O8 M2 O3 121.10(5) 3_656 3_756 ?

O3 M2 O3 80.87(6) . 3_756 ?

P2 M2 O3 117.86(3) 1_554 3_756 ?

P2 M2 O3 90.16(3) . 3_756 ?

P1 M2 O3 59.88(3) 1_655 3_756 ?

P1 M2 O3 14.79(3) 3_656 3_756 ?

P2 M2 O3 100.53(3) 3_656 3_756 ?

M3 M2 O3 157.41(3) . 3_756 ?

O2 M2 O3 77.35(4) 3_656 3_756 ?

O1 M2 O3 58.35(4) 1_655 3_756 ?

M1MN M2 O3 61.60(3) . 3_756 ?

M1CA M2 O3 61.60(3) . 3_756 ?

O2 M2 O3 159.01(4) 4_565 3_756 ?

O8 M2 O3 81.51(4) . 3_756 ?

O2 M2 O3 142.39(4) 1_554 3_756 ?

O4 M2 O3 141.22(4) 4_565 3_756 ?

O1 M2 O3 34.40(4) 3_656 3_756 ?

O7 M2 O3 42.04(4) 1_655 3_756 ?

O8 M2 O3 104.65(4) 1_554 3_756 ?

M1CA M2 O3 87.67(3) 1_554 3_756 ?

M1MN M2 O3 87.67(3) 1_554 3_756 ?

P2 M2 O3 147.58(3) 4_565 3_756 ?

O5 M2 O3 33.72(4) 3_656 3_756 ?

M1MN M2 O3 107.33(3) 4_565 3_756 ?

M1CA M2 O3 107.33(3) 4_565 3_756 ?

O6 M2 O3 126.33(4) 4_566 3_756 ?

M1MN M2 O3 37.19(3) 3_756 3_756 ?

M1CA M2 O3 37.19(3) 3_756 3_756 ?

O2 M2 O3 109.31(3) . 3_756 ?

M3 M2 O3 75.32(3) 3_655 3_756 ?

O1 M2 O3 68.35(4) 3_655 3_756 ?

O6 M2 O3 76.48(3) 1_556 3_756 ?

O5 M2 O3 47.65(4) 2_645 3_756 ?

O3 M2 O3 106.88(2) 4_565 3_756 ?

O4 M2 O3 111.56(4) 1_554 3_756 ?

O4 M2 O3 96.95(4) 3_656 3_756 ?

O5 M3 O8 144.78(7) 4_565 3_656 ?

O5 M3 O2 107.89(7) 4_565 4_565 ?

O8 M3 O2 106.48(7) 3_656 4_565 ?

O5 M3 O5 93.32(7) 4_565 . ?

O8 M3 O5 103.30(7) 3_656 . ?

O2 M3 O5 74.02(7) 4_565 . ?

O5 M3 O2 74.64(7) 4_565 1_554 ?

O8 M3 O2 88.08(6) 3_656 1_554 ?

O2 M3 O2 107.31(7) 4_565 1_554 ?

O5 M3 O2 167.79(7) . 1_554 ?

O5 M3 M2 150.16(5) 4_565 . ?

O8 M3 M2 38.84(5) 3_656 . ?

O2 M3 M2 75.08(5) 4_565 . ?

O5 M3 M2 115.48(5) . . ?

O2 M3 M2 76.20(4) 1_554 . ?

O5 M3 M2 78.80(5) 4_565 3_655 ?

O8 M3 M2 66.17(5) 3_656 3_655 ?

O2 M3 M2 160.33(5) 4_565 3_655 ?

O5 M3 M2 124.81(5) . 3_655 ?

O2 M3 M2 55.73(5) 1_554 3_655 ?

M2 M3 M2 89.985(12) . 3_655 ?

O5 M3 M2 61.67(5) 4_565 2_655 ?

O8 M3 M2 153.44(5) 3_656 2_655 ?

O2 M3 M2 47.18(5) 4_565 2_655 ?

O5 M3 M2 69.45(5) . 2_655 ?

O2 M3 M2 102.21(5) 1_554 2_655 ?

M2 M3 M2 119.624(12) . 2_655 ?

M2 M3 M2 139.456(13) 3_655 2_655 ?

O5 M3 M2 80.65(6) 4_565 4_565 ?

O8 M3 M2 109.16(5) 3_656 4_565 ?

O2 M3 M2 62.38(5) 4_565 4_565 ?

O5 M3 M2 131.09(5) . 4_565 ?

O2 M3 M2 46.00(5) 1_554 4_565 ?

M2 M3 M2 74.645(14) . 4_565 ?

M2 M3 M2 101.716(9) 3_655 4_565 ?

M2 M3 M2 65.064(11) 2_655 4_565 ?

O5 M3 M2 132.64(6) 4_565 3_656 ?

O8 M3 M2 46.18(5) 3_656 3_656 ?

O2 M3 M2 99.50(5) 4_565 3_656 ?

O5 M3 M2 57.91(5) . 3_656 ?

O2 M3 M2 132.35(5) 1_554 3_656 ?

M2 M3 M2 73.638(12) . 3_656 ?

M2 M3 M2 88.171(11) 3_655 3_656 ?

M2 M3 M2 124.645(12) 2_655 3_656 ?

M2 M3 M2 146.707(9) 4_565 3_656 ?

O5 M3 M2 125.01(6) 4_565 4_566 ?

O8 M3 M2 89.90(5) 3_656 4_566 ?

O2 M3 M2 17.57(5) 4_565 4_566 ?

O5 M3 M2 71.64(5) . 4_566 ?

O2 M3 M2 113.37(5) 1_554 4_566 ?

M2 M3 M2 62.708(12) . 4_566 ?

M2 M3 M2 152.690(10) 3_655 4_566 ?

M2 M3 M2 63.544(10) 2_655 4_566 ?

M2 M3 M2 72.832(8) 4_565 4_566 ?

M2 M3 M2 83.816(8) 3_656 4_566 ?

O7 P1 O1 114.13(11) . . ?

O7 P1 O3 107.68(12) . 1_455 ?

O1 P1 O3 110.89(11) . 1_455 ?

O7 P1 O5 110.30(11) . . ?

O1 P1 O5 105.25(10) . . ?

O3 P1 O5 108.47(11) 1_455 . ?

O7 P1 M1CA 130.98(8) . 4_465 ?

O1 P1 M1CA 113.06(8) . 4_465 ?

O3 P1 M1CA 41.18(8) 1_455 4_465 ?

O5 P1 M1CA 68.37(8) . 4_465 ?

O7 P1 M1CA 50.01(8) . 1_455 ?

O1 P1 M1CA 136.83(7) . 1_455 ?

O3 P1 M1CA 58.19(8) 1_455 1_455 ?

O5 P1 M1CA 117.88(7) . 1_455 ?

M1CA P1 M1CA 85.854(17) 4_465 1_455 ?

O7 P1 M1CA 81.22(8) . 3_656 ?

O1 P1 M1CA 34.35(7) . 3_656 ?

O3 P1 M1CA 114.95(8) 1_455 3_656 ?

O5 P1 M1CA 128.86(8) . 3_656 ?

M1CA P1 M1CA 139.997(19) 4_465 3_656 ?

M1CA P1 M1CA 107.507(18) 1_455 3_656 ?

O7 P1 M2 96.65(8) . 1_455 ?

O1 P1 M2 81.64(7) . 1_455 ?

O3 P1 M2 40.32(8) 1_455 1_455 ?

O5 P1 M2 145.44(8) . 1_455 ?

M1CA P1 M2 77.707(17) 4_465 1_455 ?

M1CA P1 M2 64.275(14) 1_455 1_455 ?

M1CA P1 M2 75.073(16) 3_656 1_455 ?

O7 P1 M2 26.39(8) . 3_656 ?

O1 P1 M2 92.27(7) . 3_656 ?

O3 P1 M2 132.06(9) 1_455 3_656 ?

O5 P1 M2 104.58(8) . 3_656 ?

M1CA P1 M2 154.63(2) 4_465 3_656 ?

M1CA P1 M2 75.980(16) 1_455 3_656 ?

M1CA P1 M2 63.927(15) 3_656 3_656 ?

M2 P1 M2 108.993(18) 1_455 3_656 ?

O7 P1 M1CA 142.59(8) . 1_454 ?

O1 P1 M1CA 31.41(7) . 1_454 ?

O3 P1 M1CA 85.33(8) 1_455 1_454 ?

O5 P1 M1CA 97.62(7) . 1_454 ?

M1CA P1 M1CA 81.846(17) 4_465 1_454 ?

M1CA P1 M1CA 134.61(2) 1_455 1_454 ?

M1CA P1 M1CA 61.701(15) 3_656 1_454 ?

M2 P1 M1CA 70.433(15) 1_455 1_454 ?

M2 P1 M1CA 123.529(19) 3_656 1_454 ?

O7 P1 M2 156.60(8) . 4_465 ?

O1 P1 M2 78.30(7) . 4_465 ?

O3 P1 M2 49.03(8) 1_455 4_465 ?

O5 P1 M2 83.48(8) . 4_465 ?

M1CA P1 M2 35.474(11) 4_465 4_465 ?

M1CA P1 M2 107.091(15) 1_455 4_465 ?

M1CA P1 M2 105.281(16) 3_656 4_465 ?

M2 P1 M2 64.477(14) 1_455 4_465 ?

M2 P1 M2 169.049(18) 3_656 4_465 ?

M1CA P1 M2 46.886(11) 1_454 4_465 ?

O7 P1 M2 109.54(8) . 3_655 ?

O1 P1 M2 22.02(7) . 3_655 ?

O3 P1 M2 130.52(8) 1_455 3_655 ?

O5 P1 M2 87.77(7) . 3_655 ?

M1CA P1 M2 119.188(17) 4_465 3_655 ?

M1CA P1 M2 150.433(18) 1_455 3_655 ?

M1CA P1 M2 43.328(11) 3_656 3_655 ?

M2 P1 M2 103.604(14) 1_455 3_655 ?

M2 P1 M2 83.773(14) 3_656 3_655 ?

M1CA P1 M2 45.629(10) 1_454 3_655 ?

M2 P1 M2 89.231(9) 4_465 3_655 ?

O2 P2 O4 110.04(10) . . ?

O2 P2 O6 110.63(10) . 1_556 ?

O4 P2 O6 103.55(10) . 1_556 ?

O2 P2 O8 110.34(10) . . ?

O4 P2 O8 111.60(10) . . ?

O6 P2 O8 110.51(9) 1_556 . ?

O2 P2 M1CA 130.55(7) . . ?

O4 P2 M1CA 52.16(7) . . ?

O6 P2 M1CA 51.95(6) 1_556 . ?

O8 P2 M1CA 119.11(7) . . ?

O2 P2 M2 92.79(7) . 1_556 ?

O4 P2 M2 128.78(7) . 1_556 ?

O6 P2 M2 26.03(6) 1_556 1_556 ?

O8 P2 M2 101.32(7) . 1_556 ?

M1CA P2 M2 77.904(18) . 1_556 ?

O2 P2 M2 116.61(7) . . ?

O4 P2 M2 24.09(7) . . ?

O6 P2 M2 118.35(7) 1_556 . ?

O8 P2 M2 88.00(7) . . ?

M1CA P2 M2 67.397(15) . . ?

M2 P2 M2 144.04(2) 1_556 . ?

O2 P2 M2 79.00(7) . 3_656 ?

O4 P2 M2 119.17(7) . 3_656 ?

O6 P2 M2 130.15(7) 1_556 3_656 ?

O8 P2 M2 31.96(6) . 3_656 ?

M1CA P2 M2 149.99(2) . 3_656 ?

M2 P2 M2 109.676(17) 1_556 3_656 ?

M2 P2 M2 96.611(17) . 3_656 ?

O2 P2 M2 62.46(7) . 4_566 ?

O4 P2 M2 65.54(7) . 4_566 ?

O6 P2 M2 80.89(7) 1_556 4_566 ?

O8 P2 M2 168.50(7) . 4_566 ?

M1CA P2 M2 68.752(15) . 4_566 ?

M2 P2 M2 88.342(16) 1_556 4_566 ?

M2 P2 M2 87.740(16) . 4_566 ?

M2 P2 M2 138.386(18) 3_656 4_566 ?

P1 O1 M1MN 122.37(11) . 3_656 ?

P1 O1 M1CA 122.37(11) . 3_656 ?

M1MN O1 M1CA 0.00(2) 3_656 3_656 ?

P1 O1 M1CA 128.25(11) . 1_454 ?

M1MN O1 M1CA 100.86(7) 3_656 1_454 ?

M1CA O1 M1CA 100.86(7) 3_656 1_454 ?

P1 O1 M1MN 128.25(11) . 1_454 ?

M1MN O1 M1MN 100.86(7) 3_656 1_454 ?

M1CA O1 M1MN 100.86(7) 3_656 1_454 ?

M1CA O1 M1MN 0.00(3) 1_454 1_454 ?

P1 O1 M2 72.26(7) . 1_455 ?

M1MN O1 M2 87.99(6) 3_656 1_455 ?

M1CA O1 M2 87.99(6) 3_656 1_455 ?

M1CA O1 M2 83.28(5) 1_454 1_455 ?

M1MN O1 M2 83.28(5) 1_454 1_455 ?

P1 O1 M2 63.24(7) . 3_656 ?

M1MN O1 M2 67.01(5) 3_656 3_656 ?

M1CA O1 M2 67.01(5) 3_656 3_656 ?

M1CA O1 M2 167.69(7) 1_454 3_656 ?

M1MN O1 M2 167.69(7) 1_454 3_656 ?

M2 O1 M2 97.92(4) 1_455 3_656 ?

P1 O1 M2 150.12(9) . 3_655 ?

M1MN O1 M2 67.13(4) 3_656 3_655 ?

M1CA O1 M2 67.13(4) 3_656 3_655 ?

M1CA O1 M2 69.33(4) 1_454 3_655 ?

M1MN O1 M2 69.33(4) 1_454 3_655 ?

M2 O1 M2 137.53(5) 1_455 3_655 ?

M2 O1 M2 102.60(4) 3_656 3_655 ?

P2 O2 M3 135.00(10) . 4_566 ?

P2 O2 M3 123.91(10) . 1_556 ?

M3 O2 M3 101.09(7) 4_566 1_556 ?

P2 O2 M2 75.06(7) . 3_656 ?

M3 O2 M2 105.97(6) 4_566 3_656 ?

M3 O2 M2 91.73(6) 1_556 3_656 ?

P2 O2 M2 94.99(8) . 4_566 ?

M3 O2 M2 69.64(5) 4_566 4_566 ?

M3 O2 M2 106.98(6) 1_556 4_566 ?

M2 O2 M2 161.24(6) 3_656 4_566 ?

P2 O2 M2 62.25(6) . 1_556 ?

M3 O2 M2 152.28(7) 4_566 1_556 ?

M3 O2 M2 66.99(4) 1_556 1_556 ?

M2 O2 M2 99.53(4) 3_656 1_556 ?

M2 O2 M2 89.39(4) 4_566 1_556 ?

P2 O2 M2 44.24(5) . . ?

M3 O2 M2 90.91(5) 4_566 . ?

M3 O2 M2 167.23(7) 1_556 . ?

M2 O2 M2 80.68(4) 3_656 . ?

M2 O2 M2 81.16(4) 4_566 . ?

M2 O2 M2 103.95(4) 1_556 . ?

P1 O3 M1MN 111.22(11) 1_655 4_565 ?

P1 O3 M1CA 111.22(11) 1_655 4_565 ?

M1MN O3 M1CA 0.00(3) 4_565 4_565 ?

P1 O3 M2 114.72(11) 1_655 . ?

M1MN O3 M2 124.47(9) 4_565 . ?

M1CA O3 M2 124.47(9) 4_565 . ?

P1 O3 M1CA 93.32(9) 1_655 . ?

M1MN O3 M1CA 121.24(8) 4_565 . ?

M1CA O3 M1CA 121.24(8) 4_565 . ?

M2 O3 M1CA 85.57(7) . . ?

P1 O3 M2 143.57(10) 1_655 4_566 ?

M1MN O3 M2 64.19(5) 4_565 4_566 ?

M1CA O3 M2 64.19(5) 4_565 4_566 ?

M2 O3 M2 93.39(5) . 4_566 ?

M1CA O3 M2 64.95(4) . 4_566 ?

P1 O3 M2 33.15(6) 1_655 3_756 ?

M1MN O3 M2 136.01(7) 4_565 3_756 ?

M1CA O3 M2 136.01(7) 4_565 3_756 ?

M2 O3 M2 99.13(6) . 3_756 ?

M1CA O3 M2 62.18(4) . 3_756 ?

M2 O3 M2 124.18(5) 4_566 3_756 ?

P1 O3 M2 116.45(10) 1_655 4_565 ?

M1MN O3 M2 45.57(4) 4_565 4_565 ?

M1CA O3 M2 45.57(4) 4_565 4_565 ?

M2 O3 M2 85.90(6) . 4_565 ?

M1CA O3 M2 149.87(6) . 4_565 ?

M2 O3 M2 86.81(3) 4_566 4_565 ?

M2 O3 M2 147.87(5) 3_756 4_565 ?

P2 O4 M2 137.35(11) . . ?

P2 O4 M1CA 97.30(9) . . ?

M2 O4 M1CA 105.83(7) . . ?

P2 O4 M1MN 97.30(9) . . ?

M2 O4 M1MN 105.83(7) . . ?

M1CA O4 M1MN 0.000(19) . . ?

P2 O4 M2 91.86(7) . 4_566 ?

M2 O4 M2 126.37(7) . 4_566 ?

M1CA O4 M2 81.16(5) . 4_566 ?

M1MN O4 M2 81.16(5) . 4_566 ?

P2 O4 M2 35.26(5) . 1_556 ?

M2 O4 M2 153.21(7) . 1_556 ?

M1CA O4 M2 63.35(4) . 1_556 ?

M1MN O4 M2 63.35(4) . 1_556 ?

M2 O4 M2 78.00(3) 4_566 1_556 ?

P2 O4 M2 42.90(5) . 3_656 ?

M2 O4 M2 96.43(6) . 3_656 ?

M1CA O4 M2 130.41(6) . 3_656 ?

M1MN O4 M2 130.41(6) . 3_656 ?

M2 O4 M2 119.41(4) 4_566 3_656 ?

M2 O4 M2 76.85(3) 1_556 3_656 ?

P1 O5 M3 129.07(11) . 4_566 ?

P1 O5 M3 112.86(10) . . ?

M3 O5 M3 103.71(8) 4_566 . ?

P1 O5 M1CA 82.14(8) . 4_465 ?

M3 O5 M1CA 102.02(7) 4_566 4_465 ?

M3 O5 M1CA 128.44(8) . 4_465 ?

P1 O5 M2 53.41(6) . 3_656 ?

M3 O5 M2 91.14(6) 4_566 3_656 ?

M3 O5 M2 93.85(6) . 3_656 ?

M1CA O5 M2 129.43(5) 4_465 3_656 ?

P1 O5 M2 144.59(10) . 2_655 ?

M3 O5 M2 72.93(5) 4_566 2_655 ?

M3 O5 M2 81.46(5) . 2_655 ?

M1CA O5 M2 64.71(4) 4_465 2_655 ?

M2 O5 M2 161.61(5) 3_656 2_655 ?

P1 O5 M2 23.77(6) . 1_455 ?

M3 O5 M2 133.48(7) 4_566 1_455 ?

M3 O5 M2 121.54(6) . 1_455 ?

M1CA O5 M2 58.92(3) 4_465 1_455 ?

M2 O5 M2 76.62(3) 3_656 1_455 ?

M2 O5 M2 120.99(5) 2_655 1_455 ?

P1 O5 M2 113.49(9) . . ?

M3 O5 M2 74.44(6) 4_566 . ?

M3 O5 M2 40.03(4) . . ?

M1CA O5 M2 162.69(5) 4_465 . ?

M2 O5 M2 67.87(3) 3_656 . ?

M2 O5 M2 98.31(3) 2_655 . ?

M2 O5 M2 135.51(4) 1_455 . ?

P2 O6 M2 133.83(10) 1_554 . ?

P2 O6 M1CA 97.43(8) 1_554 1_554 ?

M2 O6 M1CA 128.56(8) . 1_554 ?

P2 O6 M1MN 97.43(8) 1_554 1_554 ?

M2 O6 M1MN 128.56(8) . 1_554 ?

M1CA O6 M1MN 0.00(3) 1_554 1_554 ?

P2 O6 M2 77.04(7) 1_554 4_565 ?

M2 O6 M2 109.82(6) . 4_565 ?

M1CA O6 M2 72.53(4) 1_554 4_565 ?

M1MN O6 M2 72.53(4) 1_554 4_565 ?

P2 O6 M2 42.94(5) 1_554 1_554 ?

M2 O6 M2 173.78(8) . 1_554 ?

M1CA O6 M2 55.58(3) 1_554 1_554 ?

M1MN O6 M2 55.58(3) 1_554 1_554 ?

M2 O6 M2 75.42(3) 4_565 1_554 ?

P2 O6 M2 34.84(5) 1_554 3_655 ?

M2 O6 M2 105.67(6) . 3_655 ?

M1CA O6 M2 123.17(6) 1_554 3_655 ?

M1MN O6 M2 123.17(6) 1_554 3_655 ?

M2 O6 M2 106.99(4) 4_565 3_655 ?

M2 O6 M2 69.07(3) 1_554 3_655 ?

P1 O7 M2 134.40(13) . 3_656 ?

P1 O7 M1CA 102.61(10) . 1_455 ?

M2 O7 M1CA 121.99(8) 3_656 1_455 ?

P1 O7 M1MN 102.61(10) . 1_455 ?

M2 O7 M1MN 121.99(8) 3_656 1_455 ?

M1CA O7 M1MN 0.000(12) 1_455 1_455 ?

P1 O7 M2 59.98(7) . 1_455 ?

M2 O7 M2 131.35(7) 3_656 1_455 ?

M1CA O7 M2 62.91(4) 1_455 1_455 ?

M1MN O7 M2 62.91(4) 1_455 1_455 ?

P2 O8 M3 125.68(10) . 3_656 ?

P2 O8 M2 126.57(10) . 3_656 ?

M3 O8 M2 104.84(7) 3_656 3_656 ?

P2 O8 M2 66.30(6) . . ?

M3 O8 M2 108.52(6) 3_656 . ?

M2 O8 M2 116.14(6) 3_656 . ?

P2 O8 M2 55.41(6) . 1_556 ?

M3 O8 M2 83.61(5) 3_656 1_556 ?

M2 O8 M2 123.71(6) 3_656 1_556 ?

M2 O8 M2 112.91(4) . 1_556 ?

_diffrn_measured_fraction_theta_max    1.000

_diffrn_reflns_theta_full              30.06

_diffrn_measured_fraction_theta_full   1.000

_refine_diff_density_max    0.789

_refine_diff_density_min   -0.745

_refine_diff_density_rms    0.102