data_b5

_audit_creation_method            SHELXL-97

_chemical_name_systematic

;

?

;

_chemical_name_common             ?

_chemical_melting_point           ?

_chemical_formula_moiety          ?

_chemical_formula_sum

'Ca2.32 Fe6.62 Mg0.59 Mn2.44 O232 P8'

_chemical_formula_weight          1370.85

loop_

_atom_type_symbol

_atom_type_description

_atom_type_scat_dispersion_real

_atom_type_scat_dispersion_imag

_atom_type_scat_source

'O'  'O2-'   0.0080   0.0060

'International Tables Vol C Tables 4.2.6.8 and 6.1.1.4'

'P'  'P'   0.1023   0.0942

'International Tables Vol C Tables 4.2.6.8 and 6.1.1.4'

'Ca'  'Ca'   0.2262   0.3064

'International Tables Vol C Tables 4.2.6.8 and 6.1.1.4'

'Mn'  'Mn'   0.3368   0.7283

'International Tables Vol C Tables 4.2.6.8 and 6.1.1.4'

'Fe'  'Fe'   0.3463   0.8444

'International Tables Vol C Tables 4.2.6.8 and 6.1.1.4'

'Mg'  'Mg'   0.0486   0.0363

'International Tables Vol C Tables 4.2.6.8 and 6.1.1.4'

_symmetry_cell_setting            ?

_symmetry_space_group_name_H-M    ?

loop_

_symmetry_equiv_pos_as_xyz

'x, y, z'

'-x, y+1/2, -z+1/2'

'-x, -y, -z'

'x, -y-1/2, z-1/2'

_cell_length_a                    8.799

_cell_length_b                    11.570

_cell_length_c                    6.137

_cell_angle_alpha                 90.00

_cell_angle_beta                  99.32

_cell_angle_gamma                 90.00

_cell_volume                      616.5

_cell_formula_units_Z             1

_cell_measurement_temperature     293(2)

_cell_measurement_reflns_used     ?

_cell_measurement_theta_min       ?

_cell_measurement_theta_max       ?

_exptl_crystal_description        ?

_exptl_crystal_colour             ?

_exptl_crystal_size_max           ?

_exptl_crystal_size_mid           ?

_exptl_crystal_size_min           ?

_exptl_crystal_density_meas       ?

_exptl_crystal_density_diffrn     3.692

_exptl_crystal_density_method     'not measured'

_exptl_crystal_F_000              712

_exptl_absorpt_coefficient_mu     6.134

_exptl_absorpt_correction_type    ?

_exptl_absorpt_correction_T_min   ?

_exptl_absorpt_correction_T_max   ?

_exptl_absorpt_process_details    ?

_exptl_special_details

;

?

;

_diffrn_ambient_temperature       293(2)

_diffrn_radiation_wavelength      0.71073

_diffrn_radiation_type            MoK\a

_diffrn_radiation_source          'fine-focus sealed tube'

_diffrn_radiation_monochromator   graphite

_diffrn_measurement_device_type   ?

_diffrn_measurement_method        ?

_diffrn_detector_area_resol_mean  ?

_diffrn_reflns_number             1969

_diffrn_reflns_av_R_equivalents   0.0113

_diffrn_reflns_av_sigmaI/netI     0.0217

_diffrn_reflns_limit_h_min        -12

_diffrn_reflns_limit_h_max        12

_diffrn_reflns_limit_k_min        0

_diffrn_reflns_limit_k_max        16

_diffrn_reflns_limit_l_min        0

_diffrn_reflns_limit_l_max        8

_diffrn_reflns_theta_min          2.93

_diffrn_reflns_theta_max          30.05

_reflns_number_total              1813

_reflns_number_gt                 1592

_reflns_threshold_expression      >2sigma(I)

_computing_data_collection        ?

_computing_cell_refinement        ?

_computing_data_reduction         ?

_computing_structure_solution     'SHELXS-97 (Sheldrick, 2008)'

_computing_structure_refinement   'SHELXL-97 (Sheldrick, 2008)'

_computing_molecular_graphics     ?

_computing_publication_material   ?

_refine_special_details

;

Refinement of F^2^ against ALL reflections.  The weighted R-factor wR and

goodness of fit S are based on F^2^, conventional R-factors R are based

on F, with F set to zero for negative F^2^. The threshold expression of

F^2^ > 2sigma(F^2^) is used only for calculating R-factors(gt) etc. and is

not relevant to the choice of reflections for refinement.  R-factors based

on F^2^ are statistically about twice as large as those based on F, and R-

factors based on ALL data will be even larger.

;

_refine_ls_structure_factor_coef  Fsqd

_refine_ls_matrix_type            full

_refine_ls_weighting_scheme       calc

_refine_ls_weighting_details

'calc w=1/[\s^2^(Fo^2^)+(0.1000P)^2^+0.0000P] where P=(Fo^2^+2Fc^2^)/3'

_atom_sites_solution_primary      direct

_atom_sites_solution_secondary    difmap

_atom_sites_solution_hydrogens    geom

_refine_ls_hydrogen_treatment     mixed

_refine_ls_extinction_method      none

_refine_ls_extinction_coef        ?

_refine_ls_number_reflns          1813

_refine_ls_number_parameters      121

_refine_ls_number_restraints      0

_refine_ls_R_factor_all           0.0353

_refine_ls_R_factor_gt            0.0302

_refine_ls_wR_factor_ref          0.1067

_refine_ls_wR_factor_gt           0.1022

_refine_ls_goodness_of_fit_ref    0.856

_refine_ls_restrained_S_all       0.856

_refine_ls_shift/su_max           9.428

_refine_ls_shift/su_mean          0.078

loop_

_atom_site_label

_atom_site_type_symbol

_atom_site_fract_x

_atom_site_fract_y

_atom_site_fract_z

_atom_site_U_iso_or_equiv

_atom_site_adp_type

_atom_site_occupancy

_atom_site_symmetry_multiplicity

_atom_site_calc_flag

_atom_site_refinement_flags

_atom_site_disorder_assembly

_atom_site_disorder_group

M1CA Ca 0.94688(7) 0.12103(5) 0.83518(10) 0.01875(19) Uani 0.526(13) 1 d P . .

M1MN Mn 0.94688(7) 0.12103(5) 0.83518(10) 0.01875(19) Uani 0.474(13) 1 d P . .

M2 Fe 0.71462(6) 0.07891(5) 0.32686(8) 0.02071(19) Uani 0.960(3) 1 d P . .

M3 Mn 0.36258(5) 0.19165(4) 0.12925(7) 0.01262(17) Uani 1.000(3) 1 d . . .

P1 P 0.09476(8) 0.13445(7) 0.39630(12) 0.00999(19) Uani 1 1 d . . .

P2 P 0.60221(8) 0.08856(6) 0.80641(12) 0.00881(19) Uani 1 1 d . . .

O1 O2- 0.0798(3) 0.0690(2) 0.1773(4) 0.0158(5) Uani 1 1 d . . .

O2 O2- 0.4732(3) 0.17525(19) 0.8292(4) 0.0128(4) Uani 1 1 d . . .

03 O2- 0.9420(3) 0.1925(2) 0.4231(5) 0.0229(5) Uani 1 1 d . . .

04 O2- 0.6894(3) 0.1267(2) 0.6230(4) 0.0136(4) Uani 1 1 d . . .

05 O2- 0.2171(3) 0.2289(2) 0.3832(4) 0.0187(5) Uani 1 1 d . . .

06 O2- 0.7256(2) 0.08990(19) 0.0148(4) 0.0123(4) Uani 1 1 d . . .

07 O2- 0.1420(3) 0.0592(2) 0.5991(4) 0.0178(5) Uani 1 1 d . . .

O8 O2- 0.5350(3) -0.03489(19) 0.7647(4) 0.0125(4) Uani 1 1 d . . .

loop_

_atom_site_aniso_label

_atom_site_aniso_U_11

_atom_site_aniso_U_22

_atom_site_aniso_U_33

_atom_site_aniso_U_23

_atom_site_aniso_U_13

_atom_site_aniso_U_12

M1CA 0.0193(3) 0.0126(3) 0.0215(3) -0.0042(2) -0.0052(2) 0.00203(19)

M1MN 0.0193(3) 0.0126(3) 0.0215(3) -0.0042(2) -0.0052(2) 0.00203(19)

M2 0.0212(3) 0.0340(3) 0.0071(3) 0.00027(18) 0.00263(18) 0.0083(2)

M3 0.0143(3) 0.0129(3) 0.0103(3) 0.00021(15) 0.00113(17) 0.00202(15)

P1 0.0088(3) 0.0121(3) 0.0091(3) -0.0009(2) 0.0017(2) -0.0007(2)

P2 0.0091(3) 0.0108(3) 0.0067(3) 0.0002(2) 0.0017(2) 0.0010(2)

O1 0.0198(11) 0.0159(10) 0.0118(10) -0.0039(8) 0.0027(8) -0.0009(8)

O2 0.0121(9) 0.0144(10) 0.0124(10) 0.0016(8) 0.0032(8) 0.0040(8)

03 0.0137(11) 0.0352(15) 0.0211(12) -0.0061(10) 0.0067(9) 0.0090(10)

04 0.0145(10) 0.0188(11) 0.0080(9) 0.0015(8) 0.0037(8) -0.0011(8)

05 0.0246(12) 0.0194(11) 0.0125(10) 0.0007(9) 0.0043(9) -0.0135(9)

06 0.0095(9) 0.0207(11) 0.0066(9) 0.0008(7) 0.0009(7) 0.0012(8)

07 0.0245(12) 0.0150(10) 0.0131(10) 0.0039(8) 0.0004(9) -0.0034(9)

O8 0.0128(9) 0.0130(10) 0.0120(9) 0.0004(7) 0.0031(7) -0.0005(8)

_geom_special_details

;

All esds (except the esd in the dihedral angle between two l.s. planes)

are estimated using the full covariance matrix.  The cell esds are taken

into account individually in the estimation of esds in distances, angles

and torsion angles; correlations between esds in cell parameters are only

used when they are defined by crystal symmetry.  An approximate (isotropic)

treatment of cell esds is used for estimating esds involving l.s. planes.

;

loop_

_geom_bond_atom_site_label_1

_geom_bond_atom_site_label_2

_geom_bond_distance

_geom_bond_site_symmetry_2

_geom_bond_publ_flag

M1CA O1 2.212(2) 3_656 ?

M1CA 03 2.226(3) 4_566 ?

M1CA O1 2.312(2) 1_656 ?

M1CA 06 2.415(2) 1_556 ?

M1CA 04 2.424(2) . ?

M1CA 07 2.523(3) 1_655 ?

M1CA 03 2.654(3) . ?

M1CA 05 2.920(3) 4_666 ?

M1CA P2 3.0326(9) . ?

M1CA P1 3.1112(9) 4_666 ?

M1CA P1 3.1791(10) 1_655 ?

M1CA P1 3.2743(9) 3_656 ?

M1MN O1 2.212(2) 3_656 ?

M1MN 03 2.226(3) 4_566 ?

M1MN O1 2.312(2) 1_656 ?

M1MN 06 2.415(2) 1_556 ?

M1MN 04 2.424(2) . ?

M1MN 07 2.523(3) 1_655 ?

M1MN M2 3.4757(8) . ?

M1MN M1CA 3.4925(12) 3_757 ?

M1MN M2 3.9391(8) 1_556 ?

M1MN M2 4.0213(8) 3_756 ?

M1MN M2 4.0246(8) 4_566 ?

M2 06 1.937(2) . ?

M2 04 1.946(2) . ?

M2 07 2.041(3) 3_656 ?

M2 O8 2.236(2) 3_656 ?

M2 03 2.386(3) . ?

M2 P2 3.1889(9) 1_554 ?

M2 P2 3.2549(9) . ?

M2 P1 3.2971(9) 3_656 ?

M2 P1 3.3647(9) 1_655 ?

M2 P2 3.3848(9) 3_656 ?

M2 M3 3.3986(7) . ?

M2 O2 3.433(2) 3_656 ?

M2 O1 3.484(2) 1_655 ?

M2 O2 3.552(2) 4_565 ?

M2 O8 3.582(2) . ?

M2 O2 3.603(2) 1_554 ?

M2 04 3.623(2) 4_565 ?

M2 O1 3.698(2) 3_656 ?

M2 O8 3.790(2) 1_554 ?

M2 07 3.867(3) 1_655 ?

M2 M1CA 3.9392(8) 1_554 ?

M2 M1MN 3.9392(8) 1_554 ?

M2 P2 3.9693(9) 4_565 ?

M2 05 3.983(3) 3_656 ?

M2 06 3.998(2) 4_566 ?

M2 M1MN 4.0213(8) 3_756 ?

M2 M1CA 4.0213(8) 3_756 ?

M2 M1CA 4.0247(8) 4_565 ?

M2 M1MN 4.0247(8) 4_565 ?

M2 O2 4.169(2) . ?

M2 M3 4.1810(7) 3_655 ?

M2 O1 4.194(2) 3_655 ?

M2 06 4.209(2) 1_556 ?

M2 05 4.321(2) 2_645 ?

M2 04 4.325(2) 1_554 ?

M2 03 4.329(3) 4_565 ?

M2 04 4.330(2) 3_656 ?

M2 03 4.455(3) 3_756 ?

M3 05 2.034(2) 4_565 ?

M3 O8 2.082(2) 3_656 ?

M3 O2 2.107(2) 4_565 ?

M3 05 2.214(3) . ?

M3 O2 2.226(2) 1_554 ?

M3 M2 4.1810(7) 3_655 ?

M3 M2 4.5464(7) 2_655 ?

M3 M2 4.6848(7) 4_565 ?

M3 M2 4.7049(7) 3_656 ?

M3 M2 5.5385(7) 4_566 ?

P1 07 1.520(2) . ?

P1 O1 1.529(2) . ?

P1 03 1.535(2) 1_455 ?

P1 05 1.545(2) . ?

P1 M1CA 3.1111(9) 4_465 ?

P1 M1CA 3.1791(10) 1_455 ?

P1 M1CA 3.2744(9) 3_656 ?

P1 M2 3.2971(9) 3_656 ?

P1 M2 3.3647(9) 1_455 ?

P1 M1CA 3.4820(9) 1_454 ?

P1 M2 5.5329(9) 4_465 ?

P1 M2 5.5691(9) 3_655 ?

P2 04 1.527(2) . ?

P2 O2 1.538(2) . ?

P2 06 1.538(2) 1_556 ?

P2 O8 1.551(2) . ?

P2 M2 3.1889(9) 1_556 ?

P2 M2 3.3848(9) 3_656 ?

P2 M2 3.9693(9) 4_566 ?

O1 M1MN 2.212(2) 3_656 ?

O1 M1CA 2.212(2) 3_656 ?

O1 M1CA 2.312(2) 1_454 ?

O1 M1MN 2.312(2) 1_454 ?

O1 M2 3.484(2) 1_455 ?

O1 M2 3.698(2) 3_656 ?

O1 M2 4.194(2) 3_655 ?

O2 M3 2.107(2) 4_566 ?

O2 M3 2.226(2) 1_556 ?

O2 M2 3.433(2) 3_656 ?

O2 M2 3.552(2) 4_566 ?

O2 M2 3.603(2) 1_556 ?

03 P1 1.535(2) 1_655 ?

03 M1MN 2.226(3) 4_565 ?

03 M1CA 2.226(3) 4_565 ?

03 M2 4.329(3) 4_566 ?

03 M2 4.455(3) 3_756 ?

03 M2 4.692(3) 4_565 ?

04 M2 3.623(2) 4_566 ?

04 M2 4.325(2) 1_556 ?

04 M2 4.330(2) 3_656 ?

05 M3 2.034(2) 4_566 ?

05 M1CA 2.920(3) 4_465 ?

05 M2 3.984(3) 3_656 ?

05 M2 4.321(2) 2_655 ?

05 M2 4.710(2) 1_455 ?

06 P2 1.538(2) 1_554 ?

06 M1CA 2.415(2) 1_554 ?

06 M1MN 2.415(2) 1_554 ?

06 M2 3.998(2) 4_565 ?

06 M2 4.209(2) 1_554 ?

06 M2 4.537(2) 3_655 ?

07 M2 2.041(3) 3_656 ?

07 M1CA 2.523(3) 1_455 ?

07 M1MN 2.523(3) 1_455 ?

07 M2 3.867(3) 1_455 ?

O8 M3 2.082(2) 3_656 ?

O8 M2 2.236(2) 3_656 ?

O8 M2 3.790(2) 1_556 ?

loop_

_geom_angle_atom_site_label_1

_geom_angle_atom_site_label_2

_geom_angle_atom_site_label_3

_geom_angle

_geom_angle_site_symmetry_1

_geom_angle_site_symmetry_3

_geom_angle_publ_flag

O1 M1CA 03 165.01(9) 3_656 4_566 ?

O1 M1CA O1 78.94(9) 3_656 1_656 ?

03 M1CA O1 93.37(9) 4_566 1_656 ?

O1 M1CA 06 77.21(8) 3_656 1_556 ?

03 M1CA 06 89.15(9) 4_566 1_556 ?

O1 M1CA 06 82.72(8) 1_656 1_556 ?

O1 M1CA 04 85.61(8) 3_656 . ?

03 M1CA 04 92.91(9) 4_566 . ?

O1 M1CA 04 141.85(8) 1_656 . ?

06 M1CA 04 59.79(7) 1_556 . ?

O1 M1CA 07 77.09(8) 3_656 1_655 ?

03 M1CA 07 117.11(9) 4_566 1_655 ?

O1 M1CA 07 99.01(8) 1_656 1_655 ?

06 M1CA 07 153.38(8) 1_556 1_655 ?

04 M1CA 07 111.28(8) . 1_655 ?

O1 M1CA 03 106.94(9) 3_656 . ?

03 M1CA 03 86.05(7) 4_566 . ?

O1 M1CA 03 150.96(9) 1_656 . ?

06 M1CA 03 126.26(8) 1_556 . ?

04 M1CA 03 67.05(8) . . ?

07 M1CA 03 56.55(7) 1_655 . ?

O1 M1CA 05 132.44(8) 3_656 4_666 ?

03 M1CA 05 56.41(8) 4_566 4_666 ?

O1 M1CA 05 77.24(8) 1_656 4_666 ?

06 M1CA 05 138.26(8) 1_556 4_666 ?

04 M1CA 05 135.47(8) . 4_666 ?

07 M1CA 05 66.90(7) 1_655 4_666 ?

03 M1CA 05 78.36(8) . 4_666 ?

O1 M1CA P2 77.01(7) 3_656 . ?

03 M1CA P2 94.34(7) 4_566 . ?

O1 M1CA P2 112.01(6) 1_656 . ?

06 M1CA P2 30.16(5) 1_556 . ?

04 M1CA P2 29.93(5) . . ?

07 M1CA P2 134.32(6) 1_655 . ?

03 M1CA P2 96.97(6) . . ?

05 M1CA P2 150.43(5) 4_666 . ?

O1 M1CA P1 161.51(7) 3_656 4_666 ?

03 M1CA P1 27.58(7) 4_566 4_666 ?

O1 M1CA P1 89.25(6) 1_656 4_666 ?

06 M1CA P1 115.66(6) 1_556 4_666 ?

04 M1CA P1 112.11(6) . 4_666 ?

07 M1CA P1 90.96(6) 1_655 4_666 ?

03 M1CA P1 76.91(7) . 4_666 ?

05 M1CA P1 29.47(5) 4_666 4_666 ?

P2 M1CA P1 120.96(3) . 4_666 ?

O1 M1CA P1 94.30(6) 3_656 1_655 ?

03 M1CA P1 100.65(7) 4_566 1_655 ?

O1 M1CA P1 124.47(6) 1_656 1_655 ?

06 M1CA P1 149.88(6) 1_556 1_655 ?

04 M1CA P1 91.07(6) . 1_655 ?

07 M1CA P1 28.03(5) 1_655 1_655 ?

03 M1CA P1 28.76(5) . 1_655 ?

05 M1CA P1 67.55(5) 4_666 1_655 ?

P2 M1CA P1 119.96(3) . 1_655 ?

P1 M1CA P1 80.63(2) 4_666 1_655 ?

O1 M1CA P1 23.58(6) 3_656 3_656 ?

03 M1CA P1 167.14(7) 4_566 3_656 ?

O1 M1CA P1 99.43(6) 1_656 3_656 ?

06 M1CA P1 91.23(6) 1_556 3_656 ?

04 M1CA P1 76.24(6) . 3_656 ?

07 M1CA P1 62.20(6) 1_655 3_656 ?

03 M1CA P1 83.37(6) . 3_656 ?

05 M1CA P1 127.78(5) 4_666 3_656 ?

P2 M1CA P1 79.76(2) . 3_656 ?

P1 M1CA P1 152.68(2) 4_666 3_656 ?

P1 M1CA P1 73.08(2) 1_655 3_656 ?

O1 M1MN 03 165.01(9) 3_656 4_566 ?

O1 M1MN O1 78.94(9) 3_656 1_656 ?

03 M1MN O1 93.37(9) 4_566 1_656 ?

O1 M1MN 06 77.21(8) 3_656 1_556 ?

03 M1MN 06 89.15(9) 4_566 1_556 ?

O1 M1MN 06 82.72(8) 1_656 1_556 ?

O1 M1MN 04 85.61(8) 3_656 . ?

03 M1MN 04 92.91(9) 4_566 . ?

O1 M1MN 04 141.85(8) 1_656 . ?

06 M1MN 04 59.79(7) 1_556 . ?

O1 M1MN 07 77.09(8) 3_656 1_655 ?

03 M1MN 07 117.11(9) 4_566 1_655 ?

O1 M1MN 07 99.01(8) 1_656 1_655 ?

06 M1MN 07 153.38(8) 1_556 1_655 ?

04 M1MN 07 111.28(8) . 1_655 ?

O1 M1MN M2 77.63(6) 3_656 . ?

03 M1MN M2 108.77(7) 4_566 . ?

O1 M1MN M2 156.39(6) 1_656 . ?

06 M1MN M2 89.34(6) 1_556 . ?

04 M1MN M2 32.77(5) . . ?

07 M1MN M2 78.51(6) 1_655 . ?

O1 M1MN M1CA 40.51(6) 3_656 3_757 ?

03 M1MN M1CA 130.59(8) 4_566 3_757 ?

O1 M1MN M1CA 38.43(6) 1_656 3_757 ?

06 M1MN M1CA 77.05(6) 1_556 3_757 ?

04 M1MN M1CA 118.17(6) . 3_757 ?

07 M1MN M1CA 87.83(6) 1_655 3_757 ?

M2 M1MN M1CA 118.08(3) . 3_757 ?

O1 M1MN M2 80.69(6) 3_656 1_556 ?

03 M1MN M2 84.33(7) 4_566 1_556 ?

O1 M1MN M2 61.38(6) 1_656 1_556 ?

06 M1MN M2 22.35(5) 1_556 1_556 ?

04 M1MN M2 81.91(5) . 1_556 ?

07 M1MN M2 152.96(6) 1_655 1_556 ?

M2 M1MN M2 111.57(2) . 1_556 ?

M1CA M1MN M2 65.20(2) 3_757 1_556 ?

O1 M1MN M2 59.88(6) 3_656 3_756 ?

03 M1MN M2 131.43(7) 4_566 3_756 ?

O1 M1MN M2 77.81(6) 1_656 3_756 ?

06 M1MN M2 135.34(6) 1_556 3_756 ?

04 M1MN M2 123.22(6) . 3_756 ?

07 M1MN M2 25.13(5) 1_655 3_756 ?

M2 M1MN M2 92.797(18) . 3_756 ?

M1CA M1MN M2 62.771(19) 3_757 3_756 ?

M2 M1MN M2 127.967(17) 1_556 3_756 ?

O1 M1MN M2 143.75(7) 3_656 4_566 ?

03 M1MN M2 30.38(7) 4_566 4_566 ?

O1 M1MN M2 114.66(6) 1_656 4_566 ?

06 M1MN M2 71.89(5) 1_556 4_566 ?

04 M1MN M2 62.70(6) . 4_566 ?

07 M1MN M2 128.95(6) 1_655 4_566 ?

M2 M1MN M2 83.453(18) . 4_566 ?

M1CA M1MN M2 141.89(3) 3_757 4_566 ?

M2 M1MN M2 77.938(17) 1_556 4_566 ?

M2 M1MN M2 152.63(2) 3_756 4_566 ?

06 M2 04 159.37(10) . . ?

06 M2 07 98.25(10) . 3_656 ?

04 M2 07 100.04(10) . 3_656 ?

06 M2 O8 88.32(9) . 3_656 ?

04 M2 O8 92.50(9) . 3_656 ?

07 M2 O8 115.09(9) 3_656 3_656 ?

06 M2 03 91.98(10) . . ?

04 M2 03 80.22(9) . . ?

07 M2 03 85.01(9) 3_656 . ?

O8 M2 03 159.65(9) 3_656 . ?

06 M2 P2 20.71(7) . 1_554 ?

04 M2 P2 149.48(7) . 1_554 ?

07 M2 P2 109.31(7) 3_656 1_554 ?

O8 M2 P2 67.88(6) 3_656 1_554 ?

03 M2 P2 109.89(7) . 1_554 ?

06 M2 P2 164.30(7) . . ?

04 M2 P2 17.97(7) . . ?

07 M2 P2 95.33(7) 3_656 . ?

O8 M2 P2 78.77(6) 3_656 . ?

03 M2 P2 97.04(7) . . ?

P2 M2 P2 144.49(3) 1_554 . ?

06 M2 P1 117.12(7) . 3_656 ?

04 M2 P1 81.78(7) . 3_656 ?

07 M2 P1 19.01(7) 3_656 3_656 ?

O8 M2 P1 110.86(6) 3_656 3_656 ?

03 M2 P1 87.06(7) . 3_656 ?

P2 M2 P1 126.28(2) 1_554 3_656 ?

P2 M2 P1 76.32(2) . 3_656 ?

06 M2 P1 84.54(7) . 1_655 ?

04 M2 P1 95.10(7) . 1_655 ?

07 M2 P1 63.61(7) 3_656 1_655 ?

O8 M2 P1 172.41(6) 3_656 1_655 ?

03 M2 P1 24.10(6) . 1_655 ?

P2 M2 P1 105.12(2) 1_554 1_655 ?

P2 M2 P1 108.68(2) . 1_655 ?

P1 M2 P1 70.45(2) 3_656 1_655 ?

06 M2 P2 88.26(7) . 3_656 ?

04 M2 P2 100.04(7) . 3_656 ?

07 M2 P2 93.48(7) 3_656 3_656 ?

O8 M2 P2 21.84(6) 3_656 3_656 ?

03 M2 P2 178.49(7) . 3_656 ?

P2 M2 P2 70.63(2) 1_554 3_656 ?

P2 M2 P2 83.06(2) . 3_656 ?

P1 M2 P2 91.50(2) 3_656 3_656 ?

P1 M2 P2 154.54(3) 1_655 3_656 ?

06 M2 M3 79.08(7) . . ?

04 M2 M3 89.37(7) . . ?

07 M2 M3 151.00(7) 3_656 . ?

O8 M2 M3 36.51(6) 3_656 . ?

03 M2 M3 123.78(7) . . ?

P2 M2 M3 60.807(17) 1_554 . ?

P2 M2 M3 85.218(19) . . ?

P1 M2 M3 146.04(2) 3_656 . ?

P1 M2 M3 143.30(2) 1_655 . ?

P2 M2 M3 57.728(16) 3_656 . ?

06 M2 O2 83.06(8) . 3_656 ?

04 M2 O2 112.43(8) . 3_656 ?

07 M2 O2 69.12(8) 3_656 3_656 ?

O8 M2 O2 47.61(7) 3_656 3_656 ?

03 M2 O2 152.52(7) . 3_656 ?

P2 M2 O2 72.14(4) 1_554 3_656 ?

P2 M2 O2 94.52(4) . 3_656 ?

P1 M2 O2 71.59(4) 3_656 3_656 ?

P1 M2 O2 128.51(4) 1_655 3_656 ?

P2 M2 O2 26.07(4) 3_656 3_656 ?

M3 M2 O2 81.92(4) . 3_656 ?

06 M2 M1CA 139.62(7) . . ?

04 M2 M1CA 42.40(7) . . ?

07 M2 M1CA 69.98(7) 3_656 . ?

O8 M2 M1CA 131.95(6) 3_656 . ?

03 M2 M1CA 49.69(7) . . ?

P2 M2 M1CA 159.38(3) 1_554 . ?

P2 M2 M1CA 53.437(18) . . ?

P1 M2 M1CA 57.750(18) 3_656 . ?

P1 M2 M1CA 55.359(18) 1_655 . ?

P2 M2 M1CA 129.70(2) 3_656 . ?

M3 M2 M1CA 129.49(2) . . ?

O2 M2 M1CA 123.86(4) 3_656 . ?

06 M2 M1MN 139.62(7) . . ?

04 M2 M1MN 42.40(7) . . ?

07 M2 M1MN 69.98(7) 3_656 . ?

O8 M2 M1MN 131.95(6) 3_656 . ?

03 M2 M1MN 49.69(7) . . ?

P2 M2 M1MN 159.38(3) 1_554 . ?

P2 M2 M1MN 53.437(18) . . ?

P1 M2 M1MN 57.750(18) 3_656 . ?

P1 M2 M1MN 55.359(18) 1_655 . ?

P2 M2 M1MN 129.70(2) 3_656 . ?

M3 M2 M1MN 129.49(2) . . ?

O2 M2 M1MN 123.86(4) 3_656 . ?

M1CA M2 M1MN 0.0 . . ?

06 M2 O1 62.99(8) . 1_655 ?

04 M2 O1 120.32(8) . 1_655 ?

07 M2 O1 57.98(8) 3_656 1_655 ?

O8 M2 O1 146.80(7) 3_656 1_655 ?

03 M2 O1 46.47(7) . 1_655 ?

P2 M2 O1 83.51(4) 1_554 1_655 ?

P2 M2 O1 131.88(4) . 1_655 ?

P1 M2 O1 72.38(4) 3_656 1_655 ?

P1 M2 O1 25.73(4) 1_655 1_655 ?

P2 M2 O1 132.56(4) 3_656 1_655 ?

M3 M2 O1 138.15(4) . 1_655 ?

O2 M2 O1 108.74(5) 3_656 1_655 ?

M1CA M2 O1 78.91(4) . 1_655 ?

M1MN M2 O1 78.91(4) . 1_655 ?

06 M2 O2 94.43(8) . 4_565 ?

04 M2 O2 67.04(8) . 4_565 ?

07 M2 O2 167.07(8) 3_656 4_565 ?

O8 M2 O2 67.64(7) 3_656 4_565 ?

03 M2 O2 92.06(7) . 4_565 ?

P2 M2 O2 83.53(4) 1_554 4_565 ?

P2 M2 O2 72.50(4) . 4_565 ?

P1 M2 O2 148.46(4) 3_656 4_565 ?

P1 M2 O2 115.44(4) 1_655 4_565 ?

P2 M2 O2 89.41(4) 3_656 4_565 ?

M3 M2 O2 35.20(4) . 4_565 ?

O2 M2 O2 115.215(17) 3_656 4_565 ?

M1CA M2 O2 98.58(4) . 4_565 ?

M1MN M2 O2 98.58(4) . 4_565 ?

O1 M2 O2 127.24(6) 1_655 4_565 ?

06 M2 O8 149.83(8) . . ?

04 M2 O8 43.37(8) . . ?

07 M2 O8 82.93(8) 3_656 . ?

O8 M2 O8 64.54(8) 3_656 . ?

03 M2 O8 118.08(8) . . ?

P2 M2 O8 131.41(4) 1_554 . ?

P2 M2 O8 25.66(4) . . ?

P1 M2 O8 65.64(4) 3_656 . ?

P1 M2 O8 121.70(4) 1_655 . ?

P2 M2 O8 61.62(4) 3_656 . ?

M3 M2 O8 85.49(4) . . ?

O2 M2 O8 69.12(5) 3_656 . ?

M1CA M2 O8 69.20(4) . . ?

M1MN M2 O8 69.20(4) . . ?

O1 M2 O8 136.34(5) 1_655 . ?

O2 M2 O8 87.39(5) 4_565 . ?

06 M2 O2 42.16(7) . 1_554 ?

04 M2 O2 124.25(8) . 1_554 ?

07 M2 O2 133.57(8) 3_656 1_554 ?

O8 M2 O2 55.74(7) 3_656 1_554 ?

03 M2 O2 113.27(8) . 1_554 ?

P2 M2 O2 25.25(4) 1_554 1_554 ?

P2 M2 O2 122.14(4) . 1_554 ?

P1 M2 O2 148.14(4) 3_656 1_554 ?

P1 M2 O2 119.07(4) 1_655 1_554 ?

P2 M2 O2 67.84(4) 3_656 1_554 ?

M3 M2 O2 36.92(4) . 1_554 ?

O2 M2 O2 80.64(6) 3_656 1_554 ?

M1CA M2 O2 153.86(4) . 1_554 ?

M1MN M2 O2 153.86(4) . 1_554 ?

O1 M2 O2 103.26(5) 1_655 1_554 ?

O2 M2 O2 58.98(4) 4_565 1_554 ?

O8 M2 O2 118.59(5) . 1_554 ?

06 M2 04 66.86(8) . 4_565 ?

04 M2 04 92.61(6) . 4_565 ?

07 M2 04 144.50(8) 3_656 4_565 ?

O8 M2 04 97.16(7) 3_656 4_565 ?

03 M2 04 64.52(8) . 4_565 ?

P2 M2 04 68.25(4) 1_554 4_565 ?

P2 M2 04 105.63(4) . 4_565 ?

P1 M2 04 151.58(4) 3_656 4_565 ?

P1 M2 04 82.43(4) 1_655 4_565 ?

P2 M2 04 116.92(4) 3_656 4_565 ?

M3 M2 04 60.96(4) . 4_565 ?

O2 M2 04 135.17(5) 3_656 4_565 ?

M1CA M2 04 99.93(4) . 4_565 ?

M1MN M2 04 99.93(4) . 4_565 ?

O1 M2 04 86.98(5) 1_655 4_565 ?

O2 M2 04 41.00(5) 4_565 4_565 ?

O8 M2 04 126.51(5) . 4_565 ?

O2 M2 04 54.67(5) 1_554 4_565 ?

06 M2 O1 138.38(8) . 3_656 ?

04 M2 O1 58.52(8) . 3_656 ?

07 M2 O1 41.59(8) 3_656 3_656 ?

O8 M2 O1 115.53(7) 3_656 3_656 ?

03 M2 O1 76.85(8) . 3_656 ?

P2 M2 O1 150.61(4) 1_554 3_656 ?

P2 M2 O1 56.75(4) . 3_656 ?

P1 M2 O1 24.40(4) 3_656 3_656 ?

P1 M2 O1 68.93(4) 1_655 3_656 ?

P2 M2 O1 101.99(4) 3_656 3_656 ?

M3 M2 O1 140.11(4) . 3_656 ?

O2 M2 O1 88.98(5) 3_656 3_656 ?

M1CA M2 O1 35.74(4) . 3_656 ?

M1MN M2 O1 35.74(4) . 3_656 ?

O1 M2 O1 81.52(6) 1_655 3_656 ?

O2 M2 O1 125.49(5) 4_565 3_656 ?

O8 M2 O1 55.18(5) . 3_656 ?

O2 M2 O1 169.50(5) 1_554 3_656 ?

04 M2 O1 135.54(5) 4_565 3_656 ?

06 M2 O8 37.18(8) . 1_554 ?

04 M2 O8 148.73(8) . 1_554 ?

07 M2 O8 94.71(8) 3_656 1_554 ?

O8 M2 O8 56.24(8) 3_656 1_554 ?

03 M2 O8 128.74(7) . 1_554 ?

P2 M2 O8 23.73(4) 1_554 1_554 ?

P2 M2 O8 133.78(4) . 1_554 ?

P1 M2 O8 108.13(4) 3_656 1_554 ?

P1 M2 O8 116.17(4) 1_655 1_554 ?

P2 M2 O8 51.36(4) 3_656 1_554 ?

M3 M2 O8 65.61(4) . 1_554 ?

O2 M2 O8 48.51(5) 3_656 1_554 ?

M1CA M2 O8 164.47(4) . 1_554 ?

M1MN M2 O8 164.47(4) . 1_554 ?

O1 M2 O8 90.87(5) 1_655 1_554 ?

O2 M2 O8 96.92(5) 4_565 1_554 ?

O8 M2 O8 112.68(6) . 1_554 ?

O2 M2 O8 40.03(5) 1_554 1_554 ?

04 M2 O8 91.09(5) 4_565 1_554 ?

O1 M2 O8 131.63(5) 3_656 1_554 ?

06 M2 07 103.31(8) . 1_655 ?

04 M2 07 82.14(8) . 1_655 ?

07 M2 07 48.31(9) 3_656 1_655 ?

O8 M2 07 160.43(7) 3_656 1_655 ?

03 M2 07 37.61(7) . 1_655 ?

P2 M2 07 123.85(4) 1_554 1_655 ?

P2 M2 07 91.61(4) . 1_655 ?

P1 M2 07 49.85(4) 3_656 1_655 ?

P1 M2 07 22.95(4) 1_655 1_655 ?

P2 M2 07 140.90(4) 3_656 1_655 ?

M3 M2 07 160.61(4) . 1_655 ?

O2 M2 07 117.43(5) 3_656 1_655 ?

M1CA M2 07 39.75(4) . 1_655 ?

M1MN M2 07 39.75(4) . 1_655 ?

O1 M2 07 40.34(5) 1_655 1_655 ?

O2 M2 07 125.87(5) 4_565 1_655 ?

O8 M2 07 99.82(5) . 1_655 ?

O2 M2 07 141.55(5) 1_554 1_655 ?

04 M2 07 101.86(5) 4_565 1_655 ?

O1 M2 07 46.00(5) 3_656 1_655 ?

O8 M2 07 127.28(5) 1_554 1_655 ?

06 M2 M1CA 28.30(7) . 1_554 ?

04 M2 M1CA 146.29(7) . 1_554 ?

07 M2 M1CA 83.62(7) 3_656 1_554 ?

O8 M2 M1CA 116.49(6) 3_656 1_554 ?

03 M2 M1CA 66.63(7) . 1_554 ?

P2 M2 M1CA 48.978(17) 1_554 1_554 ?

P2 M2 M1CA 163.67(2) . 1_554 ?

P1 M2 M1CA 101.75(2) 3_656 1_554 ?

P1 M2 M1CA 56.284(17) 1_655 1_554 ?

P2 M2 M1CA 113.260(19) 3_656 1_554 ?

M3 M2 M1CA 103.600(16) . 1_554 ?

O2 M2 M1CA 100.27(4) 3_656 1_554 ?

M1CA M2 M1CA 111.57(2) . 1_554 ?

M1MN M2 M1CA 111.57(2) . 1_554 ?

O1 M2 M1CA 35.62(4) 1_655 1_554 ?

O2 M2 M1CA 106.80(4) 4_565 1_554 ?

O8 M2 M1CA 165.22(4) . 1_554 ?

O2 M2 M1CA 67.68(4) 1_554 1_554 ?

04 M2 M1CA 68.25(4) 4_565 1_554 ?

O1 M2 M1CA 116.24(4) 3_656 1_554 ?

O8 M2 M1CA 62.44(3) 1_554 1_554 ?

07 M2 M1CA 75.48(4) 1_655 1_554 ?

06 M2 M1MN 28.30(7) . 1_554 ?

04 M2 M1MN 146.29(7) . 1_554 ?

07 M2 M1MN 83.62(7) 3_656 1_554 ?

O8 M2 M1MN 116.49(6) 3_656 1_554 ?

03 M2 M1MN 66.63(7) . 1_554 ?

P2 M2 M1MN 48.978(17) 1_554 1_554 ?

P2 M2 M1MN 163.67(2) . 1_554 ?

P1 M2 M1MN 101.75(2) 3_656 1_554 ?

P1 M2 M1MN 56.284(17) 1_655 1_554 ?

P2 M2 M1MN 113.260(19) 3_656 1_554 ?

M3 M2 M1MN 103.600(16) . 1_554 ?

O2 M2 M1MN 100.27(4) 3_656 1_554 ?

M1CA M2 M1MN 111.57(2) . 1_554 ?

M1MN M2 M1MN 111.57(2) . 1_554 ?

O1 M2 M1MN 35.62(4) 1_655 1_554 ?

O2 M2 M1MN 106.80(4) 4_565 1_554 ?

O8 M2 M1MN 165.22(4) . 1_554 ?

O2 M2 M1MN 67.68(4) 1_554 1_554 ?

04 M2 M1MN 68.25(4) 4_565 1_554 ?

O1 M2 M1MN 116.24(4) 3_656 1_554 ?

O8 M2 M1MN 62.44(3) 1_554 1_554 ?

07 M2 M1MN 75.48(4) 1_655 1_554 ?

M1CA M2 M1MN 0.000(13) 1_554 1_554 ?

06 M2 P2 87.55(7) . 4_565 ?

04 M2 P2 71.86(7) . 4_565 ?

07 M2 P2 155.20(7) 3_656 4_565 ?

O8 M2 P2 89.04(6) 3_656 4_565 ?

03 M2 P2 70.65(6) . 4_565 ?

P2 M2 P2 84.21(2) 1_554 4_565 ?

P2 M2 P2 83.38(2) . 4_565 ?

P1 M2 P2 147.71(2) 3_656 4_565 ?

P1 M2 P2 93.23(2) 1_655 4_565 ?

P2 M2 P2 110.854(16) 3_656 4_565 ?

M3 M2 P2 53.750(15) . 4_565 ?

O2 M2 P2 135.67(4) 3_656 4_565 ?

M1CA M2 P2 89.986(19) . 4_565 ?

M1MN M2 P2 89.986(19) . 4_565 ?

O1 M2 P2 105.02(4) 1_655 4_565 ?

O2 M2 P2 22.74(4) 4_565 4_565 ?

O8 M2 P2 104.01(4) . 4_565 ?

O2 M2 P2 64.13(4) 1_554 4_565 ?

04 M2 P2 22.61(4) 4_565 4_565 ?

O1 M2 P2 124.11(4) 3_656 4_565 ?

O8 M2 P2 104.06(4) 1_554 4_565 ?

07 M2 P2 106.90(4) 1_655 4_565 ?

M1CA M2 P2 90.767(18) 1_554 4_565 ?

M1MN M2 P2 90.767(18) 1_554 4_565 ?

06 M2 05 118.18(8) . 3_656 ?

04 M2 05 82.46(8) . 3_656 ?

07 M2 05 32.58(8) 3_656 3_656 ?

O8 M2 05 88.83(7) 3_656 3_656 ?

03 M2 05 108.78(8) . 3_656 ?

P2 M2 05 118.60(4) 1_554 3_656 ?

P2 M2 05 70.90(4) . 3_656 ?

P1 M2 05 22.02(4) 3_656 3_656 ?

P1 M2 05 92.25(4) 1_655 3_656 ?

P2 M2 05 69.81(4) 3_656 3_656 ?

M3 M2 05 124.43(4) . 3_656 ?

O2 M2 05 52.39(5) 3_656 3_656 ?

M1CA M2 05 72.55(4) . 3_656 ?

M1MN M2 05 72.55(4) . 3_656 ?

O1 M2 05 90.54(6) 1_655 3_656 ?

O2 M2 05 139.58(5) 4_565 3_656 ?

O8 M2 05 52.34(5) . 3_656 ?

O2 M2 05 132.91(5) 1_554 3_656 ?

04 M2 05 172.42(5) 4_565 3_656 ?

O1 M2 05 36.90(5) 3_656 3_656 ?

O8 M2 05 96.11(5) 1_554 3_656 ?

07 M2 05 71.85(5) 1_655 3_656 ?

M1CA M2 05 113.16(4) 1_554 3_656 ?

M1MN M2 05 113.16(4) 1_554 3_656 ?

P2 M2 05 154.10(4) 4_565 3_656 ?

06 M2 06 102.68(7) . 4_566 ?

04 M2 06 57.28(8) . 4_566 ?

07 M2 06 134.50(8) 3_656 4_566 ?

O8 M2 06 105.53(7) 3_656 4_566 ?

03 M2 06 54.60(7) . 4_566 ?

P2 M2 06 104.15(4) 1_554 4_566 ?

P2 M2 06 72.72(3) . 4_566 ?

P1 M2 06 125.62(4) 3_656 4_566 ?

P1 M2 06 78.66(4) 1_655 4_566 ?

P2 M2 06 126.79(4) 3_656 4_566 ?

M3 M2 06 73.33(3) . 4_566 ?

O2 M2 06 152.82(5) 3_656 4_566 ?

M1CA M2 06 67.88(3) . 4_566 ?

M1MN M2 06 67.88(3) . 4_566 ?

O1 M2 06 97.31(5) 1_655 4_566 ?

O2 M2 06 38.54(5) 4_565 4_566 ?

O8 M2 06 97.40(5) . 4_566 ?

O2 M2 06 86.07(5) 1_554 4_566 ?

04 M2 06 36.48(5) 4_565 4_566 ?

O1 M2 06 102.74(5) 3_656 4_566 ?

O8 M2 06 125.63(5) 1_554 4_566 ?

07 M2 06 87.45(5) 1_655 4_566 ?

M1CA M2 06 96.38(3) 1_554 4_566 ?

M1MN M2 06 96.38(3) 1_554 4_566 ?

P2 M2 06 22.25(3) 4_565 4_566 ?

05 M2 06 137.15(5) 3_656 4_566 ?

06 M2 M1MN 68.64(7) . 3_756 ?

04 M2 M1MN 126.54(7) . 3_756 ?

07 M2 M1MN 31.66(7) 3_656 3_756 ?

O8 M2 M1MN 122.92(6) 3_656 3_756 ?

03 M2 M1MN 75.72(6) . 3_756 ?

P2 M2 M1MN 83.940(19) 1_554 3_756 ?

P2 M2 M1MN 126.09(2) . 3_756 ?

P1 M2 M1MN 50.309(17) 3_656 3_756 ?

P1 M2 M1MN 51.703(17) 1_655 3_756 ?

P2 M2 M1MN 103.00(2) 3_656 3_756 ?

M3 M2 M1MN 143.255(19) . 3_756 ?

O2 M2 M1MN 77.32(4) 3_656 3_756 ?

M1CA M2 M1MN 87.203(18) . 3_756 ?

M1MN M2 M1MN 87.203(18) . 3_756 ?

O1 M2 M1MN 33.31(4) 1_655 3_756 ?

O2 M2 M1MN 158.31(4) 4_565 3_756 ?

O8 M2 M1MN 114.11(4) . 3_756 ?

O2 M2 M1MN 109.09(4) 1_554 3_756 ?

04 M2 M1MN 117.50(4) 4_565 3_756 ?

O1 M2 M1MN 69.76(4) 3_656 3_756 ?

O8 M2 M1MN 77.96(4) 1_554 3_756 ?

07 M2 M1MN 50.61(4) 1_655 3_756 ?

M1CA M2 M1MN 52.034(17) 1_554 3_756 ?

M1MN M2 M1MN 52.034(17) 1_554 3_756 ?

P2 M2 M1MN 137.77(2) 4_565 3_756 ?

05 M2 M1MN 62.09(4) 3_656 3_756 ?

06 M2 M1MN 129.67(4) 4_566 3_756 ?

06 M2 M1CA 68.64(7) . 3_756 ?

04 M2 M1CA 126.54(7) . 3_756 ?

07 M2 M1CA 31.66(7) 3_656 3_756 ?

O8 M2 M1CA 122.92(6) 3_656 3_756 ?

03 M2 M1CA 75.72(6) . 3_756 ?

P2 M2 M1CA 83.940(19) 1_554 3_756 ?

P2 M2 M1CA 126.09(2) . 3_756 ?

P1 M2 M1CA 50.309(17) 3_656 3_756 ?

P1 M2 M1CA 51.703(17) 1_655 3_756 ?

P2 M2 M1CA 103.00(2) 3_656 3_756 ?

M3 M2 M1CA 143.255(19) . 3_756 ?

O2 M2 M1CA 77.32(4) 3_656 3_756 ?

M1CA M2 M1CA 87.203(18) . 3_756 ?

M1MN M2 M1CA 87.203(18) . 3_756 ?

O1 M2 M1CA 33.31(4) 1_655 3_756 ?

O2 M2 M1CA 158.31(4) 4_565 3_756 ?

O8 M2 M1CA 114.11(4) . 3_756 ?

O2 M2 M1CA 109.09(4) 1_554 3_756 ?

04 M2 M1CA 117.50(4) 4_565 3_756 ?

O1 M2 M1CA 69.76(4) 3_656 3_756 ?

O8 M2 M1CA 77.96(4) 1_554 3_756 ?

07 M2 M1CA 50.61(4) 1_655 3_756 ?

M1CA M2 M1CA 52.034(17) 1_554 3_756 ?

M1MN M2 M1CA 52.034(17) 1_554 3_756 ?

P2 M2 M1CA 137.77(2) 4_565 3_756 ?

05 M2 M1CA 62.09(4) 3_656 3_756 ?

06 M2 M1CA 129.67(4) 4_566 3_756 ?

M1MN M2 M1CA 0.00(2) 3_756 3_756 ?

06 M2 M1CA 81.34(7) . 4_565 ?

04 M2 M1CA 82.96(7) . 4_565 ?

07 M2 M1CA 112.23(7) 3_656 4_565 ?

O8 M2 M1CA 132.52(6) 3_656 4_565 ?

03 M2 M1CA 28.15(7) . 4_565 ?

P2 M2 M1CA 93.27(2) 1_554 4_565 ?

P2 M2 M1CA 100.78(2) . 4_565 ?

P1 M2 M1CA 115.11(2) 3_656 4_565 ?

P1 M2 M1CA 48.799(17) 1_655 4_565 ?

P2 M2 M1CA 153.32(2) 3_656 4_565 ?

M3 M2 M1CA 96.032(17) . 4_565 ?

O2 M2 M1CA 164.37(4) 3_656 4_565 ?

M1CA M2 M1CA 69.152(16) . 4_565 ?

M1MN M2 M1CA 69.152(16) . 4_565 ?

O1 M2 M1CA 62.83(4) 1_655 4_565 ?

O2 M2 M1CA 67.17(4) 4_565 4_565 ?

O8 M2 M1CA 126.33(4) . 4_565 ?

O2 M2 M1CA 88.42(4) 1_554 4_565 ?

04 M2 M1CA 36.49(4) 4_565 4_565 ?

O1 M2 M1CA 102.07(4) 3_656 4_565 ?

O8 M2 M1CA 116.56(4) 1_554 4_565 ?

07 M2 M1CA 65.73(4) 1_655 4_565 ?

M1CA M2 M1CA 65.014(16) 1_554 4_565 ?

M1MN M2 M1CA 65.014(16) 1_554 4_565 ?

P2 M2 M1CA 44.581(15) 4_565 4_565 ?

05 M2 M1CA 136.56(4) 3_656 4_565 ?

06 M2 M1CA 35.03(3) 4_566 4_565 ?

M1MN M2 M1CA 95.995(12) 3_756 4_565 ?

M1CA M2 M1CA 95.995(12) 3_756 4_565 ?

06 M2 M1MN 81.34(7) . 4_565 ?

04 M2 M1MN 82.96(7) . 4_565 ?

07 M2 M1MN 112.23(7) 3_656 4_565 ?

O8 M2 M1MN 132.52(6) 3_656 4_565 ?

03 M2 M1MN 28.15(7) . 4_565 ?

P2 M2 M1MN 93.27(2) 1_554 4_565 ?

P2 M2 M1MN 100.78(2) . 4_565 ?

P1 M2 M1MN 115.11(2) 3_656 4_565 ?

P1 M2 M1MN 48.799(17) 1_655 4_565 ?

P2 M2 M1MN 153.32(2) 3_656 4_565 ?

M3 M2 M1MN 96.032(17) . 4_565 ?

O2 M2 M1MN 164.37(4) 3_656 4_565 ?

M1CA M2 M1MN 69.152(16) . 4_565 ?

M1MN M2 M1MN 69.152(16) . 4_565 ?

O1 M2 M1MN 62.83(4) 1_655 4_565 ?

O2 M2 M1MN 67.17(4) 4_565 4_565 ?

O8 M2 M1MN 126.33(4) . 4_565 ?

O2 M2 M1MN 88.42(4) 1_554 4_565 ?

04 M2 M1MN 36.49(4) 4_565 4_565 ?

O1 M2 M1MN 102.07(4) 3_656 4_565 ?

O8 M2 M1MN 116.56(4) 1_554 4_565 ?

07 M2 M1MN 65.73(4) 1_655 4_565 ?

M1CA M2 M1MN 65.014(16) 1_554 4_565 ?

M1MN M2 M1MN 65.014(16) 1_554 4_565 ?

P2 M2 M1MN 44.581(15) 4_565 4_565 ?

05 M2 M1MN 136.56(4) 3_656 4_565 ?

06 M2 M1MN 35.03(3) 4_566 4_565 ?

M1MN M2 M1MN 95.995(12) 3_756 4_565 ?

M1CA M2 M1MN 95.995(12) 3_756 4_565 ?

M1CA M2 M1MN 0.00(3) 4_565 4_565 ?

06 M2 O2 145.74(7) . . ?

04 M2 O2 23.76(7) . . ?

07 M2 O2 114.53(8) 3_656 . ?

O8 M2 O2 69.47(7) 3_656 . ?

03 M2 O2 100.18(7) . . ?

P2 M2 O2 128.23(4) 1_554 . ?

P2 M2 O2 19.33(3) . . ?

P1 M2 O2 95.55(3) 3_656 . ?

P1 M2 O2 118.06(4) 1_655 . ?

P2 M2 O2 80.41(3) 3_656 . ?

M3 M2 O2 67.49(3) . . ?

O2 M2 O2 98.95(5) 3_656 . ?

M1CA M2 O2 66.10(3) . . ?

M1MN M2 O2 66.10(3) . . ?

O1 M2 O2 143.69(5) 1_655 . ?

O2 M2 O2 53.56(4) 4_565 . ?

O8 M2 O2 37.24(5) . . ?

O2 M2 O2 104.06(5) 1_554 . ?

04 M2 O2 89.66(5) 4_565 . ?

O1 M2 O2 75.83(5) 3_656 . ?

O8 M2 O2 125.36(5) 1_554 . ?

07 M2 O2 105.82(5) 1_655 . ?

M1CA M2 O2 157.38(4) 1_554 . ?

M1MN M2 O2 157.38(4) 1_554 . ?

P2 M2 O2 67.05(3) 4_565 . ?

05 M2 O2 88.10(5) 3_656 . ?

06 M2 O2 61.44(4) 4_566 . ?

M1MN M2 O2 145.40(3) 3_756 . ?

M1CA M2 O2 145.40(3) 3_756 . ?

M1CA M2 O2 94.51(3) 4_565 . ?

M1MN M2 O2 94.51(3) 4_565 . ?

06 M2 M3 54.27(7) . 3_655 ?

04 M2 M3 143.82(7) . 3_655 ?

07 M2 M3 65.82(7) 3_656 3_655 ?

O8 M2 M3 67.34(6) 3_656 3_655 ?

03 M2 M3 128.09(6) . 3_655 ?

P2 M2 M3 50.597(16) 1_554 3_655 ?

P2 M2 M3 126.22(2) . 3_655 ?

P1 M2 M3 78.365(18) 3_656 3_655 ?

P1 M2 M3 106.151(19) 1_655 3_655 ?

P2 M2 M3 51.057(16) 3_656 3_655 ?

M3 M2 M3 90.492(15) . 3_655 ?

O2 M2 M3 32.12(4) 3_656 3_655 ?

M1CA M2 M3 135.563(19) . 3_655 ?

M1MN M2 M3 135.563(19) . 3_655 ?

O1 M2 M3 81.71(4) 1_655 3_655 ?

O2 M2 M3 124.75(4) 4_565 3_655 ?

O8 M2 M3 100.57(4) . 3_655 ?

O2 M2 M3 69.79(4) 1_554 3_655 ?

04 M2 M3 118.58(4) 4_565 3_655 ?

O1 M2 M3 102.07(4) 3_656 3_655 ?

O8 M2 M3 29.77(3) 1_554 3_655 ?

07 M2 M3 106.64(4) 1_655 3_655 ?

M1CA M2 M3 68.159(13) 1_554 3_655 ?

M1MN M2 M3 68.159(13) 1_554 3_655 ?

P2 M2 M3 133.782(18) 4_565 3_655 ?

05 M2 M3 68.04(4) 3_656 3_655 ?

06 M2 M3 154.74(3) 4_566 3_655 ?

M1MN M2 M3 56.649(12) 3_756 3_655 ?

M1CA M2 M3 56.649(12) 3_756 3_655 ?

M1CA M2 M3 132.956(17) 4_565 3_655 ?

M1MN M2 M3 132.956(17) 4_565 3_655 ?

O2 M2 M3 130.41(4) . 3_655 ?

06 M2 O1 36.96(7) . 3_655 ?

04 M2 O1 158.88(8) . 3_655 ?

07 M2 O1 61.31(8) 3_656 3_655 ?

O8 M2 O1 104.18(7) 3_656 3_655 ?

03 M2 O1 87.88(7) . 3_655 ?

P2 M2 O1 51.40(4) 1_554 3_655 ?

P2 M2 O1 155.73(4) . 3_655 ?

P1 M2 O1 80.23(4) 3_656 3_655 ?

P1 M2 O1 68.45(4) 1_655 3_655 ?

P2 M2 O1 91.42(4) 3_656 3_655 ?

M3 M2 O1 111.74(4) . 3_655 ?

O2 M2 O1 71.94(5) 3_656 3_655 ?

M1CA M2 O1 117.27(4) . 3_655 ?

M1MN M2 O1 117.27(4) . 3_655 ?

O1 M2 O1 42.76(6) 1_655 3_655 ?

O2 M2 O1 131.27(5) 4_565 3_655 ?

O8 M2 O1 134.34(5) . 3_655 ?

O2 M2 O1 76.49(5) 1_554 3_655 ?

04 M2 O1 97.96(5) 4_565 3_655 ?

O1 M2 O1 101.90(6) 3_656 3_655 ?

O8 M2 O1 49.67(5) 1_554 3_655 ?

07 M2 O1 77.83(5) 1_655 3_655 ?

M1CA M2 O1 31.36(3) 1_554 3_655 ?

M1MN M2 O1 31.36(3) 1_554 3_655 ?

P2 M2 O1 120.49(4) 4_565 3_655 ?

05 M2 O1 84.99(5) 3_656 3_655 ?

06 M2 O1 127.65(5) 4_566 3_655 ?

M1MN M2 O1 32.60(3) 3_756 3_655 ?

M1CA M2 O1 32.60(3) 3_756 3_655 ?

M1CA M2 O1 94.74(4) 4_565 3_655 ?

M1MN M2 O1 94.74(4) 4_565 3_655 ?

O2 M2 O1 170.75(5) . 3_655 ?

M3 M2 O1 40.81(3) 3_655 3_655 ?

06 M2 06 173.13(10) . 1_556 ?

04 M2 06 16.76(7) . 1_556 ?

07 M2 06 83.53(7) 3_656 1_556 ?

O8 M2 06 96.96(6) 3_656 1_556 ?

03 M2 06 81.54(7) . 1_556 ?

P2 M2 06 163.05(4) 1_554 1_556 ?

P2 M2 06 18.75(3) . 1_556 ?

P1 M2 06 65.08(3) 3_656 1_556 ?

P1 M2 06 90.36(3) 1_655 1_556 ?

P2 M2 06 98.27(4) 3_656 1_556 ?

M3 M2 06 102.58(3) . 1_556 ?

O2 M2 06 103.75(5) 3_656 1_556 ?

M1CA M2 06 35.01(3) . 1_556 ?

M1MN M2 06 35.01(3) . 1_556 ?

O1 M2 06 113.13(5) 1_655 1_556 ?

O2 M2 06 83.59(5) 4_565 1_556 ?

O8 M2 06 36.85(5) . 1_556 ?

O2 M2 06 139.06(5) 1_554 1_556 ?

04 M2 06 107.95(5) 4_565 1_556 ?

O1 M2 06 42.27(5) 3_656 1_556 ?

O8 M2 06 149.53(5) 1_554 1_556 ?

07 M2 06 72.88(5) 1_655 1_556 ?

M1CA M2 06 146.52(3) 1_554 1_556 ?

M1MN M2 06 146.52(3) 1_554 1_556 ?

P2 M2 06 88.14(3) 4_565 1_556 ?

05 M2 06 66.52(5) 3_656 1_556 ?

06 M2 06 71.71(5) 4_566 1_556 ?

M1MN M2 06 111.58(3) 3_756 1_556 ?

M1CA M2 06 111.58(3) 3_756 1_556 ?

M1CA M2 06 91.84(3) 4_565 1_556 ?

M1MN M2 06 91.84(3) 4_565 1_556 ?

O2 M2 06 35.11(4) . 1_556 ?

M3 M2 06 131.99(3) 3_655 1_556 ?

O1 M2 06 144.07(5) 3_655 1_556 ?

06 M2 05 74.63(7) . 2_645 ?

04 M2 05 125.96(8) . 2_645 ?

07 M2 05 38.91(8) 3_656 2_645 ?

O8 M2 05 83.68(7) 3_656 2_645 ?

03 M2 05 116.00(7) . 2_645 ?

P2 M2 05 76.68(4) 1_554 2_645 ?

P2 M2 05 112.28(4) . 2_645 ?

P1 M2 05 50.83(4) 3_656 2_645 ?

P1 M2 05 91.91(4) 1_655 2_645 ?

P2 M2 05 62.64(4) 3_656 2_645 ?

M3 M2 05 114.58(4) . 2_645 ?

O2 M2 05 36.66(5) 3_656 2_645 ?

M1CA M2 05 108.01(4) . 2_645 ?

M1MN M2 05 108.01(4) . 2_645 ?

O1 M2 05 73.26(5) 1_655 2_645 ?

O2 M2 05 149.76(5) 4_565 2_645 ?

O8 M2 05 88.79(5) . 2_645 ?

O2 M2 05 97.38(5) 1_554 2_645 ?

04 M2 05 141.41(5) 4_565 2_645 ?

O1 M2 05 74.84(5) 3_656 2_645 ?

O8 M2 05 57.36(5) 1_554 2_645 ?

07 M2 05 84.32(5) 1_655 2_645 ?

M1CA M2 05 76.88(4) 1_554 2_645 ?

M1MN M2 05 76.88(4) 1_554 2_645 ?

P2 M2 05 160.89(4) 4_565 2_645 ?

05 M2 05 43.707(9) 3_656 2_645 ?

06 M2 05 170.45(5) 4_566 2_645 ?

M1MN M2 05 40.78(4) 3_756 2_645 ?

M1CA M2 05 40.78(4) 3_756 2_645 ?

M1CA M2 05 135.83(4) 4_565 2_645 ?

M1MN M2 05 135.83(4) 4_565 2_645 ?

O2 M2 05 125.68(5) . 2_645 ?

M3 M2 05 27.62(3) 3_655 2_645 ?

O1 M2 05 45.57(5) 3_655 2_645 ?

06 M2 05 110.23(5) 1_556 2_645 ?

06 M2 04 6.76(7) . 1_554 ?

04 M2 04 154.30(10) . 1_554 ?

07 M2 04 104.62(8) 3_656 1_554 ?

O8 M2 04 83.60(6) 3_656 1_554 ?

03 M2 04 94.72(8) . 1_554 ?

P2 M2 04 15.78(3) 1_554 1_554 ?

P2 M2 04 157.63(4) . 1_554 ?

P1 M2 04 123.36(4) 3_656 1_554 ?

P1 M2 04 89.50(3) 1_655 1_554 ?

P2 M2 04 85.69(3) 3_656 1_554 ?

M3 M2 04 72.43(3) . 1_554 ?

O2 M2 04 83.47(5) 3_656 1_554 ?

M1CA M2 04 143.72(4) . 1_554 ?

M1MN M2 04 143.72(4) . 1_554 ?

O1 M2 04 68.99(5) 1_655 1_554 ?

O2 M2 04 88.15(5) 4_565 1_554 ?

O8 M2 04 147.03(5) . 1_554 ?

O2 M2 04 35.51(5) 1_554 1_554 ?

04 M2 04 62.90(5) 4_565 1_554 ?

O1 M2 04 145.09(5) 3_656 1_554 ?

O8 M2 04 35.80(5) 1_554 1_554 ?

07 M2 04 109.15(5) 1_655 1_554 ?

M1CA M2 04 33.71(3) 1_554 1_554 ?

M1MN M2 04 33.71(3) 1_554 1_554 ?

P2 M2 04 82.66(3) 4_565 1_554 ?

05 M2 04 122.69(5) 3_656 1_554 ?

06 M2 04 99.24(5) 4_566 1_554 ?

M1MN M2 04 75.33(3) 3_756 1_554 ?

M1CA M2 04 75.33(3) 3_756 1_554 ?

M1CA M2 04 81.15(3) 4_565 1_554 ?

M1MN M2 04 81.15(3) 4_565 1_554 ?

O2 M2 04 138.99(4) . 1_554 ?

M3 M2 04 56.67(3) 3_655 1_554 ?

O1 M2 04 43.43(4) 3_655 1_554 ?

06 M2 04 170.78(5) 1_556 1_554 ?

05 M2 04 78.99(5) 2_645 1_554 ?

06 M2 03 44.97(8) . 4_565 ?

04 M2 03 119.60(8) . 4_565 ?

07 M2 03 106.24(8) 3_656 4_565 ?

O8 M2 03 121.43(7) 3_656 4_565 ?

03 M2 03 50.11(5) . 4_565 ?

P2 M2 03 60.16(4) 1_554 4_565 ?

P2 M2 03 137.12(4) . 4_565 ?

P1 M2 03 120.58(4) 3_656 4_565 ?

P1 M2 03 54.11(4) 1_655 4_565 ?

P2 M2 03 130.56(4) 3_656 4_565 ?

M3 M2 03 92.31(4) . 4_565 ?

O2 M2 03 127.58(5) 3_656 4_565 ?

M1CA M2 03 99.73(4) . 4_565 ?

M1MN M2 03 99.73(4) . 4_565 ?

O1 M2 03 48.53(5) 1_655 4_565 ?

O2 M2 03 81.10(5) 4_565 4_565 ?

O8 M2 03 162.74(6) . 4_565 ?

O2 M2 03 65.77(5) 1_554 4_565 ?

04 M2 03 40.19(5) 4_565 4_565 ?

O1 M2 03 122.95(5) 3_656 4_565 ?

O8 M2 03 81.63(5) 1_554 4_565 ?

07 M2 03 77.06(5) 1_655 4_565 ?

M1CA M2 03 30.78(4) 1_554 4_565 ?

M1MN M2 03 30.78(4) 1_554 4_565 ?

P2 M2 03 61.68(4) 4_565 4_565 ?

05 M2 03 138.73(5) 3_656 4_565 ?

06 M2 03 65.66(5) 4_566 4_565 ?

M1MN M2 03 77.32(4) 3_756 4_565 ?

M1CA M2 03 77.32(4) 3_756 4_565 ?

M1CA M2 03 36.82(4) 4_565 4_565 ?

M1MN M2 03 36.82(4) 4_565 4_565 ?

O2 M2 03 126.72(5) . 4_565 ?

M3 M2 03 96.56(4) 3_655 4_565 ?

O1 M2 03 62.14(5) 3_655 4_565 ?

06 M2 03 128.16(5) 1_556 4_565 ?

05 M2 03 107.60(5) 2_645 4_565 ?

04 M2 03 45.89(5) 1_554 4_565 ?

06 M2 04 106.22(8) . 3_656 ?

04 M2 04 82.57(8) . 3_656 ?

07 M2 04 92.23(8) 3_656 3_656 ?

O8 M2 04 26.91(6) 3_656 3_656 ?

03 M2 04 161.80(8) . 3_656 ?

P2 M2 04 88.02(3) 1_554 3_656 ?

P2 M2 04 65.25(3) . 3_656 ?

P1 M2 04 84.66(4) 3_656 3_656 ?

P1 M2 04 155.06(4) 1_655 3_656 ?

P2 M2 04 18.02(3) 3_656 3_656 ?

M3 M2 04 61.63(3) . 3_656 ?

O2 M2 04 35.46(5) 3_656 3_656 ?

M1CA M2 04 112.55(3) . 3_656 ?

M1MN M2 04 112.55(3) . 3_656 ?

O1 M2 04 143.49(5) 1_655 3_656 ?

O2 M2 04 86.63(5) 4_565 3_656 ?

O8 M2 04 43.74(5) . 3_656 ?

O2 M2 04 81.49(5) 1_554 3_656 ?

04 M2 04 122.42(3) 4_565 3_656 ?

O1 M2 04 89.14(5) 3_656 3_656 ?

O8 M2 04 69.38(4) 1_554 3_656 ?

07 M2 04 133.57(5) 1_655 3_656 ?

M1CA M2 04 131.02(3) 1_554 3_656 ?

M1MN M2 04 131.02(3) 1_554 3_656 ?

P2 M2 04 109.36(3) 4_565 3_656 ?

05 M2 04 62.82(5) 3_656 3_656 ?

06 M2 04 119.20(4) 4_566 3_656 ?

M1MN M2 04 110.55(3) 3_756 3_656 ?

M1CA M2 04 110.55(3) 3_756 3_656 ?

M1CA M2 04 153.40(3) 4_565 3_656 ?

M1MN M2 04 153.40(3) 4_565 3_656 ?

O2 M2 04 64.64(4) . 3_656 ?

M3 M2 04 65.79(3) 3_655 3_656 ?

O1 M2 04 106.58(4) 3_655 3_656 ?

06 M2 04 80.27(4) 1_556 3_656 ?

05 M2 04 70.23(5) 2_645 3_656 ?

04 M2 04 103.38(4) 1_554 3_656 ?

03 M2 04 146.85(5) 4_565 3_656 ?

06 M2 03 104.30(8) . 3_756 ?

04 M2 03 93.00(8) . 3_756 ?

07 M2 03 8.54(7) 3_656 3_756 ?

O8 M2 03 120.66(7) 3_656 3_756 ?

03 M2 03 78.95(8) . 3_756 ?

P2 M2 03 116.92(4) 1_554 3_756 ?

P2 M2 03 90.07(4) . 3_756 ?

P1 M2 03 15.12(4) 3_656 3_756 ?

P1 M2 03 59.07(4) 1_655 3_756 ?

P2 M2 03 99.55(4) 3_656 3_756 ?

M3 M2 03 157.17(4) . 3_756 ?

O2 M2 03 76.19(5) 3_656 3_756 ?

M1CA M2 03 61.46(4) . 3_756 ?

M1MN M2 03 61.46(4) . 3_756 ?

O1 M2 03 57.62(5) 1_655 3_756 ?

O2 M2 03 159.39(5) 4_565 3_756 ?

O8 M2 03 80.77(5) . 3_756 ?

O2 M2 03 141.63(5) 1_554 3_756 ?

04 M2 03 141.43(5) 4_565 3_756 ?

O1 M2 03 34.54(5) 3_656 3_756 ?

O8 M2 03 103.19(5) 1_554 3_756 ?

07 M2 03 41.55(5) 1_655 3_756 ?

M1CA M2 03 86.78(4) 1_554 3_756 ?

M1MN M2 03 86.78(4) 1_554 3_756 ?

P2 M2 03 147.76(4) 4_565 3_756 ?

05 M2 03 34.00(5) 3_656 3_756 ?

06 M2 03 126.36(5) 4_566 3_756 ?

M1MN M2 03 36.04(4) 3_756 3_756 ?

M1CA M2 03 36.04(4) 3_756 3_756 ?

M1CA M2 03 106.80(4) 4_565 3_756 ?

M1MN M2 03 106.80(4) 4_565 3_756 ?

O2 M2 03 109.40(5) . 3_756 ?

M3 M2 03 74.36(4) 3_655 3_756 ?

O1 M2 03 67.47(5) 3_655 3_756 ?

06 M2 03 76.80(5) 1_556 3_756 ?

05 M2 03 47.37(5) 2_645 3_756 ?

04 M2 03 110.88(5) 1_554 3_756 ?

03 M2 03 106.10(3) 4_565 3_756 ?

04 M2 03 96.15(5) 3_656 3_756 ?

05 M3 O8 144.49(10) 4_565 3_656 ?

05 M3 O2 106.15(10) 4_565 4_565 ?

O8 M3 O2 108.61(9) 3_656 4_565 ?

05 M3 05 93.92(10) 4_565 . ?

O8 M3 05 102.72(9) 3_656 . ?

O2 M3 05 73.30(9) 4_565 . ?

05 M3 O2 74.41(9) 4_565 1_554 ?

O8 M3 O2 87.66(8) 3_656 1_554 ?

O2 M3 O2 108.77(9) 4_565 1_554 ?

05 M3 O2 168.31(9) . 1_554 ?

05 M3 M2 149.99(7) 4_565 . ?

O8 M3 M2 39.72(6) 3_656 . ?

O2 M3 M2 76.37(6) 4_565 . ?

05 M3 M2 114.91(7) . . ?

O2 M3 M2 76.53(6) 1_554 . ?

05 M3 M2 80.02(7) 4_565 3_655 ?

O8 M3 M2 64.67(6) 3_656 3_655 ?

O2 M3 M2 161.27(6) 4_565 3_655 ?

05 M3 M2 124.57(6) . 3_655 ?

O2 M3 M2 55.09(6) 1_554 3_655 ?

M2 M3 M2 89.508(15) . 3_655 ?

05 M3 M2 61.10(7) 4_565 2_655 ?

O8 M3 M2 154.33(6) 3_656 2_655 ?

O2 M3 M2 45.92(6) 4_565 2_655 ?

05 M3 M2 69.95(6) . 2_655 ?

O2 M3 M2 102.86(6) 1_554 2_655 ?

M2 M3 M2 119.564(16) . 2_655 ?

M2 M3 M2 140.169(17) 3_655 2_655 ?

05 M3 M2 80.04(8) 4_565 4_565 ?

O8 M3 M2 109.69(6) 3_656 4_565 ?

O2 M3 M2 62.86(6) 4_565 4_565 ?

05 M3 M2 131.56(6) . 4_565 ?

O2 M3 M2 46.76(6) 1_554 4_565 ?

M2 M3 M2 74.688(17) . 4_565 ?

M2 M3 M2 101.841(10) 3_655 4_565 ?

M2 M3 M2 65.149(13) 2_655 4_565 ?

05 M3 M2 132.95(8) 4_565 3_656 ?

O8 M3 M2 45.86(6) 3_656 3_656 ?

O2 M3 M2 100.32(6) 4_565 3_656 ?

05 M3 M2 57.58(7) . 3_656 ?

O2 M3 M2 131.52(6) 1_554 3_656 ?

M2 M3 M2 73.707(15) . 3_656 ?

M2 M3 M2 87.153(14) 3_655 3_656 ?

M2 M3 M2 125.001(15) 2_655 3_656 ?

M2 M3 M2 147.005(11) 4_565 3_656 ?

05 M3 M2 124.29(7) 4_565 4_566 ?

O8 M3 M2 90.94(6) 3_656 4_566 ?

O2 M3 M2 18.48(6) 4_565 4_566 ?

05 M3 M2 71.17(6) . 4_566 ?

O2 M3 M2 114.56(6) 1_554 4_566 ?

M2 M3 M2 62.921(16) . 4_566 ?

M2 M3 M2 152.407(13) 3_655 4_566 ?

M2 M3 M2 63.389(12) 2_655 4_566 ?

M2 M3 M2 73.245(10) 4_565 4_566 ?

M2 M3 M2 84.113(8) 3_656 4_566 ?

07 P1 O1 114.15(14) . . ?

07 P1 03 106.91(15) . 1_455 ?

O1 P1 03 111.01(15) . 1_455 ?

07 P1 05 110.32(14) . . ?

O1 P1 05 105.41(14) . . ?

03 P1 05 109.00(16) 1_455 . ?

07 P1 M1CA 132.29(10) . 4_465 ?

O1 P1 M1CA 111.67(10) . 4_465 ?

03 P1 M1CA 42.17(11) 1_455 4_465 ?

05 P1 M1CA 68.39(11) . 4_465 ?

07 P1 M1CA 51.23(10) . 1_455 ?

O1 P1 M1CA 137.02(10) . 1_455 ?

03 P1 M1CA 56.28(11) 1_455 1_455 ?

05 P1 M1CA 117.57(10) . 1_455 ?

M1CA P1 M1CA 85.76(2) 4_465 1_455 ?

07 P1 M1CA 80.49(10) . 3_656 ?

O1 P1 M1CA 35.35(9) . 3_656 ?

03 P1 M1CA 113.76(11) 1_455 3_656 ?

05 P1 M1CA 130.24(11) . 3_656 ?

M1CA P1 M1CA 138.88(2) 4_465 3_656 ?

M1CA P1 M1CA 106.92(2) 1_455 3_656 ?

07 P1 M2 25.93(10) . 3_656 ?

O1 P1 M2 92.66(10) . 3_656 ?

03 P1 M2 130.80(12) 1_455 3_656 ?

05 P1 M2 104.84(11) . 3_656 ?

M1CA P1 M2 155.63(3) 4_465 3_656 ?

M1CA P1 M2 76.75(2) 1_455 3_656 ?

M1CA P1 M2 63.863(19) 3_656 3_656 ?

07 P1 M2 97.40(10) . 1_455 ?

O1 P1 M2 81.49(9) . 1_455 ?

03 P1 M2 39.40(11) 1_455 1_455 ?

05 P1 M2 144.58(11) . 1_455 ?

M1CA P1 M2 76.74(2) 4_465 1_455 ?

M1CA P1 M2 64.093(18) 1_455 1_455 ?

M1CA P1 M2 74.55(2) 3_656 1_455 ?

M2 P1 M2 109.55(2) 3_656 1_455 ?

07 P1 M1CA 142.45(10) . 1_454 ?

O1 P1 M1CA 31.10(9) . 1_454 ?

03 P1 M1CA 86.11(11) 1_455 1_454 ?

05 P1 M1CA 97.57(10) . 1_454 ?

M1CA P1 M1CA 80.75(2) 4_465 1_454 ?

M1CA P1 M1CA 134.19(3) 1_455 1_454 ?

M1CA P1 M1CA 62.16(2) 3_656 1_454 ?

M2 P1 M1CA 123.62(3) 3_656 1_454 ?

M2 P1 M1CA 70.222(19) 1_455 1_454 ?

07 P1 M2 156.54(10) . 4_465 ?

O1 P1 M2 77.55(10) . 4_465 ?

03 P1 M2 49.85(11) 1_455 4_465 ?

05 P1 M2 84.14(10) . 4_465 ?

M1CA P1 M2 34.970(15) 4_465 4_465 ?

M1CA P1 M2 106.01(2) 1_455 4_465 ?

M1CA P1 M2 104.67(2) 3_656 4_465 ?

M2 P1 M2 168.32(2) 3_656 4_465 ?

M2 P1 M2 63.100(17) 1_455 4_465 ?

M1CA P1 M2 46.466(14) 1_454 4_465 ?

07 P1 M2 108.71(10) . 3_655 ?

O1 P1 M2 22.26(9) . 3_655 ?

03 P1 M2 131.40(11) 1_455 3_655 ?

05 P1 M2 88.27(10) . 3_655 ?

M1CA P1 M2 118.75(2) 4_465 3_655 ?

M1CA P1 M2 150.57(2) 1_455 3_655 ?

M1CA P1 M2 44.034(16) 3_656 3_655 ?

M2 P1 M2 83.396(17) 3_656 3_655 ?

M2 P1 M2 103.646(18) 1_455 3_655 ?

M1CA P1 M2 45.944(14) 1_454 3_655 ?

M2 P1 M2 89.521(12) 4_465 3_655 ?

04 P2 O2 110.19(13) . . ?

04 P2 06 103.83(12) . 1_556 ?

O2 P2 06 110.48(13) . 1_556 ?

04 P2 O8 111.61(13) . . ?

O2 P2 O8 110.37(12) . . ?

06 P2 O8 110.20(12) 1_556 . ?

04 P2 M1CA 52.40(9) . . ?

O2 P2 M1CA 131.29(9) . . ?

06 P2 M1CA 52.10(8) 1_556 . ?

O8 P2 M1CA 118.33(9) . . ?

04 P2 M2 129.60(9) . 1_556 ?

O2 P2 M2 92.60(9) . 1_556 ?

06 P2 M2 26.45(8) 1_556 1_556 ?

O8 P2 M2 100.43(9) . 1_556 ?

M1CA P2 M2 78.52(2) . 1_556 ?

04 P2 M2 23.15(9) . . ?

O2 P2 M2 116.20(9) . . ?

06 P2 M2 118.38(9) 1_556 . ?

O8 P2 M2 89.02(8) . . ?

M1CA P2 M2 67.01(2) . . ?

M2 P2 M2 144.49(3) 1_556 . ?

04 P2 M2 118.68(9) . 3_656 ?

O2 P2 M2 78.70(9) . 3_656 ?

06 P2 M2 130.51(9) 1_556 3_656 ?

O8 P2 M2 32.44(8) . 3_656 ?

M1CA P2 M2 149.51(3) . 3_656 ?

M2 P2 M2 109.37(2) 1_556 3_656 ?

M2 P2 M2 96.94(2) . 3_656 ?

04 P2 M2 65.84(9) . 4_566 ?

O2 P2 M2 63.19(9) . 4_566 ?

06 P2 M2 79.93(9) 1_556 4_566 ?

O8 P2 M2 169.77(9) . 4_566 ?

M1CA P2 M2 68.677(19) . 4_566 ?

M2 P2 M2 88.11(2) 1_556 4_566 ?

M2 P2 M2 87.20(2) . 4_566 ?

M2 P2 M2 138.92(2) 3_656 4_566 ?

P1 O1 M1MN 121.07(14) . 3_656 ?

P1 O1 M1CA 121.07(14) . 3_656 ?

M1MN O1 M1CA 0.00(3) 3_656 3_656 ?

P1 O1 M1CA 128.93(14) . 1_454 ?

M1MN O1 M1CA 101.07(9) 3_656 1_454 ?

M1CA O1 M1CA 101.07(9) 3_656 1_454 ?

P1 O1 M1MN 128.93(14) . 1_454 ?

M1MN O1 M1MN 101.07(9) 3_656 1_454 ?

M1CA O1 M1MN 101.07(9) 3_656 1_454 ?

M1CA O1 M1MN 0.00(4) 1_454 1_454 ?

P1 O1 M2 72.78(9) . 1_455 ?

M1MN O1 M2 86.81(7) 3_656 1_455 ?

M1CA O1 M2 86.81(7) 3_656 1_455 ?

M1CA O1 M2 83.00(7) 1_454 1_455 ?

M1MN O1 M2 83.00(7) 1_454 1_455 ?

P1 O1 M2 62.94(9) . 3_656 ?

M1MN O1 M2 66.63(6) 3_656 3_656 ?

M1CA O1 M2 66.63(6) 3_656 3_656 ?

M1CA O1 M2 167.39(9) 1_454 3_656 ?

M1MN O1 M2 167.39(9) 1_454 3_656 ?

M2 O1 M2 98.48(6) 1_455 3_656 ?

P1 O1 M2 149.81(12) . 3_655 ?

M1MN O1 M2 67.95(6) 3_656 3_655 ?

M1CA O1 M2 67.95(6) 3_656 3_655 ?

M1CA O1 M2 69.59(6) 1_454 3_655 ?

M1MN O1 M2 69.59(6) 1_454 3_655 ?

M2 O1 M2 137.24(6) 1_455 3_655 ?

M2 O1 M2 101.90(6) 3_656 3_655 ?

P2 O2 M3 134.56(14) . 4_566 ?

P2 O2 M3 123.99(13) . 1_556 ?

M3 O2 M3 101.36(9) 4_566 1_556 ?

P2 O2 M2 75.23(9) . 3_656 ?

M3 O2 M2 107.91(8) 4_566 3_656 ?

M3 O2 M2 92.79(7) 1_556 3_656 ?

P2 O2 M2 94.07(10) . 4_566 ?

M3 O2 M2 68.43(6) 4_566 4_566 ?

M3 O2 M2 106.09(8) 1_556 4_566 ?

M2 O2 M2 161.11(7) 3_656 4_566 ?

P2 O2 M2 62.15(8) . 1_556 ?

M3 O2 M2 150.84(10) 4_566 1_556 ?

M3 O2 M2 66.54(6) 1_556 1_556 ?

M2 O2 M2 99.36(6) 3_656 1_556 ?

M2 O2 M2 88.87(5) 4_566 1_556 ?

P2 O2 M2 44.46(7) . . ?

M3 O2 M2 90.41(7) 4_566 . ?

M3 O2 M2 167.96(9) 1_556 . ?

M2 O2 M2 81.05(5) 3_656 . ?

M2 O2 M2 80.46(5) 4_566 . ?

M2 O2 M2 104.06(5) 1_556 . ?

P1 03 M1MN 110.25(15) 1_655 4_565 ?

P1 03 M1CA 110.25(15) 1_655 4_565 ?

M1MN 03 M1CA 0.00(5) 4_565 4_565 ?

P1 03 M2 116.49(15) 1_655 . ?

M1MN 03 M2 121.47(11) 4_565 . ?

M1CA 03 M2 121.47(11) 4_565 . ?

P1 03 M1CA 94.96(13) 1_655 . ?

M1MN 03 M1CA 122.34(11) 4_565 . ?

M1CA 03 M1CA 122.34(11) 4_565 . ?

M2 03 M1CA 87.02(9) . . ?

P1 03 M2 145.33(14) 1_655 4_566 ?

M1MN 03 M2 64.89(6) 4_565 4_566 ?

M1CA 03 M2 64.89(6) 4_565 4_566 ?

M2 03 M2 91.81(7) . 4_566 ?

M1CA 03 M2 65.34(5) . 4_566 ?

P1 03 M2 34.07(9) 1_655 3_756 ?

M1MN 03 M2 136.72(10) 4_565 3_756 ?

M1CA 03 M2 136.72(10) 4_565 3_756 ?

M2 03 M2 101.05(8) . 3_756 ?

M1CA 03 M2 63.05(5) . 3_756 ?

M2 03 M2 125.74(6) 4_566 3_756 ?

P1 03 M2 115.66(13) 1_655 4_565 ?

M1MN 03 M2 44.54(5) 4_565 4_565 ?

M1CA 03 M2 44.54(5) 4_565 4_565 ?

M2 03 M2 83.28(7) . 4_565 ?

M1CA 03 M2 149.06(8) . 4_565 ?

M2 03 M2 85.63(5) 4_566 4_565 ?

M2 03 M2 147.75(6) 3_756 4_565 ?

P2 04 M2 138.88(15) . . ?

P2 04 M1CA 97.67(11) . . ?

M2 04 M1CA 104.83(10) . . ?

P2 04 M1MN 97.67(11) . . ?

M2 04 M1MN 104.83(10) . . ?

M1CA 04 M1MN 0.00(4) . . ?

P2 04 M2 91.55(10) . 4_566 ?

M2 04 M2 125.43(9) . 4_566 ?

M1CA 04 M2 80.81(6) . 4_566 ?

M1MN 04 M2 80.81(6) . 4_566 ?

P2 04 M2 34.62(7) . 1_556 ?

M2 04 M2 154.30(10) . 1_556 ?

M1CA 04 M2 64.38(5) . 1_556 ?

M1MN 04 M2 64.38(5) . 1_556 ?

M2 04 M2 77.57(4) 4_566 1_556 ?

P2 04 M2 43.30(7) . 3_656 ?

M2 04 M2 97.43(8) . 3_656 ?

M1CA 04 M2 130.81(8) . 3_656 ?

M1MN 04 M2 130.81(8) . 3_656 ?

M2 04 M2 119.81(6) 4_566 3_656 ?

M2 04 M2 76.62(4) 1_556 3_656 ?

P1 05 M3 129.85(14) . 4_566 ?

P1 05 M3 112.70(13) . . ?

M3 05 M3 104.15(11) 4_566 . ?

P1 05 M1CA 82.14(11) . 4_465 ?

M3 05 M1CA 102.16(10) 4_566 4_465 ?

M3 05 M1CA 126.81(10) . 4_465 ?

P1 05 M2 53.14(9) . 3_656 ?

M3 05 M2 92.34(8) 4_566 3_656 ?

M3 05 M2 94.45(8) . 3_656 ?

M1CA 05 M2 129.65(7) 4_465 3_656 ?

P1 05 M2 144.12(14) . 2_655 ?

M3 05 M2 72.36(7) 4_566 2_655 ?

M3 05 M2 81.28(6) . 2_655 ?

M1CA 05 M2 64.09(5) 4_465 2_655 ?

M2 05 M2 162.36(7) 3_656 2_655 ?

P1 05 M2 24.46(8) . 1_455 ?

M3 05 M2 133.74(9) 4_566 1_455 ?

M3 05 M2 121.31(8) . 1_455 ?

M1CA 05 M2 58.16(4) 4_465 1_455 ?

M2 05 M2 77.01(4) 3_656 1_455 ?

M2 05 M2 119.85(6) 2_655 1_455 ?

P1 05 M2 113.65(12) . . ?

M3 05 M2 75.15(8) 4_566 . ?

M3 05 M2 40.22(5) . . ?

M1CA 05 M2 161.83(7) 4_465 . ?

M2 05 M2 68.49(4) 3_656 . ?

M2 05 M2 98.37(5) 2_655 . ?

M2 05 M2 136.19(6) 1_455 . ?

P2 06 M2 132.84(14) 1_554 . ?

P2 06 M1CA 97.74(11) 1_554 1_554 ?

M2 06 M1CA 129.35(11) . 1_554 ?

P2 06 M1MN 97.74(11) 1_554 1_554 ?

M2 06 M1MN 129.35(11) . 1_554 ?

M1CA 06 M1MN 0.00(4) 1_554 1_554 ?

P2 06 M2 77.81(9) 1_554 4_565 ?

M2 06 M2 110.20(8) . 4_565 ?

M1CA 06 M2 73.08(5) 1_554 4_565 ?

M1MN 06 M2 73.08(5) 1_554 4_565 ?

P2 06 M2 42.87(7) 1_554 1_554 ?

M2 06 M2 173.13(10) . 1_554 ?

M1CA 06 M2 55.66(5) 1_554 1_554 ?

M1MN 06 M2 55.66(5) 1_554 1_554 ?

M2 06 M2 75.17(4) 4_565 1_554 ?

P2 06 M2 34.55(7) 1_554 3_655 ?

M2 06 M2 104.66(8) . 3_655 ?

M1CA 06 M2 122.98(7) 1_554 3_655 ?

M1MN 06 M2 122.98(7) 1_554 3_655 ?

M2 06 M2 107.48(5) 4_565 3_655 ?

M2 06 M2 69.16(4) 1_554 3_655 ?

P1 07 M2 135.06(16) . 3_656 ?

P1 07 M1CA 100.74(13) . 1_455 ?

M2 07 M1CA 123.20(10) 3_656 1_455 ?

P1 07 M1MN 100.74(13) . 1_455 ?

M2 07 M1MN 123.20(10) 3_656 1_455 ?

M1CA 07 M1MN 0.000(17) 1_455 1_455 ?

P1 07 M2 59.65(9) . 1_455 ?

M2 07 M2 131.69(9) 3_656 1_455 ?

M1CA 07 M2 61.75(5) 1_455 1_455 ?

M1MN 07 M2 61.75(5) 1_455 1_455 ?

P2 O8 M3 128.07(13) . 3_656 ?

P2 O8 M2 125.72(13) . 3_656 ?

M3 O8 M2 103.76(10) 3_656 3_656 ?

P2 O8 M2 65.32(8) . . ?

M3 O8 M2 109.48(8) 3_656 . ?

M2 O8 M2 115.46(8) 3_656 . ?

P2 O8 M2 55.84(7) . 1_556 ?

M3 O8 M2 85.57(7) 3_656 1_556 ?

M2 O8 M2 123.76(8) 3_656 1_556 ?

M2 O8 M2 112.68(6) . 1_556 ?

_diffrn_measured_fraction_theta_max    0.999

_diffrn_reflns_theta_full              30.05

_diffrn_measured_fraction_theta_full   0.999

_refine_diff_density_max    1.730

_refine_diff_density_min   -1.317

_refine_diff_density_rms    0.138