#

# h,k,l, Fc-squared, Fo-squared, sigma(Fo-squared) and status flag

#

data_b5

_shelx_title ' P21c in P2(1)/c'

_shelx_refln_list_code          4

_shelx_F_calc_maximum      184.56

_exptl_crystal_F_000       712.15

_reflns_d_resolution_high  0.7097

loop_

_symmetry_equiv_pos_as_xyz

'x, y, z'

'-x, y+1/2, -z+1/2'

'-x, -y, -z'

'x, -y-1/2, z-1/2'

_cell_length_a     8.7990

_cell_length_b    11.5700

_cell_length_c     6.1370

_cell_angle_alpha  90.000

_cell_angle_beta   99.320

_cell_angle_gamma  90.000

_shelx_F_squared_multiplier     1.000

loop_

_refln_index_h

_refln_index_k

_refln_index_l

_refln_F_squared_calc

_refln_F_squared_meas

_refln_F_squared_sigma

_refln_observed_status

2   0   0      118.21      102.61      5.52 o

3   0   0    15761.77    16100.56     44.54 o

4   0   0     1035.52     1273.86     24.69 o

5   0   0     7129.43     7385.97     40.23 o

6   0   0     3807.80     3647.38     41.41 o

7   0   0     1755.17     1904.59     26.19 o

8   0   0       27.17       27.13      8.28 o

9   0   0     4328.72     4192.87     44.54 o

10   0   0       42.39       35.64     10.01 o

11   0   0      626.70      622.20     21.67 o

12   0   0     1036.93     1008.17     28.28 o

1   1   0      214.54      245.40      4.65 o

2   1   0      155.68      291.12      6.86 o

3   1   0     2160.98     2142.97     62.82 o

4   1   0     5819.40     5737.18     31.59 o

5   1   0     8178.75     8367.93     56.41 o

6   1   0      309.79      384.56     26.25 o

7   1   0      940.79      906.22     21.57 o

8   1   0     9630.74     9458.30     71.43 o

9   1   0     1179.74     1263.06     25.42 o

10   1   0       97.03       93.04     10.82 o

11   1   0        4.59        6.88      9.40 o

12   1   0     1024.71     1069.69     28.40 o

0   2   0      277.21      213.16      7.52 o

1   2   0       25.41       40.31      4.85 o

2   2   0      191.88      191.08      6.74 o

3   2   0      526.25      556.62      9.94 o

4   2   0     1347.51     1299.21     16.13 o

5   2   0     2585.58     2753.03     59.08 o

6   2   0      790.22      855.69     20.94 o

7   2   0     5768.58     5793.07     44.98 o

8   2   0      387.76      459.23     15.14 o

9   2   0      552.23      528.95     50.00 o

10   2   0      606.83      632.61     20.22 o

11   2   0       98.90      152.53     13.59 o

12   2   0        6.48       14.50     10.50 o

1   3   0    29265.88    27454.89    180.98 o

2   3   0    24125.33    22814.58     89.86 o

3   3   0     4612.24     4500.45     47.66 o

4   3   0     4068.75     4069.38     40.96 o

5   3   0     1201.03     1046.29     17.01 o

6   3   0      903.11      929.40     18.01 o

7   3   0       13.24        7.09      7.84 o

8   3   0     5129.92     4892.06     45.42 o

9   3   0        2.56        2.80      8.32 o

10   3   0      596.80      622.47     25.33 o

11   3   0      552.86      552.36     24.55 o

12   3   0       94.71       95.04     13.47 o

0   4   0    28428.31    27120.89     83.15 o

1   4   0     4582.37     4544.01     25.20 o

2   4   0      690.77      675.57     11.27 o

3   4   0     5834.61     5681.88     32.37 o

4   4   0       85.38      115.21      7.52 o

5   4   0     3768.68     3949.56     40.00 o

6   4   0     3537.22     3603.48     34.36 o

7   4   0        0.33        8.35      7.94 o

8   4   0      582.30      550.86     17.46 o

9   4   0     1451.00     1511.55     73.30 o

10   4   0      299.12      302.40     16.13 o

11   4   0        1.68        2.92     10.50 o

1   5   0      306.87      334.63      9.06 o

2   5   0     4783.58     4878.17     30.28 o

3   5   0      488.09      511.94     11.60 o

4   5   0      154.56      187.68      8.95 o

5   5   0      532.41      545.82     27.67 o

6   5   0     1275.03     1139.86     21.11 o

7   5   0     2092.68     2016.03     29.16 o

8   5   0        5.49        4.99     12.35 o

9   5   0      228.66      206.08     18.45 o

10   5   0      372.04      352.15     27.03 o

11   5   0      446.21      451.56     20.64 o

0   6   0     5452.61     5321.73     46.59 o

1   6   0      227.83      314.51     18.28 o

2   6   0     5444.67     5326.99     81.43 o

3   6   0      497.92      488.79     12.67 o

4   6   0     1167.23     1104.53     19.39 o

5   6   0       90.03       99.03      9.50 o

6   6   0     2201.00     2249.99     55.32 o

7   6   0     3978.41     3935.28     41.10 o

8   6   0      135.70      113.09     11.27 o

9   6   0     1983.90     1912.52     32.83 o

10   6   0     1101.15     1156.17     27.84 o

11   6   0      271.01      249.69     16.34 o

1   7   0     8395.36     8655.39    119.40 o

2   7   0     6090.35     6297.49     40.45 o

3   7   0     2695.80     2668.14     47.04 o

4   7   0      806.21      822.21     28.91 o

5   7   0       67.77       60.17      8.83 o

6   7   0      538.56      528.64     16.34 o

7   7   0       89.13       65.16     10.28 o

8   7   0      323.86      324.80     23.13 o

9   7   0     1290.03     1302.17     28.72 o

10   7   0     1054.74     1144.75     38.13 o

11   7   0       39.90       50.21     12.35 o

0   8   0     2327.71     2538.03     38.75 o

1   8   0     8554.61     8361.86     49.17 o

2   8   0     1738.64     1751.74     38.13 o

3   8   0      648.09      733.16     16.91 o

4   8   0      866.82      901.98     30.47 o

5   8   0      140.72      193.35     20.32 o

6   8   0     1021.65     1074.52     24.53 o

7   8   0       98.88       78.26     10.05 o

8   8   0     1578.74     1686.80     31.16 o

9   8   0      208.81      199.95     14.47 o

10   8   0       83.32      112.10     12.71 o

1   9   0      761.73      663.86     16.69 o

2   9   0      245.90      297.87     15.94 o

3   9   0      424.65      456.56     15.03 o

4   9   0       99.56       87.39     16.58 o

5   9   0     2092.39     2215.30     64.85 o

6   9   0     3332.86     3367.80     40.32 o

7   9   0     1308.37     1240.13     26.85 o

8   9   0      801.50      823.19     41.11 o

9   9   0     2013.05     2039.32     36.91 o

10   9   0       76.32       82.47     12.92 o

0  10   0     2663.72     2829.95     47.50 o

1  10   0     1638.37     1574.13     25.64 o

2  10   0       98.34       76.69      9.94 o

3  10   0     3341.90     3455.33     88.77 o

4  10   0      340.26      422.65     35.01 o

5  10   0     1046.91      976.93     22.87 o

6  10   0       38.99       37.58      9.71 o

7  10   0      234.36      241.94     14.35 o

8  10   0      455.65      462.43     19.55 o

9  10   0     1158.66     1231.35     30.05 o

1  11   0      302.37      297.15     18.43 o

2  11   0     3795.18     3727.24     41.11 o

3  11   0      675.10      684.83     24.69 o

4  11   0      212.56      221.10     19.06 o

5  11   0     1064.63     1119.10     27.03 o

6  11   0      248.67      218.43     14.36 o

7  11   0      497.84      479.34     19.78 o

8  11   0       22.28       24.18     10.72 o

9  11   0       45.96       76.11     12.71 o

0  12   0      242.76      228.48     19.06 o

1  12   0     2413.47     2226.63     39.38 o

2  12   0     1438.69     1411.57     27.74 o

3  12   0       16.18       19.96      9.05 o

4  12   0      144.05      162.12     15.31 o

5  12   0      165.15      179.16     13.25 o

6  12   0       26.12       49.88     13.92 o

7  12   0     1512.91     1581.90     33.48 o

8  12   0      233.47      237.05     16.47 o

1  13   0      552.62      512.20     19.11 o

2  13   0       80.37       99.32     21.55 o

3  13   0      302.12      296.64     16.02 o

4  13   0        9.30       17.50      9.37 o

5  13   0       27.29       28.33     12.82 o

6  13   0       43.17       43.87     11.39 o

7  13   0     2162.05     2124.74     48.30 o

0  14   0       13.58       19.39     13.44 o

1  14   0      394.57      345.67     17.34 o

2  14   0      302.37      310.02     16.79 o

3  14   0        0.17        6.49      9.82 o

4  14   0       16.79       12.64     10.05 o

5  14   0      313.35      287.74     17.79 o

6  14   0      309.76      350.37     21.42 o

1  15   0      627.50      679.29     23.44 o

2  15   0     2115.18     2211.42     39.34 o

3  15   0       25.05       29.32     11.39 o

4  15   0      339.98      347.12     18.77 o

0  16   0     1326.46     1354.03     46.26 o

1  16   0      775.75      750.53     25.30 o

2  16   0      167.96      150.20     25.62 o

-12   1   1      439.44      486.34     28.76 o

-11   1   1       92.79       86.28     17.50 o

-10   1   1      496.15      511.35     25.93 o

-9   1   1      380.86      380.70     21.89 o

-8   1   1      484.79      482.30     22.51 o

-7   1   1     1596.35     1749.43     35.33 o

-6   1   1     5460.53     5157.30     52.83 o

-5   1   1     3683.74     3632.61     40.63 o

-4   1   1       73.88       66.56      8.75 o

-3   1   1    32043.19    30156.52     89.08 o

-2   1   1     2174.33     2298.92     22.19 o

-1   1   1      301.14      235.05      8.43 o

0   1   1        3.03        6.86      5.63 o

1   1   1     2751.84     2472.71     20.95 o

2   1   1     1783.30     1715.34     20.30 o

3   1   1    14920.52    14547.68     65.94 o

4   1   1       29.34       31.26      7.52 o

5   1   1      820.89      769.21     20.95 o

6   1   1     6045.80     6060.62     60.64 o

7   1   1      327.86      291.63     18.45 o

8   1   1     1009.33      963.34     30.32 o

9   1   1      201.84      184.40     17.83 o

10   1   1      315.33      308.19     21.89 o

11   1   1        0.54       12.20     13.76 o

-12   2   1       16.56       18.12     15.94 o

-11   2   1     3281.12     3425.08     64.71 o

-10   2   1      309.89      306.30     21.89 o

-9   2   1       23.91       18.45     12.82 o

-8   2   1      624.54      622.00     24.69 o

-7   2   1      503.66      566.37     22.19 o

-6   2   1        5.09        2.51     10.64 o

-5   2   1      792.35      632.64     18.74 o

-4   2   1      112.99      115.66      9.99 o

-3   2   1     3649.99     3929.25     33.77 o

-2   2   1       87.45      104.07      8.75 o

-1   2   1      243.81      389.45     11.26 o

0   2   1      646.40      693.57     12.82 o

2   2   1    34063.41    32529.81     90.34 o

3   2   1      444.68      393.85     13.44 o

4   2   1       20.70       15.62      7.52 o

5   2   1     8648.79     8462.99     65.33 o

6   2   1       53.14       25.64     11.26 o

7   2   1      772.94      784.53     26.25 o

8   2   1      306.75      328.81     20.01 o

9   2   1     1585.05     1601.90     41.25 o

10   2   1       11.36        0.62     13.76 o

11   2   1     3481.86     3539.79     68.45 o

-12   3   1       32.69       20.30     17.18 o

-11   3   1        0.73        2.51     14.05 o

-10   3   1     1009.37     1035.85     34.68 o

-9   3   1      328.27      258.18     20.01 o

-8   3   1      383.33      332.55     20.01 o

-7   3   1      860.22      914.24     27.20 o

-6   3   1     7041.62     6788.90     62.82 o

-5   3   1        7.21       42.81      9.99 o

-4   3   1     2623.72     2515.52     32.21 o

-3   3   1     3714.72     3865.81     35.33 o

-2   3   1       75.31      117.83      9.08 o

-1   3   1      485.63      589.82     13.76 o

0   3   1      695.36      862.68     15.94 o

1   3   1    19313.99    19205.21     68.77 o

2   3   1      165.90      206.62     10.31 o

3   3   1       26.18       29.08      7.81 o

4   3   1     7320.83     7685.64     58.46 o

5   3   1     3911.64     4120.21     47.82 o

6   3   1      261.89      260.98     16.56 o

7   3   1        5.81        1.89     10.31 o

8   3   1      382.00      428.85     21.89 o

9   3   1      315.45      303.18     21.24 o

10   3   1      560.67      534.81     28.14 o

11   3   1       39.59       38.13     16.27 o

-12   4   1       41.43       32.50     15.94 o

-11   4   1       17.07       14.05     14.70 o

-10   4   1        2.33       -4.68     12.82 o

-9   4   1     1104.49     1084.29     34.39 o

-8   4   1     1477.73     1552.80     37.51 o

-7   4   1     2305.85     2190.45     41.25 o

-6   4   1     1669.79     1578.15     32.50 o

-5   4   1    16024.46    15900.14     89.69 o

-4   4   1    11291.03    11356.09     70.01 o

-3   4   1      701.54      650.43     17.50 o

-2   4   1     2822.75     2880.90     30.94 o

-1   4   1     1486.07     1605.96     22.51 o

0   4   1       59.50       91.91      8.75 o

1   4   1     1732.82     1671.29     23.46 o

2   4   1      608.46      703.27     16.88 o

3   4   1     7629.69     8127.60     57.81 o

4   4   1    11584.44    11343.89     74.08 o

5   4   1     2510.88     2521.44     39.07 o

6   4   1     1755.83     1874.46     37.51 o

7   4   1     2505.03     2529.58     45.94 o

8   4   1      837.02      828.62     29.70 o

9   4   1     1113.62     1079.61     35.62 o

10   4   1      539.77      568.87     28.43 o

11   4   1      232.83      220.35     21.89 o

-11   5   1     1060.45     1070.53     38.75 o

-10   5   1       76.85      109.41     17.83 o

-9   5   1     2479.98     2442.39     50.33 o

-8   5   1      216.79      240.35     18.74 o

-7   5   1       53.93       73.13     13.44 o

-6   5   1        3.20        0.94     11.55 o

-5   5   1     4768.65     4714.11     51.89 o

-4   5   1     1994.61     2241.40     33.77 o

-3   5   1     5543.80     5282.65     47.50 o

-2   5   1    10328.68    10449.04     63.15 o

-1   5   1      583.13      650.14     16.56 o

0   5   1      421.54      421.01     14.38 o

1   5   1     9804.83    10041.43     60.93 o

2   5   1     1113.44     1226.82     23.46 o

3   5   1    11455.10    11271.08     72.19 o

4   5   1     1178.12     1185.86     26.87 o

5   5   1      757.26      793.90     24.37 o

6   5   1     3768.57     3688.89     52.83 o

7   5   1        1.93        6.25     10.93 o

8   5   1     1386.75     1350.28     38.13 o

9   5   1      128.10      156.29     17.18 o

10   5   1      295.61      332.26     23.75 o

11   5   1      697.48      709.84     34.68 o

-11   6   1       67.37       55.01     17.50 o

-10   6   1        0.54       13.44     14.05 o

-9   6   1      965.26      949.25     33.12 o

-8   6   1        0.42        0.33     12.49 o

-7   6   1      553.84      592.00     24.37 o

-6   6   1      721.48      714.20     24.69 o

-5   6   1        5.71        1.89     11.55 o

-4   6   1     3016.92     3309.13     43.14 o

-3   6   1       38.78       61.26     10.64 o

-2   6   1      378.79      334.15     14.70 o

-1   6   1     2328.80     2637.42     34.39 o

0   6   1    13317.45    13729.38     76.26 o

1   6   1      731.41      702.32     19.39 o

2   6   1      622.90      566.04     18.45 o

3   6   1    19578.51    19675.93    101.57 o

4   6   1     2998.45     2919.03     42.81 o

5   6   1      740.89      680.75     23.46 o

6   6   1     1356.83     1401.85     35.01 o

7   6   1     1720.05     1918.51     42.52 o

8   6   1     1146.90     1262.77     37.84 o

9   6   1      524.81      529.48     27.20 o

10   6   1     2561.96     2633.97     59.37 o

11   6   1      125.48      153.17     20.30 o

-11   7   1      379.28      300.05     25.02 o

-10   7   1      365.99      325.69     24.07 o

-9   7   1      754.66      779.85     31.88 o

-8   7   1        0.65       -2.51     12.82 o

-7   7   1     2276.50     2216.71     44.70 o

-6   7   1     1447.52     1555.96     35.95 o

-5   7   1     1726.64     1698.78     35.95 o

-4   7   1    12558.77    12332.54     87.51 o

-3   7   1     1720.78     1858.52     33.77 o

-2   7   1     1306.44     1390.59     28.43 o

-1   7   1     2405.57     2420.20     35.62 o

0   7   1      214.98      231.60     13.76 o

1   7   1       78.64       52.18     10.64 o

2   7   1     2986.21     2961.84     41.58 o

3   7   1      236.36      195.65     15.00 o

4   7   1      302.19      246.60     17.18 o

5   7   1     1083.69     1163.06     31.56 o

6   7   1     3484.69     3459.14     55.63 o

7   7   1       17.29        8.75     11.87 o

8   7   1     1111.26     1098.02     35.95 o

9   7   1        2.99        4.39     13.14 o

10   7   1      170.59      162.86     19.68 o

-10   8   1       39.55       28.43     15.00 o

-9   8   1        5.33        1.89     13.76 o

-8   8   1       36.03       30.00     13.14 o

-7   8   1      131.64      162.86     17.18 o

-6   8   1      635.45      627.95     25.02 o

-5   8   1      267.56      263.19     18.12 o

-4   8   1      243.56      239.41     17.18 o

-3   8   1       43.76       40.31     12.20 o

-2   8   1     3502.45     3432.60     45.94 o

-1   8   1       45.69       50.00     12.20 o

0   8   1        6.51       17.18     10.31 o

1   8   1       86.31       67.21     12.82 o

2   8   1     1572.98     1516.89     32.50 o

3   8   1      249.20      238.17     17.18 o

4   8   1     2769.39     2576.46     45.32 o

5   8   1     1219.07     1146.50     32.50 o

6   8   1       36.35       36.57     12.82 o

7   8   1       53.62       58.46     14.38 o

8   8   1       37.29       20.63     13.44 o

9   8   1        1.47        0.94     13.76 o

10   8   1      210.35      210.68     23.46 o

-10   9   1       60.42       75.02     17.83 o

-9   9   1      603.17      567.60     29.70 o

-8   9   1       35.06       27.49     13.76 o

-7   9   1      472.02      385.71     23.75 o

-6   9   1       11.21       20.95     11.87 o

-5   9   1      465.75      435.10     22.19 o

-4   9   1      356.31      331.64     19.39 o

-3   9   1      645.45      655.77     24.37 o

-2   9   1      442.52      457.61     21.24 o

-1   9   1     2416.68     2450.20     42.20 o

0   9   1       61.02       56.90     13.14 o

1   9   1      133.82      132.54     14.70 o

2   9   1       14.96       21.89     11.87 o

3   9   1      121.39      109.70     14.70 o

4   9   1      378.93      350.06     19.68 o

5   9   1      457.12      485.43     23.75 o

6   9   1      131.85      143.76     17.50 o

7   9   1       10.59        5.95     13.44 o

8   9   1      406.56      341.30     25.02 o

9   9   1      176.44      165.33     20.30 o

-9  10   1      607.50      665.14     32.21 o

-8  10   1       18.02        4.39     14.38 o

-7  10   1       11.36       -7.52     12.49 o

-6  10   1       47.47       44.38     14.70 o

-5  10   1     1847.67     1829.76     42.81 o

-4  10   1      360.73      343.19     20.63 o

-3  10   1     1169.60     1120.54     32.21 o

-2  10   1     1433.98     1509.05     35.95 o

-1  10   1        2.53       -5.30     10.93 o

0  10   1     1217.84     1195.23     33.12 o

1  10   1     3853.11     3747.03     55.01 o

2  10   1        1.58        5.95     11.87 o

3  10   1     7327.41     7195.24     78.76 o

4  10   1     2433.81     2395.51     47.50 o

5  10   1       31.89       38.75     13.76 o

6  10   1      315.70      238.50     20.63 o

7  10   1       15.05       22.51     14.05 o

8  10   1     1710.20     1609.38     46.88 o

9  10   1      650.26      626.68     33.77 o

-9  11   1      335.16      334.77     26.87 o

-8  11   1      829.08      788.28     34.68 o

-7  11   1     1486.80     1456.86     43.43 o

-6  11   1      969.15     1113.67     36.89 o

-5  11   1     2519.98     2501.47     51.56 o

-4  11   1     3920.73     3925.18     62.20 o

-3  11   1      447.27      495.41     25.02 o

-2  11   1     2957.75     2897.78     51.56 o

-1  11   1      487.54      454.16     23.13 o

0  11   1     2296.91     2329.24     46.26 o

1  11   1       46.58       75.02     13.76 o

2  11   1     1666.63     1718.49     41.25 o

3  11   1      156.75      150.04     17.18 o

4  11   1       17.80       20.01     12.20 o

5  11   1     2078.51     2096.98     49.39 o

6  11   1     1375.18     1375.27     42.20 o

7  11   1       54.53       50.95     16.27 o

8  11   1       61.06      112.21     18.74 o

-8  12   1     1504.41     1413.11     45.64 o

-7  12   1        9.00        7.52     14.70 o

-6  12   1      145.03      130.65     17.50 o

-5  12   1     1053.36     1122.42     37.51 o

-4  12   1      204.04      227.24     20.01 o

-3  12   1       74.06       81.59     15.62 o

-2  12   1       34.89       24.69     12.82 o

-1  12   1     1743.30     1757.24     42.81 o

0  12   1       79.90       74.70     15.00 o

1  12   1        0.12        1.56     12.82 o

2  12   1      112.52      153.78     17.18 o

3  12   1      730.39      804.87     31.56 o

4  12   1      158.65      177.86     18.12 o

5  12   1       22.43       18.74     13.76 o

6  12   1     1154.66     1156.49     40.63 o

7  12   1      158.63      128.47     20.30 o

-7  13   1        1.76       10.93     14.70 o

-6  13   1       66.49       54.07     18.12 o

-5  13   1       44.04       62.20     15.94 o

-4  13   1      787.39      732.03     32.21 o

-3  13   1      550.82      647.02     29.08 o

-2  13   1      308.48      339.12     23.75 o

-1  13   1      645.83      646.07     29.08 o

0  13   1      997.86     1012.40     35.62 o

1  13   1     1073.07     1112.11     37.19 o

2  13   1      101.31       99.39     17.50 o

3  13   1      141.33      125.02     18.12 o

4  13   1     1630.39     1540.31     45.64 o

5  13   1        1.34        5.30     14.05 o

6  13   1       17.96       16.56     16.56 o

7  13   1     1242.10     1201.51     44.99 o

-6  14   1      347.31      378.20     28.14 o

-5  14   1     1458.79     1702.23     48.44 o

-4  14   1     1056.65     1095.23     39.69 o

-3  14   1      139.00      131.89     18.74 o

-2  14   1     1813.75     1986.05     50.00 o

-1  14   1     2122.11     2139.50     51.27 o

0  14   1       56.72       70.34     15.94 o

1  14   1      559.67      590.74     29.38 o

2  14   1     1107.10     1144.61     40.02 o

3  14   1        2.86        5.30     14.05 o

4  14   1     2428.89     2527.40     59.37 o

5  14   1        2.24       -2.51     15.00 o

-4  15   1      491.21      485.43     30.32 o

-3  15   1      720.25      822.37     35.62 o

-2  15   1       46.25       52.83     16.88 o

-1  15   1        1.21        6.86     15.00 o

0  15   1       52.82       49.71     16.56 o

1  15   1      260.92      297.87     23.75 o

2  15   1      105.90       75.02     17.50 o

3  15   1       70.42       52.51     17.18 o

4  15   1      479.40      512.92     30.65 o

-2  16   1       60.86       59.37     17.18 o

-1  16   1       17.49       18.12     15.94 o

0  16   1      543.64      520.11     30.94 o

1  16   1      288.37      309.45     25.02 o

-12   0   2       70.38      106.29     18.45 o

-11   0   2        0.23       -2.51     15.00 o

-10   0   2     2433.72     2344.23     50.95 o

-9   0   2     4717.54     4636.90     66.27 o

-8   0   2     5745.63     5317.95     65.94 o

-7   0   2        3.06       -5.01     12.82 o

-6   0   2     6794.69     7109.29     64.09 o

-5   0   2        3.97        6.86      9.08 o

-4   0   2     5881.01     6220.03     50.00 o

-3   0   2     4060.30     4366.20     38.45 o

-2   0   2    13312.35    13023.93     60.02 o

-1   0   2    31801.37    30089.31     84.39 o

0   0   2    11973.97    11079.79     50.95 o

1   0   2     3534.38     3709.19     31.56 o

2   0   2      496.20      618.26     15.32 o

3   0   2     9773.46     9957.66     61.59 o

4   0   2     8271.22     8155.75     61.59 o

5   0   2        8.97       15.00     10.31 o

6   0   2     2577.81     2539.89     41.87 o

7   0   2       93.79       90.64     13.44 o

8   0   2     2436.89     2112.63     45.64 o

9   0   2       16.28       29.08     12.49 o

10   0   2      863.06      872.99     34.39 o

11   0   2      296.69      299.43     24.37 o

-12   1   2        0.02        7.81     14.05 o

-11   1   2      144.35      158.14     19.06 o

-10   1   2      880.65      867.98     32.50 o

-9   1   2     1087.73     1029.90     32.83 o

-8   1   2      395.33      430.09     21.24 o

-7   1   2        8.73       10.31     12.20 o

-6   1   2     3634.80     3662.64     46.88 o

-5   1   2     1286.46     1324.03     26.25 o

-4   1   2     8676.32     8573.63     58.75 o

-3   1   2     1661.64     1845.37     25.64 o

-2   1   2     2423.69     2549.58     27.49 o

-1   1   2    12776.70    12549.76     55.34 o

0   1   2     4843.64     4420.92     33.12 o

1   1   2     4898.67     5130.43     37.51 o

2   1   2     2057.31     2096.37     26.58 o

3   1   2     2587.15     2797.13     33.44 o

4   1   2     3121.35     3343.20     40.31 o

5   1   2     1508.99     1407.48     29.38 o

6   1   2     5205.01     5117.29     59.37 o

7   1   2      459.08      513.53     22.51 o

8   1   2     3100.33     3184.40     55.34 o

9   1   2       43.78       41.58     14.38 o

10   1   2      425.82      455.72     27.49 o

11   1   2      546.57      601.70     31.26 o

-12   2   2      148.42      175.35     21.24 o

-11   2   2      292.45      288.18     23.13 o

-10   2   2       10.73       14.70     12.49 o

-9   2   2      411.53      413.82     23.46 o

-8   2   2      997.60     1033.02     30.65 o

-7   2   2       11.38       10.64     11.87 o

-6   2   2     1416.48     1459.37     30.94 o

-5   2   2     3407.93     3373.81     41.25 o

-4   2   2      584.04      656.71     18.12 o

-3   2   2     2195.84     2304.54     29.08 o

-2   2   2     1373.08     1455.63     22.19 o

-1   2   2     2506.82     2253.27     25.31 o

0   2   2     3292.31     3285.06     30.32 o

1   2   2      748.47      693.28     15.94 o

2   2   2     4066.51     4246.18     38.45 o

3   2   2      473.32      471.66     15.94 o

4   2   2       93.96      110.97     10.93 o

5   2   2     1377.67     1396.84     30.00 o

6   2   2     3980.44     3983.64     53.13 o

7   2   2       14.26       10.31     10.93 o

8   2   2      122.58      125.97     15.94 o

9   2   2     1366.64     1383.73     39.69 o

10   2   2      181.85      220.35     20.63 o

11   2   2      176.21      170.67     20.63 o

-12   3   2      665.91      641.06     32.83 o

-11   3   2      968.00      966.75     36.57 o

-10   3   2       65.33       46.88     15.00 o

-9   3   2     3110.47     2943.72     53.45 o

-8   3   2     1927.43     1931.33     40.96 o

-7   3   2      143.94      165.33     15.32 o

-6   3   2      498.48      442.29     20.01 o

-5   3   2       80.98       83.45     11.87 o

-4   3   2       32.03       14.70      8.43 o

-3   3   2    13498.15    13052.69     69.69 o

-2   3   2      219.66      219.73     11.55 o

-1   3   2      323.53      285.05     11.87 o

0   3   2     8497.40     8664.27     51.89 o

1   3   2     4413.42     4465.91     38.75 o

2   3   2      492.87      523.23     15.94 o

3   3   2     3537.18     3593.24     40.31 o

4   3   2     1727.06     1720.35     31.26 o

5   3   2      412.97      364.44     18.12 o

6   3   2     2166.43     2110.13     40.31 o

7   3   2       68.74       50.00     12.82 o

8   3   2      818.21      769.21     29.70 o

9   3   2      712.56      712.96     30.65 o

10   3   2      147.09      103.16     17.50 o

11   3   2        9.74       10.31     15.32 o

-11   4   2      156.00      175.65     20.30 o

-10   4   2        0.30        4.39     12.49 o

-9   4   2     1227.28     1250.25     36.57 o

-8   4   2     2803.80     2699.01     48.77 o

-7   4   2      312.23      291.30     18.45 o

-6   4   2     3385.19     3319.12     46.88 o

-5   4   2      799.44      777.96     22.51 o

-4   4   2       39.43       47.21     10.31 o

-3   4   2     1210.93     1058.66     22.51 o

-2   4   2       36.79       21.89      8.43 o

-1   4   2        0.45       17.83      8.13 o

0   4   2     1131.93     1019.26     20.63 o

1   4   2      993.59      923.32     20.01 o

2   4   2      304.94      347.88     14.70 o

3   4   2      507.18      469.16     17.18 o

4   4   2       25.95       27.20     10.31 o

5   4   2     3763.20     3715.44     50.00 o

6   4   2     1104.41     1026.45     29.70 o

7   4   2      225.85      225.68     17.83 o

8   4   2     1161.64     1156.81     35.33 o

9   4   2      220.34      247.25     20.63 o

10   4   2       22.23       21.89     15.00 o

11   4   2      533.00      441.67     29.38 o

-11   5   2       13.54       16.88     15.32 o

-10   5   2      152.51      172.85     18.45 o

-9   5   2      113.29      119.40     15.62 o

-8   5   2      745.61      717.65     27.82 o

-7   5   2      376.43      368.21     20.63 o

-6   5   2      386.46      415.38     19.68 o

-5   5   2       67.07       80.65     12.20 o

-4   5   2      107.08      108.47     11.87 o

-3   5   2      298.59      359.46     15.94 o

-2   5   2    14924.07    14880.56     80.94 o

-1   5   2     5333.10     5322.67     47.82 o

0   5   2      384.65      363.52     14.38 o

1   5   2     9054.42     9189.71     63.44 o

2   5   2     3296.33     3439.14     40.96 o

3   5   2     5101.77     5256.40     53.78 o

4   5   2      827.31      775.17     24.07 o

5   5   2     2046.89     2060.12     39.07 o

6   5   2     1330.13     1381.84     34.39 o

7   5   2     1115.01     1017.41     33.12 o

8   5   2       79.64       70.95     15.62 o

9   5   2        0.06       -6.86     13.14 o

10   5   2       64.70       50.00     16.56 o

-11   6   2      616.69      621.06     31.88 o

-10   6   2     1102.88     1111.49     38.45 o

-9   6   2       52.04       43.43     14.38 o

-8   6   2     1622.59     1561.59     39.07 o

-7   6   2      470.66      423.84     22.51 o

-6   6   2      632.27      629.19     24.07 o

-5   6   2     1501.27     1466.23     32.83 o

-4   6   2     1532.80     1516.89     31.26 o

-3   6   2      592.88      579.19     20.01 o

-2   6   2      402.78      441.96     17.50 o

-1   6   2     1214.35     1098.67     25.02 o

0   6   2     1650.81     1543.43     28.76 o

1   6   2     1340.42     1329.66     27.20 o

2   6   2       61.88       86.28     12.20 o

3   6   2     1197.68     1230.56     28.76 o

4   6   2        8.98        5.01     11.55 o

5   6   2     1740.37     1782.88     37.84 o

6   6   2     5009.69     5008.86     66.27 o

7   6   2       17.99       24.37     13.14 o

8   6   2      735.15      728.58     31.56 o

9   6   2     2003.02     1971.34     50.62 o

10   6   2       60.40       45.94     15.94 o

-11   7   2      443.14      473.84     30.00 o

-10   7   2      578.84      569.17     30.00 o

-9   7   2      291.06      286.00     22.51 o

-8   7   2      303.78      300.67     21.57 o

-7   7   2      807.55      818.92     29.38 o

-6   7   2       30.34       42.52     12.49 o

-5   7   2     2357.10     2194.52     41.25 o

-4   7   2     1953.24     2210.46     39.69 o

-3   7   2     7951.56     7971.64     70.01 o

-2   7   2       62.37       78.14     12.20 o

-1   7   2      972.83      917.99     24.69 o

0   7   2    10454.10    10459.97     76.58 o

1   7   2      209.38      204.11     15.00 o

2   7   2      105.09      121.90     13.44 o

3   7   2       16.03       17.83     11.26 o

4   7   2     2223.03     2255.16     41.87 o

5   7   2       41.65       41.87     12.49 o

6   7   2      726.64      714.52     28.14 o

7   7   2     1335.55     1364.66     39.07 o

8   7   2      139.83      155.96     18.45 o

9   7   2      450.64      504.16     28.43 o

10   7   2        8.32        3.12     14.70 o

-10   8   2     1501.43     1573.14     46.59 o

-9   8   2      202.40      180.04     20.30 o

-8   8   2      954.33     1026.78     35.01 o

-7   8   2     1927.56     1922.28     44.08 o

-6   8   2       52.91       42.81     13.14 o

-5   8   2     1685.29     1785.38     39.07 o

-4   8   2     1151.08     1168.69     31.56 o

-3   8   2      285.57      267.23     18.12 o

-2   8   2      579.57      650.76     23.75 o

-1   8   2    13899.11    13657.80     93.47 o

0   8   2      204.32      219.44     16.27 o

1   8   2     3227.65     3500.72     48.77 o

2   8   2     3252.13     3345.38     49.39 o

3   8   2       96.04      101.89     14.70 o

4   8   2      415.99      425.08     21.89 o

5   8   2     4435.20     4357.15     63.15 o

6   8   2      214.14      198.16     18.12 o

7   8   2      606.37      622.32     28.43 o

8   8   2      215.10      190.97     21.24 o

9   8   2        1.09       -5.01     14.05 o

-10   9   2      360.18      341.30     25.93 o

-9   9   2      710.13      726.40     32.83 o

-8   9   2        2.06        2.51     12.82 o

-7   9   2     2877.37     2890.27     55.34 o

-6   9   2      207.73      217.22     19.06 o

-5   9   2      107.26      121.58     15.62 o

-4   9   2     1011.63     1105.54     31.56 o

-3   9   2      310.27      375.69     20.30 o

-2   9   2     4880.45     4812.23     60.64 o

-1   9   2      536.16      551.05     22.51 o

0   9   2     1083.10     1131.47     30.94 o

1   9   2     2112.49     1924.79     39.40 o

2   9   2      131.18      137.52     15.00 o

3   9   2        7.41        8.75     11.55 o

4   9   2     5689.45     5798.37     72.84 o

5   9   2       11.41       23.75     12.82 o

6   9   2       98.89       83.77     14.70 o

7   9   2     4612.75     4489.99     73.46 o

8   9   2      811.73      903.64     36.24 o

9   9   2      213.00      227.54     22.81 o

-9  10   2      156.71      193.80     20.63 o

-8  10   2      305.56      280.37     24.69 o

-7  10   2      386.27      410.70     24.69 o

-6  10   2     1878.01     1754.74     44.38 o

-5  10   2      455.15      518.54     25.31 o

-4  10   2     1732.60     1733.17     41.58 o

-3  10   2     1141.67     1097.11     32.83 o

-2  10   2      989.01     1058.04     31.56 o

-1  10   2     2453.30     2405.17     45.64 o

0  10   2      156.82      122.84     15.00 o

1  10   2     1560.58     1541.87     37.51 o

2  10   2      897.30      919.87     30.65 o

3  10   2     1808.54     1940.08     43.43 o

4  10   2       20.29       30.32     11.87 o

5  10   2       27.55       25.93     12.49 o

6  10   2      593.11      572.94     28.76 o

7  10   2      307.77      313.49     23.75 o

8  10   2        4.75        0.62     15.32 o

-9  11   2       20.25       15.94     15.62 o

-8  11   2      524.84      586.67     30.65 o

-7  11   2       63.73       25.64     15.32 o

-6  11   2       33.83       21.89     14.05 o

-5  11   2        9.73       41.58     15.32 o

-4  11   2      290.62      296.31     20.30 o

-3  11   2       26.56       39.69     13.76 o

-2  11   2     3082.74     3068.75     54.40 o

-1  11   2     2512.35     2588.66     49.71 o

0  11   2       59.16       66.89     14.05 o

1  11   2     4336.28     4340.27     64.38 o

2  11   2      324.51      296.31     21.24 o

3  11   2      977.34      965.52     33.77 o

4  11   2        1.16      -10.31     12.49 o

5  11   2      153.74      138.79     19.06 o

6  11   2     1149.98     1108.99     39.40 o

7  11   2      127.52      122.23     19.68 o

8  11   2      166.01      216.28     23.13 o

-8  12   2       22.23       57.19     16.27 o

-7  12   2     1669.89     1806.63     49.06 o

-6  12   2      513.97      453.54     28.43 o

-5  12   2      107.87       86.90     17.18 o

-4  12   2      306.39      270.06     21.24 o

-3  12   2      296.39      292.57     22.19 o

-2  12   2        0.42        5.63     13.44 o

-1  12   2     1276.92     1165.85     35.95 o

0  12   2      126.76      122.52     15.94 o

1  12   2        8.47       -4.39     12.20 o

2  12   2      470.60      408.52     24.69 o

3  12   2      147.76      145.36     17.83 o

4  12   2      174.05      152.84     18.74 o

5  12   2       12.06       10.64     13.76 o

6  12   2     1572.25     1653.79     48.44 o

7  12   2      380.00      326.96     25.64 o

-7  13   2       11.07       41.87     15.62 o

-6  13   2      396.19      368.50     25.64 o

-5  13   2       49.33       55.34     15.94 o

-4  13   2       96.41       89.08     17.50 o

-3  13   2       11.38        9.08     14.05 o

-2  13   2      650.10      621.67     30.32 o

-1  13   2      967.09      904.87     34.39 o

0  13   2        3.35        0.94     12.49 o

1  13   2      776.23      728.58     31.26 o

2  13   2       35.16       30.94     15.00 o

3  13   2       36.52       37.84     14.70 o

4  13   2      135.71      105.96     18.74 o

5  13   2      515.48      516.98     30.00 o

6  13   2        0.67        6.86     15.32 o

-6  14   2      235.79      223.47     22.81 o

-5  14   2       13.95       25.31     15.62 o

-4  14   2      107.48      164.71     19.68 o

-3  14   2      903.01      889.88     37.84 o

-2  14   2       46.16       33.44     16.27 o

-1  14   2       83.05       79.71     17.50 o

0  14   2        9.13        0.94     13.44 o

1  14   2        8.02       12.82     13.76 o

2  14   2      330.52      295.37     24.07 o

3  14   2      103.29      125.35     20.01 o

4  14   2      140.97      147.54     20.95 o

5  14   2        9.12       -5.95     16.27 o

-4  15   2      923.79      966.75     38.45 o

-3  15   2      239.33      253.50     25.02 o

-2  15   2     1974.11     1997.27     53.78 o

-1  15   2      584.86      563.24     31.56 o

0  15   2      364.11      390.69     27.49 o

1  15   2     1416.24     1570.96     47.82 o

2  15   2       77.54       95.32     18.74 o

3  15   2      130.83      112.53     19.68 o

-12   1   3      185.68      177.53     23.13 o

-11   1   3      545.04      608.89     30.32 o

-10   1   3      414.82      362.87     24.07 o

-9   1   3       31.36       14.05     12.82 o

-8   1   3      624.27      652.00     26.58 o

-7   1   3     3710.74     3579.48     52.83 o

-6   1   3      139.61      185.99     15.32 o

-5   1   3     7131.58     7039.24     63.44 o

-4   1   3    10438.07    10343.07     71.90 o

-3   1   3       40.23       16.27      9.08 o

-2   1   3    17009.02    16614.34     80.32 o

-1   1   3       23.77       18.12      8.13 o

0   1   3      256.05      276.92     12.20 o

1   1   3      563.23      544.80     16.56 o

2   1   3    13449.80    13440.58     76.88 o

3   1   3      192.00      222.56     13.76 o

4   1   3      159.65      127.53     13.44 o

5   1   3     2739.59     2603.65     43.43 o

6   1   3       72.73       74.40     13.44 o

7   1   3     4465.96     4371.53     63.44 o

8   1   3      511.26      510.12     25.31 o

9   1   3      381.80      408.52     24.69 o

10   1   3      511.84      499.81     30.00 o

-12   2   3     1301.42     1303.70     44.08 o

-11   2   3      996.03      925.50     36.89 o

-10   2   3      268.02      328.52     23.13 o

-9   2   3      237.21      238.50     19.68 o

-8   2   3      155.85      160.03     16.88 o

-7   2   3      992.90      985.82     29.38 o

-6   2   3    12031.31    11369.85     86.90 o

-5   2   3      183.58      174.41     13.76 o

-4   2   3      454.33      383.83     16.27 o

-3   2   3     5824.49     5599.27     50.95 o

-2   2   3     3969.93     4113.35     40.96 o

-1   2   3     5801.01     5544.90     46.26 o

0   2   3     2877.60     2759.94     33.44 o

1   2   3     3326.36     3721.39     39.69 o

2   2   3     9739.42     9540.71     66.27 o

3   2   3    12848.34    12422.88     80.65 o

4   2   3     3906.53     3993.01     50.00 o

5   2   3     1150.42     1291.53     31.56 o

6   2   3     1308.85     1218.69     33.12 o

7   2   3     1355.15     1326.54     36.57 o

8   2   3      639.82      618.26     28.76 o

9   2   3      169.30      163.77     19.06 o

10   2   3     1180.17     1156.16     40.96 o

-11   3   3       35.85       55.96     16.56 o

-10   3   3      225.18      233.49     20.30 o

-9   3   3     1055.68     1078.34     34.68 o

-8   3   3     2065.51     2065.75     44.08 o

-7   3   3      342.82      357.57     20.01 o

-6   3   3      517.25      531.36     22.19 o

-5   3   3     1918.96     1861.64     35.01 o

-4   3   3      760.53      819.54     22.81 o

-3   3   3       42.60       18.74      9.69 o

-2   3   3     2839.45     2768.69     35.01 o

-1   3   3     5946.04     6403.52     51.56 o

0   3   3     5150.16     5265.15     47.50 o

1   3   3     1365.42     1359.33     25.93 o

2   3   3      158.71      157.85     12.20 o

3   3   3     5137.09     5333.60     55.01 o

4   3   3       21.20       20.95     10.93 o

5   3   3       55.17       70.34     13.14 o

6   3   3      139.67      156.58     15.94 o

7   3   3     1774.69     1909.14     43.43 o

8   3   3      739.82      726.40     30.32 o

9   3   3      216.18      173.17     19.06 o

10   3   3     1387.84     1463.11     45.32 o

-11   4   3      240.43      283.82     23.75 o

-10   4   3      384.37      374.13     24.37 o

-9   4   3     1532.16     1509.05     41.58 o

-8   4   3      356.11      341.63     21.24 o

-7   4   3     1601.99     1712.87     38.13 o

-6   4   3     7132.96     7005.51     70.63 o

-5   4   3     5676.28     5538.95     59.37 o

-4   4   3     6052.73     6073.11     58.14 o

-3   4   3     9379.83     9310.34     69.69 o

-2   4   3     2192.62     2214.82     33.44 o

-1   4   3      276.91      244.75     13.44 o

0   4   3     7287.34     7747.85     60.02 o

1   4   3      577.86      577.30     18.74 o

2   4   3     2769.43     2906.54     40.02 o

3   4   3     4437.66     4383.08     51.56 o

4   4   3      564.10      517.31     21.57 o

5   4   3     1425.91     1390.30     33.77 o

6   4   3     2644.76     2653.66     49.71 o

7   4   3      297.09      315.38     20.95 o

8   4   3      848.31      865.18     32.50 o

9   4   3      730.13      717.32     32.21 o

10   4   3      437.91      425.08     28.14 o

-11   5   3     2031.12     2135.11     54.07 o

-10   5   3        0.85       -8.13     13.44 o

-9   5   3      320.14      375.07     22.81 o

-8   5   3      505.12      544.80     25.31 o

-7   5   3     1537.76     1319.02     35.01 o

-6   5   3       12.77       13.44     11.87 o

-5   5   3      218.11      162.21     15.62 o

-4   5   3     1493.96     1428.43     31.26 o

-3   5   3      695.31      820.81     23.75 o

-2   5   3      616.27      556.38     19.68 o

-1   5   3     7650.79     7635.31     62.82 o

0   5   3     2123.27     2178.87     34.68 o

1   5   3     1573.01     1543.14     30.32 o

2   5   3    16102.80    15855.77     95.65 o

3   5   3      971.17     1016.46     27.49 o

4   5   3       98.50      116.27     15.00 o

5   5   3     6308.48     6343.82     72.19 o

6   5   3     3897.19     3847.65     60.02 o

7   5   3        1.10       13.44     11.26 o

8   5   3      928.02      970.53     35.33 o

9   5   3      742.03      739.54     33.44 o

10   5   3       26.71       39.69     15.94 o

-11   6   3       95.78       58.46     17.50 o

-10   6   3     1828.66     1702.85     46.59 o

-9   6   3        1.27        2.18     12.82 o

-8   6   3       39.27       45.64     14.05 o

-7   6   3      161.99      165.98     17.18 o

-6   6   3     3754.13     3669.83     55.01 o

-5   6   3     1976.57     1798.49     37.51 o

-4   6   3     2523.96     2409.56     41.58 o

-3   6   3    14493.94    14455.16     95.65 o

-2   6   3      792.41      837.37     24.69 o

-1   6   3      246.24      317.26     16.56 o

0   6   3        1.10        5.30     11.26 o

1   6   3     4236.33     4114.91     50.62 o

2   6   3      503.40      488.84     20.95 o

3   6   3      675.20      617.93     23.75 o

4   6   3     1983.69     2028.24     40.63 o

5   6   3      169.27      205.67     16.88 o

6   6   3      293.02      310.69     21.24 o

7   6   3      494.76      553.55     25.93 o

8   6   3       45.85       97.21     16.27 o

9   6   3      359.92      364.14     26.58 o

-10   7   3      137.26      171.90     20.01 o

-9   7   3       13.61       16.27     13.76 o

-8   7   3      492.72      473.84     25.64 o

-7   7   3     2557.21     2603.65     50.00 o

-6   7   3      487.70      468.83     22.51 o

-5   7   3     1970.26     1971.02     40.96 o

-4   7   3     3307.62     3136.90     49.06 o

-3   7   3      841.51      933.63     27.82 o

-2   7   3     5009.03     5057.30     58.75 o

-1   7   3      164.82      157.85     15.00 o

0   7   3      233.50      252.55     16.56 o

1   7   3     1233.14     1166.18     30.00 o

2   7   3        5.70        7.81     11.26 o

3   7   3     1651.83     1574.37     36.24 o

4   7   3     6027.40     6069.69     71.57 o

5   7   3      589.61      602.32     25.64 o

6   7   3      246.65      294.75     20.95 o

7   7   3      253.93      271.00     20.95 o

8   7   3      475.22      532.60     28.14 o

9   7   3     1424.52     1385.91     45.94 o

-10   8   3      359.70      409.79     26.87 o

-9   8   3       39.60       37.51     14.70 o

-8   8   3      166.23      163.48     18.74 o

-7   8   3        3.22        0.00     12.82 o

-6   8   3      846.00      738.60     28.43 o

-5   8   3      783.53      742.34     27.82 o

-4   8   3     1589.04     1523.13     36.89 o

-3   8   3     1767.89     1767.23     38.45 o

-2   8   3       39.75       42.20     13.14 o

-1   8   3       55.44       58.46     13.76 o

0   8   3      484.46      448.21     21.24 o

1   8   3     2375.10     2375.17     43.43 o

2   8   3       30.89       35.95     13.14 o

3   8   3     1609.55     1613.15     38.45 o

4   8   3     1257.70     1221.49     34.68 o

5   8   3      394.71      348.82     21.89 o

6   8   3      985.15      986.47     35.33 o

7   8   3        5.54        8.43     14.05 o

8   8   3        3.61        0.94     12.82 o

9   8   3       61.01       56.25     17.50 o

-9   9   3      294.59      223.79     22.51 o

-8   9   3       46.05       34.06     14.70 o

-7   9   3       10.35       18.45     13.14 o

-6   9   3        1.34       11.26     12.82 o

-5   9   3        1.88        7.81     12.20 o

-4   9   3       14.08       17.18     12.20 o

-3   9   3      269.17      253.50     18.45 o

-2   9   3       62.09       78.14     14.05 o

-1   9   3      111.57      110.03     14.70 o

0   9   3      168.18      159.70     16.27 o

1   9   3     1328.65     1321.20     34.68 o

2   9   3     1243.21     1247.12     34.68 o

3   9   3      585.26      602.61     25.93 o

4   9   3        0.95        5.30     11.87 o

5   9   3       75.40       86.28     15.32 o

6   9   3      235.41      245.36     20.95 o

7   9   3        5.58       12.49     13.44 o

8   9   3      466.08      417.27     28.14 o

-9  10   3       28.22       13.44     15.00 o

-8  10   3       14.57       -0.62     14.70 o

-7  10   3      211.68      196.30     20.01 o

-6  10   3      229.42      249.11     20.95 o

-5  10   3     2506.68     2464.57     51.27 o

-4  10   3     2827.70     2849.02     53.78 o

-3  10   3      670.78      705.15     28.14 o

-2  10   3      404.90      391.34     22.19 o

-1  10   3      105.02      102.84     15.00 o

0  10   3       14.91       35.62     13.44 o

1  10   3     6542.48     6222.53     76.26 o

2  10   3      154.07      133.45     16.56 o

3  10   3      114.94      128.15     16.27 o

4  10   3     2939.19     2825.89     56.57 o

5  10   3      303.72      339.45     22.81 o

6  10   3      125.10      137.22     18.12 o

7  10   3      284.24      283.49     23.13 o

-8  11   3      263.98      277.25     25.31 o

-7  11   3     2109.67     2071.35     51.56 o

-6  11   3        0.27       -1.89     13.76 o

-5  11   3     1735.69     1853.83     47.21 o

-4  11   3     1561.20     1603.78     43.14 o

-3  11   3      124.64      148.16     18.12 o

-2  11   3     1267.80     1314.66     37.84 o

-1  11   3      594.77      639.21     27.82 o

0  11   3      529.79      577.92     26.58 o

1  11   3     1590.26     1516.89     41.25 o

2  11   3       95.32       94.09     15.94 o

3  11   3      112.05       98.77     15.94 o

4  11   3     2727.95     2763.68     58.14 o

5  11   3       66.56       57.52     16.27 o

6  11   3       80.59       95.65     18.45 o

7  11   3       21.47       46.88     16.56 o

-7  12   3       62.04       59.08     17.50 o

-6  12   3      436.79      480.42     28.43 o

-5  12   3       44.05       50.33     17.50 o

-4  12   3      751.82      676.07     30.94 o

-3  12   3      394.59      456.96     26.25 o

-2  12   3      382.13      372.89     25.02 o

-1  12   3       44.98       51.27     14.70 o

0  12   3      165.65      145.36     17.83 o

1  12   3      735.53      834.25     32.21 o

2  12   3       53.46       77.53     15.94 o

3  12   3      348.61      325.36     24.07 o

4  12   3       92.51      115.33     18.45 o

5  12   3      896.43      969.58     38.75 o

6  12   3       51.55       58.75     16.56 o

-6  13   3       68.83      104.40     18.74 o

-5  13   3       86.33      127.53     18.74 o

-4  13   3        1.09       13.76     14.05 o

-3  13   3      227.38      199.10     21.24 o

-2  13   3      194.37      199.10     20.63 o

-1  13   3       45.28       44.38     15.94 o

0  13   3     2391.97     2441.12     55.34 o

1  13   3      316.64      329.43     24.37 o

2  13   3      668.99      701.09     33.12 o

3  13   3     1581.32     1597.21     47.50 o

4  13   3      216.93      196.30     22.51 o

5  13   3      951.10      911.74     39.40 o

-5  14   3     2175.58     2374.23     58.75 o

-4  14   3     1267.28     1282.45     43.43 o

-3  14   3      383.00      379.14     26.87 o

-2  14   3     1129.44     1204.63     41.87 o

-1  14   3       87.08       72.84     19.39 o

0  14   3       57.66       43.76     16.88 o

1  14   3        0.38       -4.68     15.00 o

2  14   3     2104.62     2055.73     54.69 o

3  14   3        3.73        5.95     15.32 o

-2  15   3      151.40      129.71     20.30 o

-1  15   3       27.13       42.20     16.88 o

0  15   3       17.84       11.26     16.56 o

1  15   3      505.19      468.22     30.65 o

-11   0   4     1505.58     1527.82     47.21 o

-10   0   4      881.13      786.42     33.44 o

-9   0   4     1131.80     1042.10     35.62 o

-8   0   4     1984.94     2139.50     45.94 o

-7   0   4     7174.44     7032.05     77.20 o

-6   0   4        1.14        3.45     12.49 o

-5   0   4      340.33      306.01     18.45 o

-4   0   4      123.81       80.94     13.14 o

-3   0   4     6637.74     6970.79     62.53 o

-2   0   4     1597.15     1691.30     30.94 o

-1   0   4    16504.22    15985.77     89.69 o

0   0   4    21380.26    21263.42    104.07 o

1   0   4     5029.37     4883.18     51.56 o

2   0   4      158.59      186.90     14.38 o

3   0   4      721.51      742.34     25.31 o

4   0   4    12748.73    12427.24     95.03 o

5   0   4     3972.98     3736.39     56.25 o

6   0   4       66.03       54.69     13.76 o

7   0   4      556.02      581.07     27.20 o

8   0   4      990.11      959.56     35.62 o

9   0   4      494.04      453.84     28.14 o

-11   1   4       42.58       98.45     18.45 o

-10   1   4      188.15      214.10     21.24 o

-9   1   4      105.75      105.02     16.27 o

-8   1   4     1821.77     1975.73     44.70 o

-7   1   4      103.46      104.72     15.62 o

-6   1   4      708.82      758.61     26.58 o

-5   1   4     1993.07     2086.38     39.07 o

-4   1   4      202.52      201.93     15.62 o

-3   1   4     2383.51     2232.65     36.57 o

-2   1   4     1170.55     1240.26     27.20 o

-1   1   4      621.86      582.93     19.39 o

0   1   4     2233.92     2030.42     33.44 o

1   1   4     4893.55     5165.44     53.45 o

2   1   4      569.02      607.62     21.57 o

3   1   4       85.25      105.02     13.44 o

4   1   4      894.44      885.81     27.49 o

5   1   4     1626.35     1646.89     38.45 o

6   1   4      704.02      711.69     27.82 o

7   1   4     2526.45     2520.82     52.18 o

8   1   4      844.73      805.16     32.50 o

9   1   4     2166.13     2109.51     54.40 o

-11   2   4       33.31       49.71     16.27 o

-10   2   4       37.95       35.62     15.00 o

-9   2   4      322.30      306.01     21.89 o

-8   2   4        0.74       15.00     12.49 o

-7   2   4     1726.93     1744.75     39.69 o

-6   2   4      522.76      522.29     23.46 o

-5   2   4      146.32      134.10     15.62 o

-4   2   4     1803.92     1864.76     35.95 o

-3   2   4      132.70      146.27     13.44 o

-2   2   4      616.57      647.02     20.95 o

-1   2   4     5829.76     5806.50     55.34 o

0   2   4     3359.89     3526.97     44.08 o

1   2   4       10.15        9.37     10.64 o

2   2   4      278.20      268.82     16.27 o

3   2   4      457.77      437.90     20.63 o

4   2   4        1.19        5.63     11.26 o

5   2   4     1868.19     1899.44     41.25 o

6   2   4       32.28       60.64     12.82 o

7   2   4     1110.15     1083.35     36.24 o

8   2   4      979.79      927.39     36.24 o

9   2   4       30.01       41.25     16.88 o

-11   3   4      413.84      453.54     28.43 o

-10   3   4      235.62      232.22     20.63 o

-9   3   4     4720.43     4534.98     70.63 o

-8   3   4        1.69       -9.37     12.49 o

-7   3   4       83.17      104.07     15.32 o

-6   3   4     1901.14     1811.64     39.07 o

-5   3   4        3.19        9.08     12.20 o

-4   3   4        0.33       10.64     11.26 o

-3   3   4     4682.91     4434.03     51.89 o

-2   3   4       65.18       52.83     12.20 o

-1   3   4     2357.90     2601.80     38.75 o

0   3   4    10340.87    10020.18     74.70 o

1   3   4      184.01      189.41     15.32 o

2   3   4     4629.68     4591.88     54.69 o

3   3   4     1790.01     1803.18     36.89 o

4   3   4      717.54      708.90     25.93 o

5   3   4       67.17       49.39     13.14 o

6   3   4        0.63       -0.33     11.26 o

7   3   4     2586.47     2579.29     54.69 o

8   3   4       57.53       67.21     16.27 o

9   3   4     1273.56     1318.08     43.76 o

-11   4   4      111.97      134.72     20.63 o

-10   4   4       26.87       28.43     16.27 o

-9   4   4      135.38      105.02     16.88 o

-8   4   4       39.90       69.69     15.00 o

-7   4   4      475.50      403.83     22.19 o

-6   4   4        3.85        6.25     11.26 o

-5   4   4      226.89      218.17     17.18 o

-4   4   4     1610.79     1575.93     34.68 o

-3   4   4     2240.75     2199.53     38.45 o

-2   4   4     1860.84     1873.81     34.68 o

-1   4   4     6241.55     6030.91     60.02 o

0   4   4     2169.41     2196.08     37.19 o

1   4   4      305.08      270.38     16.88 o

2   4   4      290.45      336.94     18.45 o

3   4   4      758.38      683.26     25.02 o

4   4   4     2340.95     2128.25     42.81 o

5   4   4     4987.04     4867.24     66.27 o

6   4   4      891.84      848.92     31.26 o

7   4   4        0.61        0.94     12.20 o

8   4   4     1664.98     1555.02     45.94 o

9   4   4      122.59       84.07     18.74 o

-11   5   4        0.89        9.99     14.70 o

-10   5   4     1825.88     1900.09     49.39 o

-9   5   4       54.20       49.06     15.00 o

-8   5   4     1234.61     1275.59     37.51 o

-7   5   4     1877.77     1846.32     42.52 o

-6   5   4       65.01       61.88     13.44 o

-5   5   4      177.42      133.16     15.62 o

-4   5   4      530.89      537.93     23.13 o

-3   5   4       72.07       54.69     13.44 o

-2   5   4      948.92      873.32     26.25 o

-1   5   4      373.91      364.14     18.74 o

0   5   4      351.67      379.76     19.06 o

1   5   4      141.64      165.33     15.32 o

2   5   4     2773.96     2860.60     46.26 o

3   5   4      772.93      786.71     26.87 o

4   5   4       88.76       83.77     13.76 o

5   5   4      242.18      257.86     19.39 o

6   5   4      485.69      472.90     25.64 o

7   5   4      184.46      175.35     19.39 o

8   5   4      112.65      110.64     18.45 o

9   5   4        0.42        4.68     14.38 o

-10   6   4      365.39      442.58     26.58 o

-9   6   4      328.48      269.73     22.51 o

-8   6   4      283.20      275.98     20.95 o

-7   6   4       70.12       91.26     15.00 o

-6   6   4      218.00      241.62     19.06 o

-5   6   4      691.11      611.07     25.02 o

-4   6   4     2554.18     2401.10     45.32 o

-3   6   4      405.23      438.84     21.24 o

-2   6   4     2004.42     1931.33     38.75 o

-1   6   4     6624.69     6378.82     67.21 o

0   6   4      297.77      367.27     19.06 o

1   6   4     1179.43     1035.53     30.00 o

2   6   4      735.86      689.21     25.31 o

3   6   4      437.74      456.02     21.89 o

4   6   4      113.85      135.96     15.62 o

5   6   4     1093.80     1144.94     35.62 o

6   6   4       50.83       36.57     14.38 o

7   6   4      826.25      824.55     33.77 o

8   6   4     2100.63     2157.95     55.34 o

-10   7   4       16.35       39.07     15.62 o

-9   7   4     2946.78     3142.21     62.20 o

-8   7   4       60.29       57.52     14.70 o

-7   7   4       90.17       77.53     15.32 o

-6   7   4     2972.39     2817.75     52.83 o

-5   7   4     1448.08     1483.44     37.51 o

-4   7   4      853.20      832.03     28.76 o

-3   7   4      341.70      275.36     19.06 o

-2   7   4     1421.29     1400.61     34.68 o

-1   7   4      360.05      424.46     20.63 o

0   7   4     2406.58     2099.49     42.20 o

1   7   4      955.22      990.50     30.00 o

2   7   4      403.01      385.39     21.24 o

3   7   4     2591.42     2483.64     48.44 o

4   7   4      624.63      565.42     26.58 o

5   7   4      134.25      151.60     17.18 o

6   7   4       24.70       30.65     14.05 o

7   7   4       26.80       19.68     15.00 o

8   7   4       63.39       63.76     17.18 o

-9   8   4      366.14      363.82     25.02 o

-8   8   4     2003.01     1879.44     48.44 o

-7   8   4      473.60      601.05     28.14 o

-6   8   4       89.58       81.59     15.94 o

-5   8   4        6.73        5.95     12.82 o

-4   8   4     1089.40     1122.72     34.39 o

-3   8   4      287.96      238.50     19.06 o

-2   8   4     4005.75     3982.37     59.37 o

-1   8   4     1379.51     1357.47     35.01 o

0   8   4       78.41      103.46     14.70 o

1   8   4     2920.14     3053.75     52.51 o

2   8   4      585.40      512.59     24.69 o

3   8   4     2995.61     3006.87     54.69 o

4   8   4      148.78      162.21     17.50 o

5   8   4     1559.13     1513.44     42.52 o

6   8   4     2151.81     2073.56     51.89 o

7   8   4       94.45       88.78     17.83 o

8   8   4      358.12      392.28     27.20 o

-9   9   4      545.20      539.79     30.65 o

-8   9   4      175.99      178.15     20.63 o

-7   9   4     1799.51     1762.87     46.59 o

-6   9   4       68.14       98.15     16.56 o

-5   9   4     1096.80     1068.35     35.33 o

-4   9   4       16.29       13.14     12.49 o

-3   9   4      295.00      273.51     20.95 o

-2   9   4     6404.91     6322.54     77.20 o

-1   9   4      250.85      193.80     17.83 o

0   9   4     1522.50     1452.80     38.13 o

1   9   4     3255.97     3080.95     55.63 o

2   9   4      640.62      656.39     28.43 o

3   9   4      130.30      163.77     17.83 o

4   9   4       10.49        1.56     13.14 o

5   9   4      124.36      111.59     18.74 o

6   9   4     1663.95     1721.91     49.06 o

7   9   4      285.21      270.06     25.02 o

-8  10   4     1029.48     1223.99     42.20 o

-7  10   4     1334.10     1254.31     42.20 o

-6  10   4      412.21      379.14     25.64 o

-5  10   4      125.71      108.47     17.18 o

-4  10   4      385.79      416.98     24.37 o

-3  10   4      832.09      834.25     31.56 o

-2  10   4      328.25      350.06     22.19 o

-1  10   4       40.63       36.24     14.70 o

0  10   4      312.07      336.00     22.81 o

1  10   4     1572.90     1505.92     41.25 o

2  10   4      646.62      630.46     29.70 o

3  10   4      470.17      480.42     26.25 o

4  10   4        8.20       20.01     12.82 o

5  10   4      223.98      221.91     20.63 o

6  10   4       35.89       44.70     15.62 o

-7  11   4     1414.57     1397.16     45.32 o

-6  11   4        0.07        1.89     14.70 o

-5  11   4      256.05      281.61     22.81 o

-4  11   4        3.80        3.12     14.05 o

-3  11   4       46.03       36.57     13.76 o

-2  11   4       35.53       34.68     14.38 o

-1  11   4     1085.61     1066.14     36.24 o

0  11   4       46.40       37.84     14.38 o

1  11   4      391.07      325.36     23.46 o

2  11   4     2274.26     2308.90     53.13 o

3  11   4       81.92       87.51     17.83 o

4  11   4        0.92        9.08     13.44 o

5  11   4      794.03      747.97     35.01 o

6  11   4      148.04      141.29     20.63 o

-6  12   4        7.05       19.68     15.62 o

-5  12   4       42.99       47.21     17.18 o

-4  12   4       47.00       39.07     17.18 o

-3  12   4     1307.22     1380.61     43.14 o

-2  12   4     1308.23     1250.90     40.96 o

-1  12   4        1.42      -10.93     13.76 o

0  12   4      847.74      739.54     33.77 o

1  12   4     1015.69      962.69     37.51 o

2  12   4      695.16      632.02     30.94 o

3  12   4        6.34       27.20     14.70 o

4  12   4      803.60      844.85     36.89 o

5  12   4      238.07      198.78     21.89 o

-5  13   4        1.32       -4.07     15.62 o

-4  13   4       89.51      110.32     18.45 o

-3  13   4      180.29      129.71     20.63 o

-2  13   4      341.61      352.89     25.93 o

-1  13   4      291.47      321.33     24.07 o

0  13   4      350.97      311.63     25.31 o

1  13   4      171.25      172.52     20.95 o

2  13   4      391.81      322.24     25.93 o

3  13   4       83.03       89.69     19.06 o

-3  14   4      130.36      106.58     19.39 o

-2  14   4        1.09        1.56     16.56 o

-1  14   4      347.25      336.00     26.58 o

0  14   4       24.22       28.43     17.83 o

1  14   4       20.02       30.94     17.50 o

-11   1   5       22.43        0.00     15.94 o

-10   1   5       67.96       54.07     17.50 o

-9   1   5       13.19       30.00     15.32 o

-8   1   5       58.48       40.02     14.70 o

-7   1   5       91.54       95.97     15.62 o

-6   1   5     7194.99     6897.99     79.38 o

-5   1   5      164.58      172.23     16.27 o

-4   1   5     2697.14     2428.63     44.38 o

-3   1   5     4549.08     4615.01     58.14 o

-2   1   5      723.37      782.36     25.31 o

-1   1   5      507.74      525.73     21.57 o

0   1   5     2671.56     2573.04     43.14 o

1   1   5      501.82      479.15     20.95 o

2   1   5     3514.64     3349.77     51.56 o

3   1   5      795.41      699.53     25.93 o

4   1   5      118.28       99.71     14.70 o

5   1   5        1.59       -4.68     11.55 o

6   1   5      311.25      301.94     21.57 o

7   1   5      158.29      127.20     18.45 o

8   1   5       48.04       45.32     15.94 o

-11   2   5     1184.76     1237.13     44.38 o

-10   2   5       19.06       34.68     15.00 o

-9   2   5      104.76      121.90     18.74 o

-8   2   5       18.45       23.13     14.38 o

-7   2   5       21.13       16.27     12.82 o

-6   2   5     3278.98     3251.29     55.01 o

-5   2   5       63.18       54.07     13.44 o

-4   2   5       30.74       48.77     12.82 o

-3   2   5        8.69       17.83     11.87 o

-2   2   5       28.86       51.56     12.49 o

-1   2   5      778.23      793.90     25.93 o

0   2   5       16.76       28.43     11.87 o

1   2   5      941.11      947.40     28.76 o

2   2   5    11084.52    11036.03     92.52 o

3   2   5     1196.61     1143.99     32.83 o

4   2   5      704.05      820.48     28.76 o

5   2   5      279.92      315.70     21.24 o

6   2   5     3664.85     3581.99     64.38 o

7   2   5      218.99      186.28     19.68 o

8   2   5     2284.02     2212.96     55.63 o

-10   3   5     1025.09      864.57     36.57 o

-9   3   5      112.55      187.85     20.30 o

-8   3   5      242.20      247.54     21.57 o

-7   3   5       44.02       49.39     14.70 o

-6   3   5     3492.81     3482.27     57.52 o

-5   3   5      625.91      552.31     24.69 o

-4   3   5      339.22      292.86     18.74 o

-3   3   5     1489.18     1528.44     35.01 o

-2   3   5     1349.81     1447.17     34.06 o

-1   3   5       28.40       39.07     11.87 o

0   3   5      537.02      557.94     23.13 o

1   3   5     5619.96     5545.20     65.33 o

2   3   5        7.10       29.08     11.55 o

3   3   5      441.86      399.44     22.19 o

4   3   5     1996.42     1990.73     44.70 o

5   3   5      838.80      880.80     31.88 o

6   3   5       16.97       21.24     12.82 o

7   3   5       46.77       50.62     16.27 o

8   3   5      505.49      432.27     30.32 o

-10   4   5       14.03       11.26     15.94 o

-9   4   5        9.09        6.86     14.70 o

-8   4   5      838.47      948.31     34.39 o

-7   4   5     2865.75     2760.89     53.78 o

-6   4   5      489.68      464.15     24.07 o

-5   4   5     3255.84     3331.00     55.34 o

-4   4   5     6883.43     7078.64     76.26 o

-3   4   5      362.58      368.83     19.68 o

-2   4   5      280.97      302.56     18.45 o

-1   4   5     2914.39     3006.87     48.15 o

0   4   5       40.11       40.96     12.20 o

1   4   5       54.55       48.77     12.20 o

2   4   5       63.42       44.70     12.82 o

3   4   5        4.50       23.46     11.55 o

4   4   5       31.19       55.96     14.05 o

5   4   5      345.10      289.12     21.89 o

6   4   5       14.53       38.75     13.76 o

7   4   5      217.67      202.55     21.89 o

8   4   5      247.12      248.16     23.46 o

-10   5   5       15.40       62.53     16.88 o

-9   5   5       40.44       30.00     16.27 o

-8   5   5      294.70      237.56     21.89 o

-7   5   5     1454.35     1490.63     41.58 o

-6   5   5      105.98       98.45     16.27 o

-5   5   5      106.37       89.08     15.32 o

-4   5   5     2855.23     2628.35     48.44 o

-3   5   5        3.65       26.87     11.26 o

-2   5   5      444.88      466.98     22.51 o

-1   5   5      397.61      400.09     20.30 o

0   5   5     2409.97     2339.55     44.38 o

1   5   5     1388.06     1541.25     37.19 o

2   5   5     3361.29     3278.49     54.40 o

3   5   5     2372.60     2246.70     47.21 o

4   5   5     3101.70     3046.27     56.90 o

5   5   5     2777.08     2788.38     56.25 o

6   5   5      159.25      168.46     19.06 o

7   5   5       18.14       31.88     15.94 o

8   5   5      283.40      287.56     25.02 o

-10   6   5        3.84      -15.32     15.32 o

-9   6   5      217.11      161.30     20.95 o

-8   6   5      590.82      703.27     31.26 o

-7   6   5       20.98       18.12     14.38 o

-6   6   5       39.87       24.07     13.76 o

-5   6   5      570.04      562.30     26.58 o

-4   6   5      831.64      885.19     30.00 o

-3   6   5      531.86      476.67     23.75 o

-2   6   5       42.91       38.13     13.14 o

-1   6   5      121.49      106.29     14.38 o

0   6   5     2627.58     2674.93     49.06 o

1   6   5       65.78       79.71     13.44 o

2   6   5        9.52       -1.24     13.14 o

3   6   5     3538.42     3577.30     60.32 o

4   6   5       84.22       60.02     15.62 o

5   6   5      209.70      214.72     20.30 o

6   6   5       24.79       26.87     15.00 o

7   6   5     1910.62     1934.45     52.83 o

-9   7   5      501.76      460.08     28.43 o

-8   7   5      803.67      904.87     36.24 o

-7   7   5      389.93      432.27     25.02 o

-6   7   5      872.33      862.68     32.21 o

-5   7   5     4267.47     4244.62     67.21 o

-4   7   5      544.86      562.30     26.25 o

-3   7   5     1766.35     1856.63     42.81 o

-2   7   5      332.17      346.93     20.63 o

-1   7   5        6.54       -1.24     12.20 o

0   7   5      680.89      675.78     27.82 o

1   7   5      480.62      430.41     23.46 o

2   7   5       25.16       15.62     13.14 o

3   7   5       23.11       12.20     13.76 o

4   7   5      674.82      616.70     28.76 o

5   7   5      241.54      208.80     20.95 o

6   7   5      339.63      392.28     26.58 o

7   7   5       30.34       35.95     16.56 o

-9   8   5        4.90        0.62     14.70 o

-8   8   5        1.83       -7.81     14.38 o

-7   8   5      472.78      472.28     26.87 o

-6   8   5       55.82      100.01     16.56 o

-5   8   5       72.60       62.53     15.94 o

-4   8   5      585.13      618.55     28.14 o

-3   8   5     1816.46     1736.29     43.14 o

-2   8   5        4.70       -0.94     12.49 o

-1   8   5      669.11      685.44     27.82 o

0   8   5      385.90      378.52     23.13 o

1   8   5       45.08       30.65     12.82 o

2   8   5      604.72      594.51     27.49 o

3   8   5     1527.43     1487.80     42.52 o

4   8   5        2.99       11.55     14.05 o

5   8   5      177.13      212.54     21.24 o

6   8   5      182.13      181.27     20.63 o

-8   9   5      113.69      105.96     19.68 o

-7   9   5      411.02      391.96     26.87 o

-6   9   5       72.62       81.27     17.18 o

-5   9   5      351.99      361.02     24.07 o

-4   9   5      131.27      127.20     17.83 o

-3   9   5      176.10      227.86     19.68 o

-2   9   5      137.97      137.22     17.50 o

-1   9   5      166.45      189.11     18.45 o

0   9   5      448.98      437.90     24.37 o

1   9   5      191.26      192.24     19.39 o

2   9   5        1.92       -2.51     13.44 o

3   9   5      769.96      782.65     32.83 o

4   9   5      175.71      136.90     19.06 o

5   9   5      542.23      540.44     30.32 o

6   9   5       17.86        2.51     15.94 o

-7  10   5      766.28      751.42     35.62 o

-6  10   5      324.24      264.75     24.37 o

-5  10   5       12.89       -0.94     15.00 o

-4  10   5      397.00      428.85     26.58 o

-3  10   5       68.59       80.94     16.56 o

-2  10   5       27.59       43.14     15.00 o

-1  10   5        6.57        0.33     13.76 o

0  10   5     1765.72     1739.41     47.21 o

1  10   5      155.33      138.17     19.06 o

2  10   5       66.11       48.44     16.56 o

3  10   5     2580.69     2563.64     58.14 o

4  10   5      232.08      235.99     22.51 o

5  10   5      726.48      714.85     35.01 o

-6  11   5      344.39      339.12     26.58 o

-5  11   5     2351.09     2364.24     57.52 o

-4  11   5      167.37      181.92     21.57 o

-3  11   5      399.19      409.14     27.49 o

-2  11   5      784.69      793.90     34.39 o

-1  11   5      606.38      599.19     30.94 o

0  11   5      842.51      887.05     35.33 o

1  11   5      629.96      533.25     30.32 o

2  11   5      177.07      204.73     21.24 o

3  11   5       49.47       46.59     16.88 o

4  11   5       12.93       10.93     16.27 o

-5  12   5      549.94      551.66     30.94 o

-4  12   5     1143.29     1091.48     41.87 o

-3  12   5       65.36       40.96     16.88 o

-2  12   5       50.39       28.76     16.56 o

-1  12   5     2378.72     2296.74     56.90 o

0  12   5       31.89       35.01     15.32 o

1  12   5      261.08      276.92     24.07 o

2  12   5      129.17      144.09     20.63 o

3  12   5      943.08      988.94     40.63 o

-3  13   5      144.93      123.79     20.63 o

-2  13   5      163.88      170.34     20.95 o

-1  13   5       82.81       90.02     19.06 o

0  13   5       68.23       93.47     18.74 o

-10   0   6      226.93      188.79     22.81 o

-9   0   6     9759.72     9587.59    110.97 o

-8   0   6       20.28       21.24     14.70 o

-7   0   6       83.01       94.09     16.88 o

-6   0   6     1479.44     1295.27     38.45 o

-5   0   6      727.39      825.17     31.26 o

-4   0   6      875.95      911.45     30.94 o

-3   0   6     3611.23     3582.31     56.90 o

-2   0   6        0.28        4.68     12.20 o

-1   0   6       42.55       56.90     14.05 o

0   0   6     4466.28     4354.97     62.20 o

1   0   6      727.99      617.93     25.93 o

2   0   6     1484.62     1490.63     39.40 o

3   0   6     1914.46     1975.08     45.94 o

4   0   6      848.25      882.36     32.83 o

5   0   6     1725.23     1622.20     44.99 o

6   0   6       47.55       68.45     16.88 o

7   0   6      460.52      455.72     29.08 o

-10   1   6       61.83      114.71     19.68 o

-9   1   6        6.21       16.88     15.94 o

-8   1   6        1.80       19.68     14.70 o

-7   1   6       36.55       43.43     15.32 o

-6   1   6     1031.47      903.31     33.12 o

-5   1   6        4.82       11.26     13.14 o

-4   1   6     3453.38     3509.80     58.14 o

-3   1   6     1928.83     1962.26     43.43 o

-2   1   6      294.40      284.44     19.68 o

-1   1   6     6158.22     5933.71     72.19 o

0   1   6     1202.18     1241.20     35.01 o

1   1   6      114.82      159.70     16.56 o

2   1   6       22.92       20.30     12.49 o

3   1   6     1785.87     1789.12     43.43 o

4   1   6       21.76       36.89     13.14 o

5   1   6     1470.35     1482.50     43.76 o

6   1   6      184.81      214.72     20.63 o

7   1   6      207.65      192.53     22.19 o

-10   2   6        7.93        9.69     16.27 o

-9   2   6       19.42       20.01     15.94 o

-8   2   6      176.19      167.22     20.01 o

-7   2   6       10.33        8.43     14.05 o

-6   2   6       66.79       45.64     14.05 o

-5   2   6     1070.67     1054.27     35.33 o

-4   2   6      258.71      276.30     19.39 o

-3   2   6     2546.08     2627.11     49.06 o

-2   2   6     4479.63     4521.54     63.44 o

-1   2   6     1000.66      992.06     31.26 o

0   2   6      587.22      564.19     25.02 o

1   2   6       87.82      103.78     15.94 o

2   2   6      475.10      555.11     25.31 o

3   2   6        0.07        5.95     12.20 o

4   2   6        4.74       -7.19     11.87 o

5   2   6       38.20       46.26     15.94 o

6   2   6      972.10      979.57     38.13 o

7   2   6      219.38      221.91     22.81 o

-9   3   6       54.54       84.07     19.68 o

-8   3   6     1710.42     1860.37     49.71 o

-7   3   6      934.94      815.18     34.39 o

-6   3   6      243.45      226.63     20.01 o

-5   3   6      117.68      111.59     16.27 o

-4   3   6      995.03      897.36     30.94 o

-3   3   6       53.28       49.06     13.76 o

-2   3   6        2.85        5.95     12.49 o

-1   3   6     6050.98     5742.44     71.57 o

0   3   6       56.83       53.45     13.44 o

1   3   6     2175.31     2067.93     45.64 o

2   3   6      565.37      560.74     25.93 o

3   3   6       31.25       31.88     13.44 o

4   3   6     1665.65     1631.27     44.08 o

5   3   6     1832.68     1777.87     48.15 o

6   3   6      295.50      317.88     25.31 o

7   3   6      367.36      440.40     29.08 o

-9   4   6     2252.57     2372.05     57.52 o

-8   4   6       56.72       25.93     16.56 o

-7   4   6       96.27       89.08     16.88 o

-6   4   6       95.99       73.75     16.56 o

-5   4   6       16.12       18.74     12.82 o

-4   4   6     1892.63     1858.52     43.76 o

-3   4   6     2031.25     2033.54     44.70 o

-2   4   6       32.83       37.84     12.49 o

-1   4   6      297.94      286.00     20.01 o

0   4   6     1818.78     1732.22     41.58 o

1   4   6      351.79      346.02     21.89 o

2   4   6      159.53      180.36     17.50 o

3   4   6        7.76        7.81     13.14 o

4   4   6      100.21      114.71     18.12 o

5   4   6      124.20      133.45     19.68 o

6   4   6       21.97       -2.18     15.62 o

-9   5   6      183.48      133.16     20.01 o

-8   5   6      196.25      155.02     20.01 o

-7   5   6        3.75        5.63     14.70 o

-6   5   6       97.77      133.78     17.83 o

-5   5   6        9.55       -9.69     13.14 o

-4   5   6       32.20       48.15     14.05 o

-3   5   6      657.87      589.50     26.87 o

-2   5   6     1896.82     1919.16     44.08 o

-1   5   6       24.52       33.77     13.14 o

0   5   6        1.34        0.62     12.82 o

1   5   6      898.38      879.56     31.88 o

2   5   6      833.23      863.30     32.83 o

3   5   6     1382.40     1405.59     41.58 o

4   5   6      826.23      734.21     32.21 o

5   5   6      217.33      209.74     21.89 o

6   5   6     1560.82     1508.43     47.82 o

-8   6   6        6.61        5.01     16.27 o

-7   6   6       45.96       71.28     17.18 o

-6   6   6       43.84       43.76     15.94 o

-5   6   6     1472.16     1423.09     40.63 o

-4   6   6        4.43        2.18     12.49 o

-3   6   6     1810.89     1736.00     43.76 o

-2   6   6     4080.65     4051.15     64.09 o

-1   6   6      816.17      774.55     30.32 o

0   6   6     2369.83     2282.65     49.39 o

1   6   6      575.61      600.14     27.49 o

2   6   6      387.43      402.60     24.37 o

3   6   6      200.97      178.48     19.68 o

4   6   6      193.70      177.86     20.63 o

5   6   6       34.86        5.95     16.56 o

6   6   6     2084.48     1953.22     55.01 o

-8   7   6      452.58      601.37     32.21 o

-7   7   6     1104.72     1096.17     39.40 o

-6   7   6      521.15      545.12     29.70 o

-5   7   6      550.92      546.98     27.82 o

-4   7   6      104.45       95.65     15.94 o

-3   7   6      861.90      908.32     33.12 o

-2   7   6       17.56       36.57     14.05 o

-1   7   6     1081.31      984.26     34.39 o

0   7   6      355.87      424.78     25.64 o

1   7   6      509.98      542.62     27.20 o

2   7   6       61.30       53.45     15.62 o

3   7   6       39.34       35.01     14.70 o

4   7   6     1504.63     1538.75     46.59 o

5   7   6      567.43      535.72     31.56 o

-7   8   6      193.91      140.97     20.63 o

-6   8   6      329.79      403.83     27.49 o

-5   8   6       22.17       18.45     14.70 o

-4   8   6      297.78      414.47     25.31 o

-3   8   6      190.03      186.28     20.30 o

-2   8   6       84.68       59.70     15.94 o

-1   8   6     2661.73     2681.80     56.25 o

0   8   6      292.61      338.51     23.13 o

1   8   6       19.58       34.39     14.70 o

2   8   6     1223.03     1256.52     40.96 o

3   8   6      250.53      247.54     22.81 o

4   8   6       43.04       46.26     17.50 o

5   8   6     1870.23     1893.81     53.78 o

-7   9   6       82.77       82.83     18.45 o

-6   9   6       97.05      130.33     20.30 o

-5   9   6      382.76      361.96     26.87 o

-4   9   6     1126.89      991.77     38.13 o

-3   9   6     3399.45     3469.78     66.56 o

-2   9   6     1488.04     1545.94     45.32 o

-1   9   6     1120.13     1054.92     38.13 o

0   9   6     2809.79     2800.58     59.37 o

1   9   6       66.10       70.95     17.83 o

2   9   6      725.47      685.15     33.12 o

3   9   6      481.13      491.35     29.08 o

4   9   6     1828.22     1912.59     54.07 o

-6  10   6      367.53      366.65     27.49 o

-5  10   6       54.94       71.57     18.74 o

-4  10   6      582.01      578.86     31.88 o

-3  10   6       50.62       58.46     18.12 o

-2  10   6        4.68       12.82     15.62 o

-1  10   6      359.98      436.33     28.14 o

0  10   6      888.50      767.36     35.33 o

1  10   6      147.65      111.91     19.68 o

2  10   6       38.71       61.26     17.83 o

3  10   6      109.18      130.03     19.39 o

-4  11   6      217.18      195.65     23.75 o

-3  11   6       86.24       71.90     18.45 o

-2  11   6      484.70      452.60     28.14 o

-1  11   6        1.13      -15.62     15.62 o

0  11   6       35.84       48.15     17.83 o

1  11   6      272.19      266.32     25.64 o

-8   1   7      129.72      213.48     23.46 o

-7   1   7      440.03      310.37     25.02 o

-6   1   7     2493.64     2575.84     57.19 o

-5   1   7      165.25      100.01     17.50 o

-4   1   7      860.59      824.23     32.50 o

-3   1   7     1650.70     1726.92     44.08 o

-2   1   7      448.39      424.13     24.37 o

-1   1   7      114.08      137.84     16.88 o

0   1   7       16.95       26.58     13.14 o

1   1   7     2241.37     2079.81     49.71 o

2   1   7       89.55       93.47     17.50 o

3   1   7      865.12      807.99     34.39 o

4   1   7      291.75      305.68     23.75 o

5   1   7        1.74       -4.68     14.38 o

-8   2   7       78.20       56.57     17.83 o

-7   2   7     4023.73     3904.88     71.90 o

-6   2   7      196.65      188.17     21.89 o

-5   2   7        0.82        8.43     13.76 o

-4   2   7     2074.55     1839.13     46.59 o

-3   2   7        5.41       13.76     14.38 o

-2   2   7      407.03      444.47     24.69 o

-1   2   7      919.27      961.45     34.39 o

0   2   7      658.94      708.57     30.00 o

1   2   7      151.67      171.29     18.12 o

2   2   7     7421.10     7154.28     91.58 o

3   2   7      106.12      105.34     18.74 o

4   2   7      752.16      733.59     34.06 o

5   2   7     2299.75     2280.14     58.14 o

-8   3   7     1074.16     1162.73     42.81 o

-7   3   7       65.08       63.76     18.12 o

-6   3   7       40.73       61.26     17.18 o

-5   3   7      386.50      521.05     27.82 o

-4   3   7      417.42      414.15     25.64 o

-3   3   7       24.04       31.88     14.70 o

-2   3   7      202.66      205.35     20.01 o

-1   3   7      721.14      773.90     30.94 o

0   3   7     1127.76     1175.26     38.13 o

1   3   7      206.40      190.35     20.01 o

2   3   7       56.82       41.87     15.32 o

3   3   7      695.27      758.61     34.06 o

4   3   7      102.78      109.08     19.06 o

5   3   7      283.76      289.12     25.64 o

-8   4   7      385.52      404.78     29.08 o

-7   4   7       38.55       41.25     16.88 o

-6   4   7      143.05      142.85     20.63 o

-5   4   7     3095.21     3143.15     62.82 o

-4   4   7      171.63      172.23     19.39 o

-3   4   7      613.18      621.67     29.38 o

-2   4   7     2254.65     2215.47     51.27 o

-1   4   7      120.24      149.39     18.45 o

0   4   7     2637.96     2581.79     55.96 o

1   4   7       21.13       30.65     15.94 o

2   4   7      123.56      127.20     17.83 o

3   4   7      137.22      140.35     19.39 o

4   4   7        0.71       10.31     14.38 o

-7   5   7       99.54      135.96     20.95 o

-6   5   7     1694.96     1898.21     50.62 o

-5   5   7      721.71      690.45     32.50 o

-4   5   7       30.87       51.56     15.94 o

-3   5   7      471.55      453.22     26.25 o

-2   5   7       82.16       88.46     17.18 o

-1   5   7      806.66      823.93     34.06 o

0   5   7      712.67      764.23     32.50 o

1   5   7     1058.80      973.00     36.57 o

2   5   7      387.20      403.83     26.58 o

3   5   7     3911.57     3862.68     72.52 o

4   5   7     1806.92     1731.28     51.27 o

-7   6   7       15.53       11.87     15.94 o

-6   6   7     1720.88     1762.25     49.71 o

-5   6   7       34.69        6.57     15.62 o

-4   6   7      352.31      275.36     22.81 o

-3   6   7      162.71      150.34     19.06 o

-2   6   7      778.12      908.62     35.62 o

-1   6   7      897.03      946.13     35.62 o

0   6   7      277.79      286.62     24.07 o

1   6   7     2530.16     2659.29     58.75 o

2   6   7       73.96       69.69     17.83 o

3   6   7       82.20       85.63     18.45 o

-6   7   7      228.17      152.22     21.89 o

-5   7   7      156.94      175.97     21.24 o

-4   7   7      394.27      445.08     27.49 o

-3   7   7     2231.67     2027.30     52.51 o

-2   7   7      293.38      328.81     24.07 o

-1   7   7      304.22      297.55     24.07 o

0   7   7        0.49       18.45     15.00 o

1   7   7       52.17       57.19     17.50 o

2   7   7      604.44      608.89     31.88 o

3   7   7      845.85      829.56     36.89 o

-5   8   7     1087.75     1117.74     41.87 o

-4   8   7      879.12      817.36     36.57 o

-3   8   7      166.23      194.09     21.24 o

-2   8   7       82.05       88.78     17.83 o

-1   8   7        1.56        9.69     14.70 o

0   8   7      125.40      141.29     20.01 o

1   8   7      128.63      185.05     20.30 o

2   8   7      666.48      672.33     33.44 o

-4   9   7      134.82      159.41     21.57 o

-3   9   7      130.77      122.23     20.01 o

-2   9   7       32.96       51.89     17.83 o

-1   9   7      118.92      103.46     19.06 o

0   9   7        1.00      -10.64     15.32 o

-6   0   8      618.44      644.81     33.77 o

-5   0   8      204.74      213.81     21.89 o

-4   0   8      420.63      351.00     25.64 o

-3   0   8        4.54        6.57     14.05 o

-2   0   8       33.14       21.57     15.32 o

-1   0   8      435.59      334.44     26.25 o

0   0   8       11.07       19.68     15.62 o

1   0   8      904.65      976.77     39.40 o

2   0   8      442.84      471.96     28.76 o

-6   1   8     1371.83     1573.14     48.77 o

-5   1   8      193.91      181.27     21.24 o

-4   1   8      977.70     1035.20     40.31 o

-3   1   8      520.01      684.53     32.21 o

-2   1   8      461.05      443.23     27.82 o

-1   1   8     1103.09     1164.62     41.58 o

0   1   8        1.90        6.25     15.32 o

1   1   8     1273.65     1333.07     44.38 o

2   1   8      399.14      440.07     28.43 o

-6   2   8       12.29       25.64     16.88 o

-5   2   8        2.67       13.14     15.62 o

-4   2   8     1074.62     1060.55     40.02 o

-3   2   8     1174.84     1308.38     43.14 o

-2   2   8      312.29      265.05     23.75 o

-1   2   8      181.49      191.59     20.63 o

0   2   8     1201.21     1248.39     42.52 o

1   2   8      170.24      194.09     21.89 o

2   2   8      224.81      223.79     23.13 o

-5   3   8       40.39       91.26     18.74 o

-4   3   8      282.36      385.09     26.58 o

-3   3   8      327.40      414.76     26.87 o

-2   3   8      416.96      378.82     26.58 o

-1   3   8      243.58      241.30     22.19 o

0   3   8      398.82      431.32     27.20 o

1   3   8       76.78      102.51     18.12 o

2   3   8        3.14       16.27     16.27 o

-5   4   8        9.88       12.82     15.94 o

-4   4   8      505.79      426.35     29.08 o

-3   4   8      229.79      190.97     20.30 o

-2   4   8      313.28      230.04     22.81 o

-1   4   8      597.10      505.73     30.00 o

0   4   8      318.87      393.85     27.49 o

1   4   8       13.33       15.94     15.94 o

-4   5   8      376.50      411.64     27.82 o

-3   5   8      476.77      521.05     30.32 o

-2   5   8      783.45      816.42     36.57 o

-1   5   8      125.71      127.20     19.06 o

0   5   8      166.73      167.55     20.63 o

-3   6   8     1717.72     1708.80     51.27 o

-2   6   8       46.40       50.62     16.88 o

-1   6   8      661.20      745.14     35.01 o