# SUPPORTING INFORMATION (SI)

Synthesis and stability of some members of the pharmacosiderite group, AFe4(OH)4(AsO4)3·nH2O (A = K, Na, 0.5Ba, 0.5Sr)

Juraj Majzlan1,*, Patrick Haase1, Jakub Plášil2, Edgar Dachs3

1Institutes of Geosciences, Friedrich-Schiller University, Burgweg 11, D-07749 Jena, Germany

2Institute of Physics ASCR, v.v.i., Na Slovance 1999/2, 18221 Praha 8, Czech Republic

3Department of Chemistry and Physics of Materials, Division Mineralogy, University of Salzburg, Jakob-Haringerstrasse 2A, A-5020 Salzburg, Austria

*corresponding author:	email: Juraj.Majzlan@uni-jena.de

telephone: +49-3641-948700

fax: +49-3641-948602

## Number of figures: 0

## Number of tables: 5

Number of pages in SI (including the cover page): 6

Table S1. Electron microprobe analyses of the pharmacosiderite samples. All data in weight %. Note that because of extreme sensitivity of these samples to the electron beam and the dependence of the analytical results on the sample current, these analyses can be regarded only as semiquantitative.

K-pharmacosiderite

Na2O	As2O5	SrO	BaO	K2O	SO3	Fe2O3	Total

0.79	42.38	0.00	0.00	5.00	2.03	38.21	88.40

1.24	38.96	0.80	0.00	4.41	1.91	39.09	86.42

0.99	42.28	0.38	0.11	4.48	1.68	38.28	88.21

1.13	42.25	0.00	0.00	5.34	1.76	38.19	88.68

0.65	42.80	0.16	0.00	5.49	1.78	38.65	89.53

0.08	41.89	0.00	0.05	8.16	1.74	36.62	88.53

0.34	40.86	0.15	0.00	6.99	1.53	36.29	86.16

0.28	41.59	0.00	0.07	7.27	1.65	38.15	89.01

0.69	41.89	0.44	0.03	5.94	1.91	37.57	88.46

0.75	40.07	0.00	0.28	5.73	1.55	37.46	85.85

0.55	42.29	0.43	0.19	7.22	1.88	37.80	90.37

0.69	41.37	0.00	0.01	6.39	2.08	37.23	87.76

0.07	42.26	0.00	0.00	8.13	1.53	38.16	90.14

0.72	41.84	0.64	0.00	4.41	1.85	36.81	86.27

Ba-pharmacosiderite

Na2O	As2O5	SrO	BaO	K2O	SO3	Fe2O3	Total

0.04	38.93	0.04	11.64	0.00	1.73	35.89	88.27

0.04	39.62	0.10	10.18	0.00	1.87	34.18	85.99

0.06	38.71	0.18	10.35	0.01	2.02	33.67	84.99

0.04	37.16	0.00	12.64	0.01	1.81	36.36	88.03

0.05	37.19	0.00	12.32	0.02	1.95	34.75	86.27

0.07	38.60	0.12	10.83	0.00	1.79	34.27	85.68

0.05	37.60	0.10	10.63	0.02	1.84	34.09	84.33

0.00	37.76	0.21	11.75	0.00	1.84	35.40	86.95

0.00	38.00	0.26	11.16	0.00	1.87	35.30	86.60

0.03	37.87	0.00	9.85	0.01	1.75	35.37	84.88

Sr-pharmacosiderite

Na2O	As2O5	SrO	BaO	K2O	SO3	Fe2O3	Total

0.03	38.90	9.78	0.07	0.00	1.20	30.82	80.80

0.00	40.12	9.93	0.17	0.02	1.39	30.57	82.19

0.01	39.40	10.13	0.08	0.05	1.34	29.50	80.51

0.00	39.88	9.73	0.10	0.02	1.45	29.70	80.88

0.00	39.49	9.68	0.28	0.01	1.34	28.99	79.79

0.00	41.65	8.23	0.40	0.01	1.44	30.91	82.64

0.00	41.89	9.30	0.34	0.00	1.38	29.92	82.83

0.01	41.34	8.10	0.30	0.02	1.32	28.95	80.04

Na-pharmacosiderite

Na2O	As2O5	SrO	BaO	K2O	SO3	Fe2O3	Total

7.46	38.65	0.00	0.00	0.81	0.24	29.27	76.42

Table S2. Measured heat capacity for K-pharmacosiderite (composition K1.086Fe4[(AsO4)0.953(SO4)0.047]3 (OH)3.772O0.228·4.432H2O), molecular mass 824.2076 g·mol–1. Temperature (T) in K, heat capacity (Cp) in J·mol–1·K–1.

T	Cp	T	Cp	T	Cp

2.2204	4.4038	11.550	24.868	63.706	178.31

2.3263	4.8008	12.146	25.468	66.992	189.77

2.4368	5.2217	12.774	26.070	70.453	201.62

2.5538	5.6727	13.432	26.688	74.075	215.14

2.6775	6.1630	14.120	27.626	77.896	228.23

2.8061	6.6813	14.850	28.596	81.904	241.48

2.9424	7.2681	15.609	29.689	86.127	255.14

3.0843	7.8872	16.413	30.949	90.577	268.75

3.2350	8.6167	17.263	32.383	95.258	282.86

3.3966	9.3992	18.123	33.939	100.15	299.56

3.5613	10.248	19.070	35.613	105.32	315.63

3.7340	11.175	20.060	38.158	110.76	333.66

3.9154	12.171	21.104	39.795	116.47	350.45

4.1074	13.253	22.194	43.116	122.47	367.83

4.3098	14.418	23.316	45.254	128.79	385.53

4.5216	15.642	24.521	47.279	135.46	404.14

4.7453	16.815	25.781	50.383	142.44	422.36

4.9796	17.814	27.096	54.558	149.78	440.94

5.2271	18.426	28.500	58.701	157.51	458.92

5.4886	18.801	29.969	62.742	165.67	479.01

5.7648	19.128	31.513	67.513	174.22	500.25

6.0550	19.550	33.136	72.522	183.21	523.36

6.3600	19.958	34.840	77.919	192.66	547.47

6.6920	20.284	36.640	83.673	202.60	573.09

7.0362	20.636	38.527	90.122	213.06	599.83

7.3748	20.985	40.514	96.890	224.05	627.23

7.7499	21.301	42.598	104.02	235.60	650.55

8.1449	21.678	44.799	111.37	247.76	674.67

8.5603	22.030	47.115	119.20	260.54	699.72

8.9986	22.427	49.545	127.73	273.97	727.75

9.4579	22.838	52.098	136.98	288.02	763.61

9.9418	23.320	54.786	146.47	302.66	796.67

10.452	23.788	57.607	156.60

10.987	24.289	60.578	167.21

Table S3. Measured heat capacity for Ba-pharmacosiderite (composition Ba0.702Fe4[(AsO4)0.953(SO4)0.047]3(OH)3.455O0.545·5.647H2O), molecular mass 899.7194 g·mol–1. Temperature (T) in K, heat capacity (Cp) in J·mol–1·K–1.

T	Cp	T	Cp	T	Cp

2.2208	1.4848	12.779	37.876	31.512	66.448

2.3268	1.6413	12.958	38.992	33.130	71.138

2.4374	1.8083	13.210	40.431	34.836	76.108

2.5547	1.9894	13.437	41.642	36.632	81.493

2.6785	2.1869	13.463	41.971	38.522	87.447

2.8076	2.3973	13.715	43.640	40.508	93.788

2.9427	2.6315	13.966	45.100	42.594	100.58

3.0852	2.8823	14.124	46.038	44.790	107.88

3.2359	3.1755	14.216	46.761	47.104	115.73

3.3986	3.4919	14.474	48.196	49.530	124.07

3.5626	3.8285	14.731	49.706	52.085	133.10

3.7354	4.2012	14.841	50.727	54.766	142.74

3.9175	4.6020	14.984	51.417	57.597	152.49

4.1090	5.0337	15.231	52.087	60.567	163.07

4.3116	5.4985	15.482	51.546	63.692	174.17

4.5254	6.0048	15.590	51.240	66.981	186.04

4.7492	6.5475	15.729	50.282	70.437	197.64

4.9855	7.1631	15.978	48.133	74.067	210.28

5.2344	7.8141	16.221	46.456	77.888	223.23

5.4964	8.5292	16.397	44.820	81.902	235.55

5.7732	9.2907	16.494	44.198	86.126	250.79

6.0641	10.147	16.743	43.897	90.574	265.70

6.3719	11.031	16.996	43.084	95.236	282.44

6.7033	12.078	17.242	42.468	100.16	297.39

7.0507	13.187	17.243	42.549	105.31	316.95

7.3835	14.309	17.494	42.212	110.75	334.45

7.7594	15.613	17.754	41.541	116.46	352.66

8.1562	17.026	18.009	41.154	122.47	370.11

8.5719	18.568	18.119	41.896	128.79	390.25

9.0106	20.275	18.249	41.523	135.44	410.79

9.4700	22.127	18.507	41.638	142.43	430.08

9.9543	24.167	18.769	41.472	149.77	449.17

10.181	25.181	19.015	41.772	157.46	472.47

10.434	26.285	19.046	41.925	165.63	493.08

10.461	26.451	19.269	41.872	174.19	515.16

10.686	27.444	19.524	41.993	183.17	538.15

10.938	28.619	19.777	42.227	192.63	561.54

10.999	28.916	20.028	42.692	202.57	584.04

11.190	29.829	20.052	42.512	213.03	606.30

11.443	31.028	21.087	43.791	224.03	630.28

11.564	31.613	22.175	44.425	235.58	651.16

11.695	32.283	23.306	47.030	247.74	673.78

11.944	33.634	24.508	48.827	260.51	697.08

12.156	34.624	25.765	52.179	273.90	722.71

12.196	34.950	27.095	55.513	287.90	750.87

12.449	36.299	28.494	58.560	302.45	772.65

12.703	37.688	29.963	62.269

Table S4. Smoothed thermodynamic functions for K-pharmacosiderite (composition K1.086Fe4[(AsO4)0.953(SO4)0.047]3 (OH)3.772O0.228·4.432H2O), molecular mass 824.2076 g·mol–1., calculated from the measured heat capacity (see Table S2).

T	Cp	HT-H0	S	GT-G0

K	J·mol–1·K–1	J·mol–1	J·mol–1·K–1	J·mol–1

0	0	0	0	0

5.0	17.72	34.02	11.35	-22.73

10.0	23.39	138.8	25.67	-117.9

15.0	28.78	268.2	36.09	-273.2

20.0	37.47	432.6	45.49	-477.2

25.0	49.67	649.6	55.12	-728.5

30.0	63.37	931.8	65.38	-1030

35.0	77.97	1285	76.23	-1383

40.0	93.82	1714	87.66	-1793

45.0	111.3	2226	99.7	-2261

50.0	130.1	2829	112.4	-2791

55.0	148.9	3527	125.7	-3386

60.0	166.5	4316	139.4	-4048

65.0	182.8	5189	153.4	-4780

70.0	200.6	6147	167.6	-5583

75.0	218.0	7194	182.0	-6456

80.0	234.8	8326	196.6	-7403

85.0	251.3	9542	211.3	-8423

90.0	267.3	10840	226.2	-9516

95.0	283.2	12210	241.0	-10680

100.0	299.0	13670	256.0	-11930

110.0	330.2	16820	285.9	-14640

120.0	360.6	20270	316.0	-17650

130.0	389.4	24020	346.0	-20960

140.0	416.2	28050	375.8	-24570

150.0	441.3	32340	405.4	-28470

160.0	465.4	36880	434.7	-32670

170.0	489.6	41650	463.6	-37160

180.0	514.5	46670	492.3	-41940

190.0	540.3	51940	520.8	-47010

200.0	566.8	57480	549.2	-52360

210.0	592.7	63280	577.5	-57990

220.0	617.2	69330	605.6	-63910

230.0	639.5	75610	633.6	-70110

240.0	659.7	82110	661.2	-76580

250.0	678.6	88800	688.5	-83330

260.0	698.0	95690	715.5	-90350

270.0	719.4	102800	742.3	-97640

273.15	726.7	105000	750.6	-99990

280.0	743.2	110100	768.8	-105200

290.0	768.0	117600	795.4	-113000

298.15	787.1	124000	816.9	-119600

300.0	791.1	125400	821.8	-121100

Table S5. Fitting functions used to integrate heat capacity of K-pharmacosiderite (see Table S2 for the data and Table S4 for the result of integration). All functions are polynomials of the form Cp =  anT n. The exponents n and coefficients an are listed in the Table.

fit 1: polynomial from T = 0.0 to T = 4.9 K

exponent n	coefficient an

1.0	1.24623055153

3.0	0.165991131938

5.0	-0.00287207020945

fit 2: polynomial from T = 4.9 to T = 19.0 K

exponent n	coefficient an

0.0	-138.705292068

1.0	101.85993035

2.0	-27.8200457497

3.0	4.14474858941

4.0	-0.360308880387

5.0	0.0182720609325

6.0	-0.000500602950073

7.0	5.72425797346e-06

fit 3: polynomial from T = 19.0 to T = 63.47 K

exponent n	coefficient an

0.0	-16.4374675729

1.0	12.70863738

2.0	-1.70908648216

3.0	0.121392446586

4.0	-0.00466811234888

5.0	0.000104523454143

6.0	-1.3540917529e-06

7.0	9.37874484995e-09

8.0	-2.68178441905e-11

fit 4: polynomial from T = 63.47 to T = 305.0 K

exponent n	coefficient an

0.0	3656.49027305

1.0	-287.672494133

2.0	9.86368504281

3.0	-0.189437648297

4.0	0.00228574206678

5.0	-1.8124284516e-05

6.0	9.57618106365e-08

7.0	-3.33529353403e-10

8.0	7.34556581939e-13

9.0	-9.26132951976e-16

10.0	5.08958501261e-19

Table S6. Smoothed thermodynamic functions for Ba-pharmacosiderite (composition Ba0.702Fe4[(AsO4)0.953(SO4)0.047]3(OH)3.455O0.545·5.647H2O), molecular mass 899.7194 g·mol–1., calculated from the measured heat capacity (see Table S3).

T	Cp	HT-H0	S	GT-G0

K	J·mol–1·K–1	J·mol–1	J·mol–1·K–1	J·mol–1

0	0	0	0	0

5.0	7.107	12.57	3.887	-6.871

10.0	24.44	87.77	13.63	-48.55

15.0	51.46	272.8	28.27	-151.3

20.0	41.83	494.2	41.09	-327.5

25.0	50.97	723.6	51.29	-558.5

30.0	62.51	1007	61.59	-840.6

35.0	75.81	1352	72.18	-1175

40.0	92.06	1770	83.34	-1563

45.0	109.6	2274	95.2	-2009

50.0	126.1	2864	107.6	-2516

55.0	142.0	3534	120.4	-3086

60.0	161.2	4290	133.5	-3721

65.0	178.6	5139	147.1	-4422

70.0	195.9	6076	161.0	-5192

75.0	213.0	7098	175.1	-6032

80.0	230.2	8206	189.4	-6943

85.0	247.3	9400	203.8	-7926

90.0	264.3	10680	218.4	-8982

95.0	281.2	12040	233.2	-10110

100.0	298.1	13490	248.0	-11310

110.0	331.1	16640	278.0	-13940

120.0	363.2	20110	308.2	-16870

130.0	394.0	23900	338.5	-20110

140.0	423.4	27980	368.8	-23640

150.0	451.5	32360	399.0	-27480

160.0	478.5	37010	429.0	-31620

170.0	504.6	41930	458.8	-36060

180.0	529.9	47100	488.3	-40800

190.0	554.4	52520	517.6	-45830

200.0	578.0	58190	546.7	-51150

210.0	600.5	64080	575.4	-56760

220.0	621.7	70190	603.9	-62660

230.0	641.5	76510	631.9	-68840

240.0	660.0	83020	659.6	-75290

250.0	677.8	89710	686.9	-82030

260.0	695.7	96570	713.9	-89030

270.0	714.6	103600	740.5	-96300

273.15	720.9	105900	748.8	-98650

280.0	735.0	110900	766.8	-103800

290.0	755.4	118300	793.0	-111600

298.15	768.7	124500	814.1	-118200

300.0	770.7	126000	818.9	-119700

Table S7. Fitting functions used to integrate heat capacity of Ba-pharmacosiderite (see Table S3 for the data and Table S6 for the result of integration). All functions are polynomials of the form Cp =  anT n. The exponents n and coefficients an are listed in the Table.

fit 1: polynomial from T = 0.0 to T = 15.18 K

exponent n	coefficient an

1.0	0.0492843666889

2.0	0.330221604706

3.0	-0.0132451069419

4.0	0.000417148183755

fit 2: polynomial from T = 15.18 to T = 60.0 K

exponent n	coefficient an

0.0	1534.41817363

1.0	-302.396566391

2.0	25.2646807292

3.0	-1.13500568926

4.0	0.0297492917765

5.0	-0.000454180483929

6.0	3.74152309564e-06

7.0	-1.28479216135e-08

fit 3: polynomial from T = 60.0 to T = 305.0 K

exponent n	coefficient an

0.0	-99.8250082674

1.0	4.83846584516

2.0	0.0421913146894

3.0	-0.0023166606727

4.0	4.26061322896e-05

5.0	-4.15307441163e-07

6.0	2.34506337849e-09

7.0	-7.70407961485e-12

8.0	1.36717874219e-14

9.0	-1.01313790912e-17