Suppl. Table 1. Summary of APT runs performed on multiple tips and run conditions.

| Run Number | Description | Laser Energy (pJ) | Sample Stage Temperature (K) | Target Detection Rate (%) | Pule Rate (kHz) | Ions Collected (x106) |
| --- | --- | --- | --- | --- | --- | --- |
| R47_02740 | Preston (Au EGH-PR3) | 50 | 59.6 | 0.5 | 125 | 6.5 |
| R47_02741 | Preston (Au EGH-PR3) | 70 | 59.6 | 0.5 | 125 | 1.7 |
| R47_02743 | Preston (Au EGH-PR3) | 110 | 59.6 | 0.2 | 125 | 0.3 |
| R47_02784 | Preston (Au EGH-PR3) | 60 | 59.6 | 0.2 | 100 | 3.7 |
| R47_02786 | Preston (Au EGH-PR3) | 60 | 59.6 | 0.3 | 125 | 0.5 |
| R47_02744 | McLaughlin (Spot 3) | 35 | 59.6 | 0.3 | 125 | 0.9 |
| R47_02745 | McLaughlin (Spot 3) | 20 | 59.6 | 0.2 | 100 | 0.07 |
| R47_02747 | McLaughlin (Spot 3) | 50 | 59.6 | 0.2 | 125 | 0.7 |
| R47_02791 | McLaughlin (Spot 3) | 60 | 59.6 | 0.2 | 125 | 2.5 |
| R47_02788 | McLaughlin (Spot 3) | 60 | 59.6 | 0.2 | 125 | 5.5 |